Table S1  IKP for several combinations of kinetic models for BHMPD

| Kinetic model | Einv / kJ mol1 | ln Ainv A/s1 | r |
| --- | --- | --- | --- |
| AKM | 90.81 | 19.27 | 0.998 |
| AKM{F3; D1; D2; D3; D4} | 92.12 | 19.85 | 0.986 |
| AKM{F2; F3; D1; D2; D3; D4} | 91.02 | 19.41 | 0.988 |
| AKM–{F1; F2; F3; D1; D2; D3; D4; A2; A3; A4; R2; R3} | 107.59 | 26.30 | 0.979 |
| AKM–{F1; F2; F3; D1; D2; D3; D4; A2; R2; R3} | 105.13 | 26.09 | 0.981 |
| AKM–{F1; F2; F3; D1; D2; D3; D4; R2; R3} | 103.49 | 24.84 | 0.979 |
| AKM–{P2; P3; P4; F2; F3; D1; D2; D3; D4; A2; A3; A4} | 104.19 | 23.47 | 0.959 |
| AKM–{P4; F1; F2; F3; D1; D2; D3; D4; A2; R2; R3} | 103.06 | 24.39 | 0.988 |

Table S2  IKP for several combinations of kinetic models for BHMBC

| Kinetic model | Einv / kJ mol1 | ln Ainv A/s1 | r |
| --- | --- | --- | --- |
| AKM | 128.99 | 21.68 | 0.976 |
| AKM–{F2; F3; D1; D2; D3; D4; R2; R3} | 128.75 | 22.05 | 0.999 |
| AKM–{F2; F3; D1; D2; D3; D4; A2; R2; R3} | 127.20 | 21.68 | 0.988 |
| AKM–{P2; P3; P4; F2; F3; D1; D2; D3; D4; R2; R3} | 128.40 | 21.93 | 0.988 |
| AKM–{P4; F2; F3; D1; D2; D3; D4; A2; A3; A4; R2; R3} | 127.13 | 21.63 | 0.985 |
| AKM–{P2; P3; P4; D1; D2; D3; D4; A2; A3; A4; R2; R3} | 125.62 | 21.28 | 0.996 |

Figure S1  TG and DTA curves of BHMPD at (a) 10 K min–1; (b) 15 K min–1; (c) 20 K min–1 heating rates in nitrogen atmosphere

Figure S2  TG and DTA curves of BHMBC at (a) 10 K min–1; (b) 15 K min–1; (c) 20 K min–1 heating rates in nitrogen atmosphere

0.6

0.5

[1-(1-)1/2]

0.4

0.3

10 K/min-1

15 K/min-1

20 K/min-1

0.2

0.1

0.00E+00

2.00E-10

4.00E-10

6.00E-10

8.00E-10

Ea p(x)/R

Figure S3  Determination of A value by plotting [1-(1-)1/2] against Ea p(x)/R for the decomposition process of BHMPD at the different heating rates ().