Supplementary report

L-valine functionalized ionic liquid catalyzed esterification reaction under green approach

Parasuraman Karthikeyana, Prashant Narayan Muskawara, Sachin Arunrao Aswara, Pundlik Rambhau Bhagat a,*, S. Senthil kumara, Pranveer S Satvatb, Brijesh Nair A Nb

Structure of L-valine amido ethyl methyl imidazolium bromide [L-Vaemim]Br

Preparation of [L-Vaemim]Br ionic liquid

A mixture of Boc-valine (2.42 g, 11.0 mmol) and triethyl amine (2.23 g, 22.0 mmol) in tetrahydrofuran was cooled in an ice-bath. The 1-carboxy ethyl-3-methyl imidazolium bromide [Cemim]Br (2.05 g, 10.0 mmol) was added to this mixture, after 24 h stirring at room temperature. And then unreacted starting material was removed by adding CHCl3 to this solution this process was repeated three times. The viscous liquid washed with chloroform-ether. The organic layer was dried over Na2SO4 and concentrated. Then solvent was removed using rotator vapour and ionic liquid was dried under vacuum 80 OC 6 hrs.

The BOC-protected [L-Aaemim]Br deprotected was performed using 50% TFA in dichloromethane (5 mL) for 1 h at room temperature. After rotary evaporation, TFA salts were removed by triturating the viscous liquid with 5mL of methanol (saturated with ammonia), then solvent was removed using rotator vapour and ionic liquid was dried under vacuum 80 OC 3 hrs.

Spectral data for L-valine amido ethyl methyl imidazolium bromide [L-Vaemim] Br; 1H-NMR (DMSO-d6): 3.5(s, 3H),7.3(d, 1H), 6.8(d,1H), 8.2 (s, 1H), 5.1(t, 2H), 2.4(t, 2H), 7.9(s, 1H), 4.2(d, 1H), 1.7(m, 1H), 0.9 (d, 6H), 10.3(s,1H). 13C-NMR: (DMSO-d6): 36.56, 128.30, 128.90, 140.65, 54.45, 23.02, 177.01, 184.35, 65.96, and 20.97.

1H-NMR of L-valine amido ethyl methyl imidazolium bromide [L-Vaemim]Br

13C-NMR of L-valine amido ethyl methyl imidazolium bromide [L-Vaemim]Br