Supporting Information

Synthesis and Characterization of High Wash Fastness Novel Azo Reactive Dyes incorporating Novel Bridged Diamines

Aamer Saeed and Ghulam Shabir

Figure 3.1 Combined U.V Visible Spectrum of MCT Dye S1-S10

Figure 4.1 FTIR Spectrum of 4,4'-methylenebis(2-aminophenol)

Figure 4.2 FTIR Spectrum of 2,2'-methylenebis(4-aminophenol)

Figure 4.3 FTIR Spectrum of 5,5'-methylenebis(2-methoxyaniline)

Figure 4.4 FTIR Spectrum of 5,5'-methylenebis(3-nitroaniline)

Figure 4.5 FTIR Spectrum of 6,6'-methylenebis(2-amino-4-nitrophenol)

Figure 4.6 FTIR Spectrum of 6,6'-methylenebis (2-amino-4-chlorophenol)

Figure 4.7 FTIR Spectrum of 6,6'-methylenebis(3-chloroaniline)

Figure 4.8 FTIR Spectrum 5,5'-methylenebis(2-aminobenzoic acid)

Figure 4.9 FTIR Spectrum 5,5'-methylenebis(3-aminobenzoic acid)

Figure 4.10 FTIR Spectrum 5,5'-methylenebis(4-aminobenzoic acid)

Figure 4.11 FTIR Spectrum of MCT Reactive Dye S1

Figure 4.12 FTIR Spectrum of MCT Reactive Dye S2

Figure 4.13 FTIR Spectrum of MCT Reactive Dye S3

Figure 4.14 FTIR Spectrum of MCT Reactive Dye S4

Figure 4.15 FTIR Spectrum of MCT Reactive Dye S5

Figure 4.16 FTIR Spectrum of MCT Reactive Dye S6

Table S1. Characterization data of dyes S1 to S10

| Dye | Molecular Formula | Mol. Wt | yield% | C% Cal/Found | H% Cal/Found | N% Cal/Found | S% Cal/Found | Rf* Value |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| S1 | C53Cl2H34N15O21S5 | 1447 | 75.32 | 43.95/43.35 | 2.34/2.30 | 14.51/14.35 | 11.05/10.98 | 0.55 |
| S2 | C53Cl2H34N15O21S5 | 1447 | 76.11 | 43.95/43.10 | 2.34/2.26 | 14.51/14.32 | 11.05/10.95 | 0.54 |
| S3 | C53Cl2H34N15O21S5 | 1447 | 75.65 | 43.95/43.68 | 2.34/2.28 | 14.51/14.38 | 11.05/10.80 | 0.55 |
| S4 | C51Cl2H34N15O19S5 | 1391 | 81.15 | 43.99/43.55 | 2.44/2.40 | 15.09/15.00 | 11.50/10.85 | 0.47 |
| S5 | C51Cl2H34N15O19S5 | 1391 | 80.72 | 43.99/42.95 | 2.44/2.43 | 15.09/14.93 | 11.50/10.97 | 0.49 |
| S6 | C51Cl2H32N17O23S5 | 1481 | 83.22 | 41.32/40.53 | 2.16/2.05 | 16.07/15.90 | 10.80/11.00 | 0.45 |
| S7 | C51Cl4H32N15O19S5 | 1460 | 85.71 | 41.91/40.70 | 2.19/2.15 | 14.38/14.05 | 10.95/10.91 | 0.41 |
| S8 | C51Cl2H32N17O21S5 | 1449 | 78.77 | 42.23/42.06 | 2.20/2.12 | 16.42/16.22 | 11.04/10.97 | 0.43 |
| S9 | C51Cl2H36N15O19S5 | 1393 | 84.57 | 43.93/42.33 | 2.58/2.56 | 15.07/14.99 | 11.48/11.30 | 0.43 |
| S10 | C51Cl4H32N15O17S5 | 1428 | 80.43 | 42.85/41.35 | 2.24/2.18 | 14.71/14.50 | 11.20/11.15 | 0.39 |

*Toluene: Ethyl acetate (7.5: 2.5 v/v), Silica gel-G F254 TLC plate.

Table S2. Dye-bath containing materials

| Materials | Cotton |
| --- | --- |
| Fabric | 0.5g |
| Amount of Dye | 25mg |
| Sodium Sulfate | 1ml (25% W/V) |
| Sodium Carbonate | 1ml (10% W/V) |
| Sodium Chloride | 1ml (10% W/V) |
| EDTA | 1ml (10% W/V) |
| pH | 8.5-9.0 |
| Dyeing Time | 1h |
| Dyeing Temperature | 80 oC |
| Total Volume | 20 ml |