SUPPORTING INFORMATION

Fig. S1  Comparison of photocatalytic degradation of 1,2-dichlorobenzene using photocatalyst A:T850/SnO2/WO3, B:T950/SnO2/WO3 and C:T1050/SnO2/WO3 under UV (λ = 365 nm, 12 watt) and fluorescence visible light source (λ > 400 nm, 36 watt) for 4 hours.

(a)

(b)

(c)

(d)

Fig. S2  HRTEM image for T950/SnO2/WO3 and the d-spacing for (a)TiO2 (111), (b) TiO2 (101), (c) SnO2 (101) and (d) WO3 (101).

- Fig. S3 UV absorbance spectrum for photocatalytic degradation of 1,2-dichlorobenzene under visible light for 4 hours using T950/SnO2/WO3 photocatalyst immobilized on PVC. [DCB]=100ppm

- Fig. S4 (i) Adsorption in dark and (ii) photocatalytic degradation of 1,2-dichlorobenzene T950/SnO2/WO3 immobilized on PVC film for 4 hours. [DCB]=100 ppm

- Fig. S5 GCMS chromatography for the decomposition of 1,2-dichlorobenzene (DCB) before and after 4 hours irradiation under visible light using T950/SnO2/WO3 photocatalyst supported on PVC.

Table 3  Box–Behnken design experiments and experimental results

| No. of Run | Calcination Temperature (°C) | Catalyst Loading (g) | pH | Observed Response (%) | Predicted Response (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | 850 | 0.25 | 5 | 86.71 | 86.69 |
| 2 | 850 | 0.20 | 7 | 87.14 | 87.12 |
| 3 | 850 | 0.40 | 7 | 85.60 | 85.68 |
| 4 | 850 | 0.25 | 9 | 87.10 | 87.06 |
| 5 | 950 | 0.10 | 5 | 91.67 | 91.71 |
| 6 | 950 | 0.40 | 5 | 89.68 | 89.63 |
| 7 | 950 | 0.25 | 7 | 95.52 | 95.70 |
| 8 | 950 | 0.25 | 7 | 95.49 | 95.70 |
| 9 | 950 | 0.25 | 7 | 95.89 | 95.70 |
| 10 | 950 | 0.25 | 7 | 95.73 | 95.70 |
| 11 | 950 | 0.25 | 7 | 95.86 | 95.70 |
| 12 | 950 | 0.10 | 9 | 92.10 | 92.15 |
| 13 | 950 | 0.40 | 9 | 90.57 | 90.53 |
| 14 | 1050 | 0.25 | 5 | 88.73 | 88.77 |
| 15 | 1050 | 0.10 | 7 | 89.98 | 89.90 |
| 16 | 1050 | 0.40 | 7 | 87.63 | 87.65 |
| 17 | 1050 | 0.25 | 9 | 89.71 | 89.73 |

Table 4  Analysis of variance (ANOVA) for photocatalytic efficiency from Box-Behnken Design

| Source | Sum of Squares | Degree of Freedom | Mean Square | F-value | p-value Prob > F | Remark |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 210.60 | 9 | 23.40 | 1000.56 | <0.0001 | significant |
| A-Calcination Temp. | 11.28 | 1 | 11.28 | 482.38 | <0.0001 |  |
| B-Catalyst Loading | 6.86 | 1 | 6.86 | 293.48 | <0.0001 |  |
| C-pH | 0.90 | 1 | 0.90 | 38.68 | 0.0004 |  |
| AB | 0.16 | 1 | 0.16 | 7.01 | 0.0330 |  |
| AC | 0.087 | 1 | 0.087 | 3.72 | 0.0951 |  |
| BC | 0.053 | 1 | 0.053 | 2.26 | 0.1763 |  |
| A2 | 128.60 | 1 | 128.60 | 5498.86 | <0.0001 |  |
| B2 | 28.11 | 1 | 28.11 | 1202.15 | <0.0001 |  |
| C2 | 18.73 | 1 | 18.73 | 800.80 | <0.0001 |  |
| Residual | 0.16 | 7 | 0.023 |  |  |  |
| Lack of Fit | 0.025 | 3 | 8.208E-003 | 0.24 | 0.8673 | not significant |
| Pure Error | 0.14 | 4 | 0.035 |  |  |  |
| Cor. Total | 210.76 | 16 |  |  |  |  |

R2 = 99.92%; Adj. R2 = 99.82%; R2 = 99.71%