Supplementary Information

Figure S1a N2 adsorption-desorption isotherms for 20Fe-Al-CP catalysts calcined at different temperatures

Figure S1b N2 adsorption-desorption isotherms for 20Fe-Al-Imp catalysts calcined at different temperatures

Figure S1a Carbon yield for 20Fe-Al-CP catalysts calcined at different temperatures

Figure S1b Carbon yield for 20Fe-Al-Imp catalysts calcined at different temperatures

Table S1: Effect of calcination temperature on textural properties for 20 wt %Fe/Al2O3 supported catalysts.

| Catalyst preparation method | Calcination Temp. (°C) | SBET (m2/g)a | P.V (Cm3/g)a | P.D (nm)a | SBET (m2/g)b | P.V (Cm3/g)b | P.D (nm)b |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Co-precipitation | 300 | 301.9 | 0.20 | 3.3 | 150.2 | 0.6556 | 18.2 |
|  | 400 | 245.6 | 0.26 | 3.9 | 120.1 | 0.1409 | 6.0 |
|  | 500 | 237.0 | 0.27 | 4.2 | 188.5 | 0.7669 | 16.7 |
|  | 800 | 104.1 | 0.31 | 11.0 | 115.8 | 0.2817 | 11.2 |
| Impregnation | 300 | 209.4 | 0.38 | 6.8 | 177.5 | 0.7112 | 16.5 |
|  | 400 | 178.2 | 0.44 | 8.9 | 131.0 | 0.5901 | 17.9 |
|  | 500 | 155.5 | 0.37 | 8.7 | 126.5 | 0.5566 | 17.6 |
|  | 800 | 93.5 | 0.35 | 13.8 | 122.6 | 0.5990 | 19.8 |

a: Textural properties for 20Fe-Al catalysts before reaction; b: Textural properties for 20Fe-Al catalysts after reaction.