Supporting Information

for

Magnetically recoverable -Fe2O3 nanoparticles as a sustainable and highly active catalyst for Friedel–Crafts benzoylation reaction under ultrasound irradiation

Table of contents

Section S1	Syntheses of Materials						S2-S3

Section S2	Recycling of -Fe3O4 nanoparticles				S3

Section S3    1H and 13C NMR, GC-MS Data					S4-S8

Section S4    References 					S8

Section S5	1H and 13C NMR spectra                        				S10-S22

Section S1. Syntheses of Materials

Methods:

Chemicals and supplies. Anisole (analytical standard, ≥ 99.9%), benzoyl chloride (≥ 99%), benzene (≥ 99%), 1,2-dimethoxybenzene (≥ 99%), ethoxybenzene (≥ 99%), 1,3-dimethoxybenzene (> 98%), 1,4-dimethoxybenzene (assay > 99%), 1,2,4-trimethoxybenzene (≥ 97%), mesitylene (GC, ≥ 99%), m-xylene (≥ 98%), p-xylene (≥ 99%), anthracene (≥ 97%), naphthalene (≥ 99%), 1-methylnaphthalene (≥ 95%) were purchased from Sigma-Aldrich. Silica gel 230–400 mesh (for flash chromatography) was obtained from HiMedia Laboratories Pvt. Ltd. (India). TLC (silica gel 60 F254) was bought from Merck. Ethyl acetate (≥ 99.5%), petrolium ether 60 – 90, chloroform (≥ 99%) were from Xilong Chemical Co., Ltd (China). Chloroform-d, 99.8% was obtained from Armar (Switzerland).

All starting materials, reagents and solvents were directly used without further purification.

Analytical instruments.

For ultrasound reaction, the ultrasonic bath Elma S30H was used. Powder X-ray diffraction (PXRD) patterns were recorded using a Bruker D8 Advance operated at 40 kV and 40 mA with a Ni filtered Cu Kα radiation (λ = 1.54178 Å) source, scanning rate 2 per min and 2θ angle ranging from 10 to 70. The morphology of the sample was examined by transmission electron microscopy (TEM) using JEOL JEM 1400 with operating voltage at 100 kV. The magnetization of the sample was measured in the varied magnetic field between −16 and 16 kOe at room temperature using a vibrating sample magnetometer (VSM/Microsense, EV11, USA). Ultrasound irradiation was performed on an Elma apparatus. GC-MS analyses were performed on an Agilent GC System 7890 equipped with a mass selective detector Agilent 5973N and a capillary DB-5MS column (30 m × 250 μm × 0.25 μm). The 1H and 13C NMR spectra were recorded on a Bruker Advance 500 using CDCl3 as the solvent and solvent peaks or TMS as the internal standards.

Section S2. Recycling of -Fe2O3 nanoparticles

The recycling of -Fe2O3 nanoparticles catalyst was carried out in the Friedel-Crafts benzoylation of anisole under sonification for 120 min. The recovery of catalyst is easy by external magnet. Due to its high stability in our method, -Fe2O3 nanoparticles catalyst was easily recovered in a quantitative yield. After being washed with ethyl acetate, the catalyst was dried under vacuum and used for next cycle without further purification. Owning the easy of recovery and stability under this method, -Fe2O3 nanoparticles catalyst was reused over six consecutive times without any significant loss in reactivity and regioselectivity. This is promising for its application on industrial processes. The process for recycling -Fe2O3 nanoparticles is simple and effective so it could be applied on a large scale.

Section S3. 1H and 13C NMR, GC-MS data

Benzophenone 1,2,4

1H NMR (500 MHz, CDCl3): δ 7.81 – 7.59 (m, 4H), 7.55 (m, 2H), 7.45 (m, 4H).

13C NMR (125 MHz, CDCl3): δ 196.7, 137.6, 132.4, 130.1, 128.3.

GC-MS (EI, 70 eV) m/z: 182 ([M]+)

4-methoxybenzophenone1,3,6

1H NMR (300 MHz, CDCl3): δ 7.86-7.81 (m, 2H), 7.75 (dd, J = 8.3, 1.4 Hz, 2H), 7.55 (d, J = 7.5 Hz, 1H), 7.49-7.44 (m, 2H), 6.96 (d, J = 9.0 Hz, 2H), 3.88 (s, 3H).

13C NMR (75 MHz, CDCl3) δ 195.6, 163.2, 138.3, 132.6, 131.9, 130.2, 129.8, 128.2, 113.6, 55.5.

GC-MS (EI, 70 eV): m/z 212 (M+).

3,4-dimethoxybenzophenone5

1H NMR (300 MHz, CDCl3): δ 7.77 (dd, J = 8.4, 1.4 Hz, 2H), 7.49 (s, 1H), 7.46-7.36 (m, 3H), 6.90 (m, 2H), 3.96 (s, 3H), 3.95 (s, 3H).

13C NMR (75 MHz, CDCl3) δ 195.6, 153.0, 149.0, 138.3, 131.9, 130.2, 129.7, 128.2, 125.5, 112.1, 109.7, 56.1, 56.0.

GC-MS (EI, 70 eV): m/z 242 (M+).

2,4-dimethoxybenzophenone5

1H NMR (300 MHz, CDCl3): δ 7.77 (dd, J = 8.4, 1.4 Hz, 2H), 7.49 (s, 1H), 7.42 (dt, J = 1.8, 0.6 Hz, 1H), 7.39 (s, 2H), 6.53 (dd, J = 9.6, 5.3 Hz, 2H), 3.86 (s, 3H), 3.69 (s, 3H).

13C NMR (75 MHz, CDCl3) δ 195.6, 163.4, 159.6, 138.8, 132.3, 132.2, 129.7, 128.0, 121.5, 104.6, 98.8, 55.6, 55.5.

GC-MS (EI, 70 eV): m/z 242 (M+).

2, 5-dimethoxybenzophenone4,5

1H NMR (300 MHz, CDCl3): δ 7.84-7.80 (m, 2H), 7.57-7.52 (m, 1H), 7.47-7.38 (m, 2H), 7.01 (dd, J = 9.0, 3.0 Hz, 1H), 6.92 (dd, J = 6.0, 3.0 Hz, 2H), 3.78 (s, 3H), 3.66 (s, 3H).

13C NMR (75 MHz, CDCl3) δ 196.2, 153.5, 151.5, 137.6, 133.0, 129.8, 128.2, 117.3, 114.4, 113.1, 56.3, 55.8.

GC-MS (EI, 70 eV): m/z 242 (M+).

2, 4, 5-trimethoxybenzophenone4

1H NMR (500 MHz, CDCl3): δ 7.76 (d, J = 8.2 Hz, 2H), 7.51 (t, J = 6.8 Hz, 1H), 7.40 (t, J = 7.6 Hz, 2H), 7.02 (s, 1H), 6.55 (s, 1H), 3.94 (s, 3H), 3.83 (s, 3H), 3.64 (s, 3H).

13C NMR (125 MHz, CDCl3): δ 195.5, 153.4, 152.6, 143.3, 139.0, 132.3, 130.1, 129.5, 128.4, 128.0, 120.1, 113.6, 97.8, 56.6, 56.5, 56.2.

GC-MS (EI, 70 eV): m/z 272 (M+).

2, 4, 6-trimethylbenzophenone4

1H NMR (500 MHz, CDCl3): δ 7.80 (d, J = 7.2 Hz, 2H), 7.57 (t, J= 7.4 Hz, 1H), 7.44 (t, J = 7.8 Hz, 2H), 6.90 (s, 2H), 2.33 (s, 3H), 2.08 (s, 6H).

13C NMR (125 MHz, CDCl3) δ 200.8, 138.5, 137.4, 136.9, 134.2, 133.5, 129.4, 128.8, 128.4, 21.2, 19.4.

GC-MS (EI, 70 eV): m/z 223 (M+H).

2, 4-dimethylbenzophenone3

1H NMR (500 MHz, CDCl3): δ 7.77 (dd, J = 8.3, 1.2 Hz, 2H), 7.54 (t, J = 7.4 Hz, 1H), 7.42 (m, 2H), 7.21 (d, J = 7.7 Hz, 1H), 7.09 (s, 1H), 7.02 (d, J = 7.7 Hz, 1H), 2.36 (s, 3H), 2.31 (s, 3H).

13C NMR (125 MHz, CDCl3) δ 198.5, 140.6, 138.3, 137.3, 135.7, 132.8, 131.9, 130.1, 129.2, 128.4, 127.5, 125.8, 21.4, 20.1.

GC-MS (EI, 70 eV): m/z 210 (M+).

2, 5-dimethylbenzophenone3,8

1H NMR (500 MHz, CDCl3): δ 7.82 – 7.80 (m, 2H), 7.80 – 7.56 (m, 1H), 7.47 – 7.44 (m, 2H), 7.21 – 7.17 (m, 2H), 7.13 (s, 1H), 2.34 (s, 3H), 2.28 (s, 3H).

13C NMR (125 MHz, CDCl3) δ 198.9, 138.6, 137.8, 134.8, 133.4, 133.0, 130.9, 130.8, 130.1, 128.9, 128.4, 121.3, 20.8, 19.5.

GC-MS (EI, 70 eV): m/z 210 (M+).

1-benzoylnaphthalene4,7

1H NMR (500 MHz, CDCl3) δ 8.09 (d, J = 9.1 Hz, 1H), 8.01 (d, J = 8.2 Hz, 1H), 7.93 (d, J = 7.3 Hz, 1H), 7.87 (dd, J = 8.4, 1.3 Hz, 2H), 7.64 – 7.56 (m, 2H), 7.57 – 7.49 (m, 3H), 7.46 (dd, J = 8.0, 7.5 Hz, 2H).

13C NMR (125 MHz, CDCl3) δ 196.9, 138.1, 135.4, 135.0, 132.5, 132.4, 132.0, 130.3, 129.6, 128.5, 128.5, 128.5, 128.0, 127.0, 125.9.

GC-MS (EI, 70 eV) m/z 232 ([M]+).

9-benzoylanthracene4,7

1H NMR (500 MHz, CDCl3) δ 8.57 (s, 1H), 8.07 (d, J = 8.5 Hz, 2H), 7.83 (d, J = 7.4 Hz, 2H), 7.73 (dd, J = 8.7, 0.5 Hz, 2H), 7.58 (t, J = 7.4 Hz, 1H), 7.53 – 7.44 (m, 2H), 7.40 (td, J = 8.1, 4.3 Hz, 4H).

13C NMR (125 MHz, CDCl3) δ 200.2, 138.2, 134.0, 131.1, 130.1, 128.9, 128.7, 128.4, 126.6, 125.5, 125.3.

GC-MS (EI, 70 eV) m/z 282 ([M]+).

2-benzoyl-1methylnaphthalene9

1H NMR (500 MHz, CDCl3) δ 8.18 (dd, J = 8.5, 0.5 Hz, 1H), 8.09 (d, J = 8.5 Hz, 1H), 7.87 – 7.85 (m, 2H), 7.60 – 7.56 (m, 2H), 7.53 – 7.43 (m, 4H), 7.36 (dd, J = 7.5, 0.5 Hz 1H), 2.78 (s, 3H).

13C NMR (125 MHz, CDCl3) δ 198.1, 138.7, 138.3, 134.7, 133.0, 132.9, 131.1, 130.4, 128.4, 128.0, 126.4, 126.3, 125.1, 124.4, 19.9.

GC-MS (EI, 70 eV) m/z 246 ([M]+).

4-ethoxybenzophenone10

1H NMR (500 MHz, CDCl3) δ 7.81 (d, J = 8.9 Hz, 2H), 7.75 (dd, J = 8.3, 1.3 Hz, 2H), 7.55 (t, J = 6.8 Hz, 1H), 7.47 (d, J = 7.7 Hz, 2H), 6.94 (d, J = 8.9 Hz, 2H), 4.12 (q, J = 7.0 Hz, 2H), 1.45 (t, J = 7.0 Hz, 3H).

13C NMR (125 MHz, CDCl3) δ 195.6, 162.7, 138.4, 132.6, 131.8, 130.0, 129.7, 128.2, 114.0, 63.8, 14.7.

GC-MS (EI, 70 eV) m/z 226 ([M]+).

Section S4. References

1.	Desmurs, J.; Labrouillere, M.; Le Roux, C.; Gaspard, H.; Laporterie, A.; Dubac, J., Surprising catalytic activity of bismuth (III) triflate in the Friedel-Crafts acylation reaction. Tetrahedron Letters 1997, 38 (51), 8871-8874.

2.	Sartori, G.; Maggi, R., Use of solid catalysts in Friedel-Crafts acylation reactions. Chemical Reviews 2006, 106 (3), 1077-1104.

3.	Earle, M.; Seddon, K.; Adams, C., Friedel–Crafts reactions in room temperature ionic liquids. Chemical Communications 1998,  (19), 2097-2098.

4.	Sharghi, H.; Jokar, M.; Doroodmand, M. M.; Khalifeh, R., Catalytic Friedel–Crafts acylation and benzoylation of aromatic compounds using activated hematite as a novel heterogeneous catalyst. Advanced Synthesis & Catalysis 2010, 352 (17), 3031-3044.

5.	Tran, P. H.; Duus, F.; Le, T. N., Friedel–Crafts acylation using bismuth triflate in [BMI][PF 6]. Tetrahedron Letters 2012, 53 (2), 222-224.

6.	Kantam, M. L.; Ranganath, K. V. S.; Sateesh, M.; Kumar, K. B. S.; Choudary, B. M., Friedel–Crafts acylation of aromatics and heteroaromatics by beta zeolite. Journal of Molecular Catalysis A: Chemical 2005, 225 (1), 15-20.

7.	Gopalakrishnan, M.; Sureshkumar, P.; Kanagarajan, V.; Thanusu, J., Aluminium metal powder (atomized) catalyzed Friedel–Crafts acylation in solvent-free conditions: A facile and rapid synthesis of aryl ketones under microwave irradiation. Catalysis Communications 2005, 6 (12), 753-756.

8.	Kozhevnikov, I., Friedel–Crafts acylation and related reactions catalysed by heteropoly acids. Applied Catalysis A: General 2003, 256 (1), 3-18.

9.	Gmouh, S.; Yang, H.; Vaultier, M., Activation of bismuth (III) derivatives in ionic liquids: Novel and recyclable catalytic systems for Friedel-Crafts acylation of aromatic compounds. Organic letters 2003, 5 (13), 2219-2222.

10.	Duris, F.; Barbier-Baudry, D.; Dormond, A.; Desmurs, J. R.; Bernard, J. M., Lanthanide bis (trifluoromethylsulfonyl) amides vs. trifluoromethylsulfonates as catalysts for Friedel–Crafts acylations. Journal of Molecular Catalysis A: Chemical 2002, 188 (1), 97-104.

Section 5. 1H and 13C NMR spectra

1H and 13C NMR of Benzophenone

1H and 13C NMR of 4-methoxyenzophenone

1H and 13C NMR of 3,4-dimethoxybenzophenone

1H and 13C NMR of 2,4-dimethoxybenzophenone

1H and 13C NMR of 2,5-dimethoxybenzophenone

1H and 13C NMR of 2,4,5-trimethoxybenzophenone

1H and 13C NMR of 2,4,6-trimethylbenzophenone

1H and 13C NMR of 2,4-dimethylbenzophenone

1H and 13C NMR of 2,5-dimethylbenzophenone

1H and 13C NMR of 1-benzoylnaphthalene

1H and 13C NMR of 9-benzoylanthracene

1H and 13C NMR of 2-benoyl-1methylnaphthalene

1H and 13C NMR of 4-etoxibenzophenone