Impact of Ionic Liquids on Silver Thermoplastic Composite Membrane Polyurethane for Propane/Propylene Separation

Yu Wang a, Tee Yong Goh a, Peter Goodrich a, Mert Atilhan b, Majeda Khraisheh c, David Rooney a, Jillian Thompson a,*, Johan Jacquemin a,d *

a The QUILL Research Centre, School of Chemistry and Chemical Engineering, Queen’s University, Stranmillis Road, Belfast, Northern Ireland BT9 5AG, UK.

b Department of Chemical Engineering, Texas A&M University at Qatar, P.O. Box 23874, Doha, Qatar.

c  Department of Chemical Engineering, Qatar University, P.O. Box: 2713, Doha, Qatar.

d Université François Rabelais, Laboratoire PCM2E, Parc de Grandmont 37200 Tours, France.

* Corresponding authors: jillian.thompson@qub.ac.uk - johan.jacquemin@qub.ac.uk or jj@univ-tours.fr

Electronic Supporting Information

# Figure S1. TGA measurements of TPU-based membranes containing; black: pure TPU; pink: 10 wt.% Ag[Tf2N]; red: 20 wt.% Ag[Tf2N]; green: 30 wt.% Ag[Tf2N].

Figure S2. TGA measurements of TPU-based membranes containing; black: pure TPU; pink: 10 wt.% Ag[Tf2N]; red: 10 wt.% Ag[Tf2N] + 10 wt.% [C4mim][Tf2N]; green: 10 wt.% Ag[Tf2N] + 20 wt.% [C4mim][Tf2N].

# Figure S3. TGA measurements of TPU-based membranes containing; black: pure TPU; red: 10 wt.% AgNO3; green: 20 wt.% AgNO3; blue: 30 wt.% AgNO3.

# Figure S4. TGA measurements of TPU-based membranes containing; black: pure TPU; green: 10 wt.% Ag[PF6]; red: 20 wt.% Ag[PF6]; blue: 30 wt.% Ag[PF6].

Figure S5. TGA measurements of TPU-based membranes containing; black: pure TPU; blue: 10 wt.% Ag[BF4]; red: 20 wt.% Ag[BF4]; green: 30 wt.% Ag[BF4].

Figure S6. TGA measurements of TPU-based membranes containing; black: pure TPU; blue: 10 wt.% Ag[BF4]; red: 10 wt.% Ag[BF4] + 10 wt.% [C4mim][BF4]; green: 10 wt.% Ag[BF4] + 20 wt.% [C4mim][BF4].

Figure S7. TGA measurements of TPU-based membranes containing; black: pure TPU; green: 10 wt.% Ag[PF6]; red: 10 wt.% Ag[PF6] + 10 wt.% [C4mim][PF6]; blue: 10 wt.% Ag[PF6] + 20 wt.% [C4mim][PF6].

Figure S8. TGA measurements of TPU-based membranes containing; black: pure TPU; red: 10 wt.% AgNO3; green: 10 wt.% AgNO3 + 10 wt.% [C4mim][NO3]; blue: 10 wt.% AgNO3 + 20 wt.% [C4mim][NO3]; pink: 10 wt.% Ag[NO3] + 10 wt.% [C4mim][Tf2N]; dark green: 10 wt.% AgNO3 + 20 wt.% [C4mim][Tf2N].

Table S1. TGA analysis: decomposition temperature of selected membranes.

| Composition | T(K) |
| --- | --- |
| TPU | 547.8 |
| 10 wt.% AgNO3 | 382.0 |
| 20 wt.% AgNO3 | 453.9 |
| 30 wt.% AgNO3 | 468.7 |
| 10 wt.% Ag[BF4] | 532.7 |
| 20 wt.% Ag[BF4] | 445.7 |
| 30 wt.% Ag[BF4] | 354.6 |
| 10 wt.% Ag[PF6] | 477.4 |
| 20 wt.% Ag[PF6] | 449.8 |
| 30 wt.% Ag[PF6] | 405.6 |
| 10 wt.% Ag[Tf2N] | 470.9 |
| 20 wt.% Ag[Tf2N] | 461.5 |
| 30 wt.% Ag[Tf2N] | 454.1 |
| 10 wt.% AgNO3 + 10 wt.% [C4mim][NO3] | 517.2 |
| 10 wt.% AgNO3 + 20 wt.% [C4mim][NO3] | 423.7 |
| 10 wt.% AgNO3 + 10 wt.% [C4mim][Tf2N] | 499.9 |
| 10 wt.% AgNO3 + 20 wt.% [C4mim][Tf2N] | 484.9 |
| 10 wt.% Ag[BF4] + 10 wt.% [C4mim][BF4] | 546.0 |
| 10 wt.% Ag[BF4] + 20 wt.% [C4mim][BF4] | 452.4 |
| 10 wt.% Ag[PF6] + 10 wt.% [C4mim][PF6] | 463.2 |
| 10 wt.% Ag[PF6] + 20 wt.% [C4mim][PF6] | 484.9 |
| 10 wt.% Ag[Tf2N] + 10 wt.% [C4mim][Tf2N] | 476.6 |
| 10 wt.% Ag[Tf2N] + 20 wt.% [C4mim][Tf2N] | 465.6 |

u(T) = 1.0 K.

Table S2. Membrane separation data

| Composition | Temperature (K) | Selectivity | Total permeability (Barrer) |
| --- | --- | --- | --- |
| TPU | 293 | 2.0 | 1900.2 |
|  | 313 | 1.9 | 2548.3 |
|  | 333 | 1.8 | 3818.6 |
| 10 wt.% AgNO3 | 293 | 5.0 | 3535.2 |
|  | 313 | 3.1 | 4694.4 |
|  | 333 | 2.7 | 6656.6 |
| 10 wt.% Ag[BF4] | 293 | 7.5 | 2958.1 |
|  | 313 | 4.4 | 3694.2 |
|  | 333 | 3.6 | 4880.2 |
| 20 wt.% Ag[BF4] | 293 | 16.3 | 3404.3 |
|  | 313 | 10.7 | 4369.1 |
|  | 333 | 7.4 | 5243.0 |
| 30 wt.% Ag[BF4] | 293 | 28.2 | 3853.2 |
|  | 313 | 18.7 | 4689.7 |
|  | 333 | 12.2 | 5703.2 |
| 10 wt.% Ag[PF6] | 293 | 5.5 | 590.4 |
|  | 313 | 3.5 | 700.1 |
|  | 333 | 3.1 | 939.5 |
| 20 wt.% Ag[PF6] | 293 | 15.9 | 604.1 |
|  | 313 | 10.1 | 650.1 |
|  | 333 | 7.8 | 877.3 |
| 30 wt.% Ag[PF6] | 293 | 17.2 | 593.7 |
|  | 313 | 11.9 | 696.5 |
|  | 333 | 8.6 | 995.2 |
| 10 wt.% Ag[Tf2N] | 293 | 6.7 | 4478.8 |
|  | 313 | 5.7 | 5992.6 |
|  | 333 | 4.8 | 6554.6 |
| 20 wt.% Ag[Tf2N] | 293 | 17.1 | 4775.1 |
|  | 313 | 14.4 | 6248.0 |
|  | 333 | 11.2 | 7405.0 |
| 30 wt.% Ag[Tf2N] | 293 | 38.0 | 4967.5 |
|  | 313 | 29.2 | 6945.7 |
|  | 333 | 22.0 | 8512.3 |
| 10 wt.% AgNO3 + 10 wt.% [C4mim][NO3] | 293 | 10.0 | 2944.6 |
|  | 313 | 6.6 | 3503.9 |
|  | 333 | 5.0 | 4307.7 |
| 10 wt.% AgNO3 + 20 wt.% [C4mim][NO3] | 293 | 13.8 | 2889.2 |
|  | 313 | 8.5 | 3554.0 |
|  | 333 | 6.3 | 4327.3 |
| 10 wt.% AgNO3 + 10 wt.% [C4mim][Tf2N] | 293 | 10.5 | 3265.4 |
|  | 313 | 7.8 | 3822.2 |
|  | 333 | 5.3 | 5340.4 |
| 10 wt.% AgNO3 + 20 wt.% [C4mim][Tf2N] | 293 | 15.8 | 3368.1 |
|  | 313 | 12.5 | 4055.0 |
|  | 333 | 8.7 | 5621.2 |
| 10 wt.% Ag[BF4] + 10 wt.% [C4mim][BF4] | 293 | 13.0 | 2976.4 |
|  | 313 | 7.8 | 3963.9 |
|  | 333 | 6.0 | 4561.5 |
| 10 wt.% Ag[BF4] + 20 wt.% [C4mim][BF4] | 293 | 18.3 | 2998.2 |
|  | 313 | 12.5 | 3790.0 |
|  | 333 | 10.3 | 4620.9 |
| 10 wt.% Ag[PF6] + 10 wt.% [C4mim][PF6] | 293 | 8.7 | 1801.9 |
|  | 313 | 6.6 | 2338.6 |
|  | 333 | 4.8 | 2865.9 |
| 10 wt.% Ag[PF6] + 20 wt.% [C4mim][PF6] | 293 | 13.3 | 1991.2 |
|  | 313 | 7.8 | 2421.7 |
|  | 333 | 5.2 | 3075.5 |
| 10 wt.% Ag[Tf2N] + 10 wt.% [C4mim][Tf2N] | 293 | 11.3 | 4929.1 |
|  | 313 | 7.9 | 6634.3 |
|  | 333 | 6.2 | 7970.3 |
| 10 wt.% Ag[Tf2N] + 20 wt.% [C4mim][Tf2N] | 293 | 17.2 | 5272.7 |
|  | 313 | 12.8 | 7327.1 |
|  | 333 | 9.1 | 8397.8 |

u(T) = 0.5 K; u(P) = 0.05 bar; u(S) = 0.1.