SUPPLEMENTARY MATERIAL

Method to Control the Optical properties: Band Gap Energy of Mixed Halide Organolead Perovskites

Blessing N. Ezealigoa, Assumpta C Nwanyaa, Solomon Offiaha, Daniel Obib, Sabastine Ezugwuc, Rose U. Osujia,d, R. Bucherd, Malik Maazad,e, Paul Ejikemef, Fabian I. Ezemaa,d,e,g

aDepartment of Physics and Astronomy, University of Nigeria Nsukka Nigeria

bINRS Centre for Energy, Materials and Telecommunications and UNESCO Chair in Materials and Technologies for Energy Conversion, Saving and Storage, 1650, Boulevard Lionel-Boulet, Varennes, QC, CANADA J3X 1S2

cDepartment of Physics and Astronomy, University of Western Ontario, Canada

dNanosciences African Network (NANOAFNET), iThemba LABS-National Research

eUNESCO-UNISA Africa Chair in Nanosciences/Nanotechnology, College of Graduate Studies, University of South Africa (UNISA), Muckleneuk ridge, P.O. Box 392, Pretoria, South Africa

fDepartment of Pure and Industrial Chemistry, University of Nigeria, Nsukka Nigeria

gDepartment of Physics, Faculty of Natural and Applied Sciences, Coal City University, Enugu, Nigeria

Outline

- Fig. S1: Plots of the halide and mixed perovskite’s band gap with photon energy

- Fig. S2: Plots of extinction coefficient of the halide and mixed perovskite’s with wavelength

- Fig. S3: Plot of (n2-1)-1 vs (hv)2 for halide & mixed halide perovskites

- Fig. S4: Plot of (n2-1)-1 vs λ-2 for halide & mixed halide perovskites

Figure S1: Plots of (αλυ)2 versus photon energy, hυ for mixed halide perovskites comprising of MAPbI with different amount of (a) MAPbBr3, (b) MaPbCl3 (c) MAPbI3 with MAPbBr3 as inset (d) combination of the three halide perovskites with MAPbCl3 as inset.

Figure S2: Plots of extinction coefficient , k versus wavelength, λ for mixed halide perovskites comprising of MAPbI3 with different amount of (a) MAPbBr3, (b) MaPbCl3 (c) combination of the three halide perovskites

The extinction coefficient which measures the quantity of light lost due to scattering and absorption per unit distance of the penetration medium (Gedi et al., 2015) is presented in fig S2. Generally, all the perovskite samples showed that small quantity of light was lost but MAPbBr3 samples has the lowest values, which is evident in the good absorbance of the films compared to other samples. The band gap of hybrid perovskite samples showed changes in band gap as seen in figure S1(a&b). In the samples containing varying volume of methylammonium lead chloride, (hybrid MAPbCl3 sample) the estimated band gap obtained is in the same range as the MAPbI3 sample, which implies that the addition of MAPbCl3 (which has the highest band gap) to MAPbI3 enhances dispersion, the carriers and better mix-ability compared to MAPbBr3 counterpart (Mosconi et al., 2013; Ha et al., 2014). In the samples with varying concentrations of methylammonium lead bromide, (hybrid MAPbBr3 Sample) which had an estimated band gap slightly lower compared to the MAPbBr3 sample, which may be related to the asymmetry of MAPbBr3 in their band edges (Schulz et al., 2014). The obtained band gaps are in range with reports by (Philippe et at., 2015; Chae et al., 2015; Park et al., 2015) for mixed hybrid perovskites, though the values of the band gap obtained were slightly higher than the report of Atourkia et al., 2016 and Misra et al., 2016), due to the film preparation technique adopted in this work.

The optical dispersion characteristics of the deposited films were also studied. The single term Wemple DiDomenico oscillator formulae was applied in determining the expression of the parameter n below the optical band gap in relation to the energy.

The dispersion relation is given by the formula (Wemple, 1971):

(n2−1)−1=E0Ed−1E0Ed(hv)2		(4)

where Ed is the dispersion energy and E0  is the single oscillator energy. The oscillator energy is usually estimated from the relation (Tanaka, 1980): E0≈1.5Eg and the dispersion energy given by Gonza´ lez-Leal, 2013:Ed=βNcZaNe

The average value of Ed = 9.36 eV E0= 2.76 eV. The static refractive index, n0 can be determined by using the expression n0=1+EdE0= 2.1

The single term Sellmeier dispersion relation can be applied for evaluation of the dispersion

of n in the long wavelength region (Palik, 2012):

n2−1=S0λ021−λ02λ2			(5)

Simplified further, we have:

(n2−1)−1=−1S0λ−2+1S0λ02	(5a)

where λ0 is defined as average interband oscillator wavelength and S0is average oscillator position. In Fig. 4.2b we plotted the graph of (n2-1)-1 versus λ−2 of which  λ0 and S0parameters were determined from the slope (1S0) and intercept (1S0λ2). The average value ofλ0 and S0were 332 nm and 2.66 x10-5 nm-2 respectively.

Figure S3: Plot of (n2-1)-1 vs (hv)2 for mixed halide perovskites comprising of MAPbI3 with different amount of (a) MAPbBr3, (b) MaPbCl3 (c) combination of the three halide perovskites

Figure S4: Plot of (n2-1)-1 vs λ-2 for mixed halide perovskites comprising of MAPbI3 with different amount of (a) MAPbBr3, (b) MaPbCl3 (c) combination of the three halide perovskites

References

Atourkia, L., Vegab, E., Maríb, B., Mollarb, M., Ahsainec, H.A., Bouabida, K., Ihlalaa, A., 2016. Materials, Role of the chemical substitution on the structural and luminescence properties of the mixed halide perovskite thin MAPbI3 – xBrx (0 ≤ x ≤ 1) films, Applied Surface Science 371, 112–117.

Chae, J., Dong, Q., Huang, J., Centrone, A., 2015. Chloride Incorporation Process in CH3NH3PbI3-xClx Perovskites via Nanoscale Bandgap Maps, Nano Letters, 15(12), 8114–8121.

Gedi, S., Reddy, V.M., Park, C., Chan-Wook, J., Ramakrishna, K.T., 2015. Comprehensive optical studies on SnS layers synthesized by chemical bath deposition http://dx.doi.org/10.1016/j.optmat.2015.01.043.

# Ha, S.T., Liu, X., Zhang, Q., Giovanni, D., Sum, T.C., Xiong, Q., 2014. Synthesis of Organic–Inorganic Lead Halide Perovskite Nanoplatelets: Towards High-Performance Perovskite Solar Cells and Optoelectronic Devices,Advanced Optical Materials, 2, 838– 844.

Misra, R.K., Ciammaruchi, L., Aharon, S., Mogilyansky, D., Etgar, L., Visoly-Fisher, I., Katz, E.A., 2016. Effect of Halide Composition on the Photochemical Stability of Perovskite Photovoltaic Materials, ChemSusChem, 9, 1–7.

## Mosconi, E., Amat, M., Nazeeruddin, K., Grätzel, M., DeAngelis, F., 2013. First-Principles Modeling of Mixed Halide Organometal Perovskites for Photovoltaic Applications, Journal of Physical Chemistry C 117, 13902—13913.

Palik, E.D., (2012). Handbook of Optical Constants of Solids II, Academic Press, California.

Park, B., Philippe, B., Jain, S.M., Zhang, X., Edvinsson, T., Rensmo, H., Zietza, B., Boschloo, G., 2015. Chemical engineering of methylammonium lead iodide/bromide perovskites: tuning of optoelectronic properties and photovoltaic performance. Journal of Materials Chemistry A, , 3, 21760–21771.

## Philippe, B., Park, B., Lindblad, R., Oscarsson, J., Ahmadi, S., Erik, M., Johansson, J., Rensmo, H., 2015. Chemical and Electronic Structure Characterization of Lead Halide Perovskites and Stability Behavior under Different Exposures: A Photoelectron Spectroscopy Investigation, Chemistry of Materials, 27 (5), pp 1720–1731.

Tanaka, K. (1980). Properties and photo induced changes in amorphous As-S films,Thin Solid Films 66, 271–279.

### Wemple, S.H., DiDomenico, M., 1971. Behavior of the Electronic Dielectric Constant in Covalent and Ionic Materials, Phys. Rev. B 3, 1338-1351.

Author to whom corresponding should be addressed (F.I. Ezema):

E-mail address: fabian.ezema@unn.edu.ng,

+2348036239214