Supporting Information

Excellent bio-compatibility and in-vitro cytotoxicity of the highly enhanced luminescent with aqueous soluble NaGdF4:Ce/Tb nanocrystals and their potential application in anti-cancer drug

Anees A. Ansari*1, Shahanavaj Khan2, A. Aldalbahi1, A. K. Parchur3, B. Kumar3, Ashok Kumar4, Mohd Raish5, S. B. Rai3

1King Abdullah Institute for Nanotechnology, King Saud University, Riyadh-11451, Saudi Arabia

2Nanomedicine & Biotechnology Research Unit, Department of Pharmaceutics, College of Pharmacy, PO Box 2457, King Saud University, Riyadh 11451, Saudi Arabia

3Department of Physics, Banaras Hindu University, Varanasi-221005, India

4Vitiligo Research Chair, College of Medicine, King Saud University, Riyadh 11451, Saudi Arabia

5Department of Pharmaceutics, College of Pharmacy, PO Box 2457, King Saud University, Riyadh 11451, Saudi Arabia

Table S1 The lifetime parameters obtained from the biexponential fitting to the luminescence decay data of the Core, Core/Shell, and Core/Shell/SiO2 nanoparticles at 355 nm excitation (λem = 545 nm).

| Nanoparticles | I1(%) | τ1(ms) | I2(%) | τ2(ms) | τav(ms) | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| Core | 13 | 0.405 | 87 | 5.307 | 4.673 | 0.9913 |
| Core/Shell | 10 | 0.306 | 90 | 3.525 | 3.210 | 0.9923 |
| Core/Shell/SiO2 | 43 | 2.241 | 57 | 4.355 | 3.444 | 0.9830 |

Figure S1

Figure S1 Photoluminescence decay curves of core, core/shell, and core/shell/SiO2 nanoparticles at λex = 355 nm and λem = 545 nm fitted using biexponential decay equations.

Fig. S2

Fig. S2 In vitro estimation of possible cytotoxicity in HT-29 cells after incubation with different concentrations of NaGdF4:Ce/Tb@NaGdF4 (core/shell) NCs for 24 h at 37 ºC through MTT assay.

Fig. S3

Fig. S3 In vitro estimation of possible cytotoxicity in HT-29 cells after incubation with different concentrations of NaGdF4:Ce/Tb@NaGdF4/SiO2 (core/shell/SiO2) NCs for 24 h at 37 ºC through MTT assay.