Datablock: 1

| Bond precision: | C-C = 0.0056 A | Wavelength=0.71073 |
| --- | --- | --- |

| Cell: | a=24.192(3) | b=24.192(3) | c=9.6003(19) |
| --- | --- | --- | --- |
|  | alpha=90 | beta=90 | gamma=120 |
| Temperature: | 293 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 4865.9(18) | 4865.7(14) |
| Space group | R -3 | R-3 |
| Hall group | -R 3 | ? |
| Moiety formula | C9 H4 N4 O3 Zn [+ solvent] | ? |
| Sum formula | C9 H4 N4 O3 Zn [+ solvent] | C9 H6 N4 O3 Zn |
| Mr | 281.55 | 283.55 |
| Dx,g cm-3 | 1.730 | 1.742 |
| Z | 18 | 18 |
| Mu (mm-1) | 2.272 | 2.273 |
| F000 | 2520.0 | 2556.0 |
| F000' | 2525.98 |  |
| h,k,lmax | 31,31,12 | 31,31,12 |
| Nref | 2485 | 2481 |
| Tmin,Tmax | 0.752,0.761 | 0.752,0.761 |
| Tmin' | 0.737 |  |

| Correction method= # Reported T Limits: Tmin=0.752 Tmax=0.761 AbsCorr = EMPIRICAL |  |
| --- | --- |

| Data completeness= 0.998 | Theta(max)= 27.480 |
| --- | --- |

| R(reflections)= 0.0475( 2210) | wR2(reflections)= 0.1527( 2481) |
| --- | --- |

| S = 1.135 | Npar= 155 |
| --- | --- |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level B

SYMMS02_ALERT_1_B  The unit-cell lengths a and c should be equal for a

rhombohedral cell

Cell      24.1920   24.1920    9.6003

Angles    90.0000   90.0000  120.0000

SYMMS02_ALERT_1_B  Cell angles alpha and gamma should be equal for a

rhombohedral cell

Cell      24.1920   24.1920    9.6003

Angles    90.0000   90.0000  120.0000

SYMMS02_ALERT_1_B  All angles should not be 90 for a rhombohedral cell

Cell      24.1920   24.1920    9.6003

Angles    90.0000   90.0000  120.0000

PLAT430_ALERT_2_B Short Inter D...A Contact  O1     ..  Ow1     ..       2.70 Ang.

PLAT430_ALERT_2_B Short Inter D...A Contact  Ow1    ..  O2      ..       2.67 Ang.

PLAT990_ALERT_1_B Deprecated RES file style based SQUEEZE job ....          ! Note

Alert level C

PLAT250_ALERT_2_C Large U3/U1 Ratio for Average U(i,j) Tensor ....        2.1 Note

Alert level G

FORMU01_ALERT_2_G  There is a discrepancy between the atom counts in the

_chemical_formula_sum and the formula from the _atom_site* data.

Atom count from _chemical_formula_sum:C9 H6 N4 O3 Zn1

Atom count from the _atom_site data:  C9 H4 N4 O3 Zn1

CELLZ01_ALERT_1_G Difference between formula and atom_site contents detected.

CELLZ01_ALERT_1_G WARNING: H atoms missing from atom site list. Is this intentional?

From the CIF: _cell_formula_units_Z   18

From the CIF: _chemical_formula_sum  C9 H6 N4 O3 Zn

TEST: Compare cell contents of formula and atom_site data

atom    Z*formula  cif sites diff

C        162.00    162.00    0.00

H        108.00     72.00   36.00

N         72.00     72.00    0.00

O         54.00     54.00    0.00

Zn        18.00     18.00    0.00

PLAT004_ALERT_5_G Polymeric Structure Found with Maximum Dimension          1 Info

PLAT005_ALERT_5_G No Embedded Refinement Details found  in the CIF     Please Do !

PLAT007_ALERT_5_G Number of Unrefined Donor-H Atoms ..............          1 Report

PLAT041_ALERT_1_G Calc. and Reported SumFormula    Strings  Differ     Please Check

PLAT066_ALERT_1_G Predicted and Reported Tmin&Tmax Range Identical          ? Check

PLAT068_ALERT_1_G Reported F000 Differs from Calcd (or Missing)...     Please Check

PLAT083_ALERT_2_G SHELXL Second Parameter in WGHT  Unusually Large      41.24 Why ?

PLAT104_ALERT_1_G The Reported Crystal System is Inconsistent with        R-3 Check

PLAT152_ALERT_1_G The Supplied and Calc. Volume s.u. Differ by ...          4 Units

PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K)        293 Check

PLAT200_ALERT_1_G Reported   _diffrn_ambient_temperature ..... (K)        293 Check

PLAT232_ALERT_2_G Hirshfeld Test Diff (M-X)  Zn1    --  Ow1     ..        5.4 s.u.

PLAT605_ALERT_4_G Largest Solvent Accessible VOID in the Structure        351 A**3

PLAT720_ALERT_4_G Number of Unusual/Non-Standard Labels ..........          1 Note

PLAT869_ALERT_4_G ALERTS Related to the use of SQUEEZE Suppressed           ! Info

PLAT899_ALERT_4_G SHELXL97   is Deprecated and Succeeded by SHELXL       2014 Note

Datablock: 2

| Bond precision: | C-C = 0.0070 A | Wavelength=0.71073 |
| --- | --- | --- |

| Cell: | a=25.002(3) | b=25.002(3) | c=9.968(2) |
| --- | --- | --- | --- |
|  | alpha=90 | beta=90 | gamma=120 |
| Temperature: | 293 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 5396(2) | 5396.2(14) |
| Space group | R -3 | R-3 |
| Hall group | -R 3 | ? |
| Moiety formula | C9 H4 Cd N4 O3 [+ solvent] | ? |
| Sum formula | C9 H4 Cd N4 O3 [+ solvent] | C9 H6 Cd N4 O3 |
| Mr | 328.57 | 330.59 |
| Dx,g cm-3 | 1.820 | 1.831 |
| Z | 18 | 18 |
| Mu (mm-1) | 1.822 | 1.822 |
| F000 | 2844.0 | 2879.0 |
| F000' | 2830.53 |  |
| h,k,lmax | 32,32,12 | 32,32,12 |
| Nref | 2758 | 2753 |
| Tmin,Tmax | 0.789,0.818 | 0.789,0.818 |
| Tmin' | 0.789 |  |

| Correction method= # Reported T Limits: Tmin=0.789 Tmax=0.818 AbsCorr = EMPIRICAL |  |
| --- | --- |

| Data completeness= 0.998 | Theta(max)= 27.480 |
| --- | --- |

| R(reflections)= 0.0502( 2514) | wR2(reflections)= 0.1700( 2753) |
| --- | --- |

| S = 1.175 | Npar= 155 |
| --- | --- |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level B

SYMMS02_ALERT_1_B  The unit-cell lengths a and c should be equal for a

rhombohedral cell

Cell      25.0020   25.0020    9.9680

Angles    90.0000   90.0000  120.0000

SYMMS02_ALERT_1_B  Cell angles alpha and gamma should be equal for a

rhombohedral cell

Cell      25.0020   25.0020    9.9680

Angles    90.0000   90.0000  120.0000

SYMMS02_ALERT_1_B  All angles should not be 90 for a rhombohedral cell

Cell      25.0020   25.0020    9.9680

Angles    90.0000   90.0000  120.0000

PLAT094_ALERT_2_B Ratio of Maximum / Minimum Residual Density ....       5.57 Report

PLAT430_ALERT_2_B Short Inter D...A Contact  O1     ..  Ow1     ..       2.68 Ang.

PLAT430_ALERT_2_B Short Inter D...A Contact  Ow1    ..  O2      ..       2.72 Ang.

PLAT990_ALERT_1_B Deprecated RES file style based SQUEEZE job ....          ! Note

Alert level C

PLAT250_ALERT_2_C Large U3/U1 Ratio for Average U(i,j) Tensor ....        2.2 Note

Alert level G

FORMU01_ALERT_2_G  There is a discrepancy between the atom counts in the

_chemical_formula_sum and the formula from the _atom_site* data.

Atom count from _chemical_formula_sum:C9 H6 Cd1 N4 O3

Atom count from the _atom_site data:  C9 H4 Cd1 N4 O3

CELLZ01_ALERT_1_G Difference between formula and atom_site contents detected.

CELLZ01_ALERT_1_G WARNING: H atoms missing from atom site list. Is this intentional?

From the CIF: _cell_formula_units_Z   18

From the CIF: _chemical_formula_sum  C9 H6 Cd N4 O3

TEST: Compare cell contents of formula and atom_site data

atom    Z*formula  cif sites diff

C        162.00    162.00    0.00

H        108.00     72.00   36.00

Cd        18.00     18.00    0.00

N         72.00     72.00    0.00

O         54.00     54.00    0.00

PLAT004_ALERT_5_G Polymeric Structure Found with Maximum Dimension          1 Info

PLAT005_ALERT_5_G No Embedded Refinement Details found  in the CIF     Please Do !

PLAT007_ALERT_5_G Number of Unrefined Donor-H Atoms ..............          1 Report

PLAT041_ALERT_1_G Calc. and Reported SumFormula    Strings  Differ     Please Check

PLAT066_ALERT_1_G Predicted and Reported Tmin&Tmax Range Identical          ? Check

PLAT068_ALERT_1_G Reported F000 Differs from Calcd (or Missing)...     Please Check

PLAT083_ALERT_2_G SHELXL Second Parameter in WGHT  Unusually Large      56.98 Why ?

PLAT104_ALERT_1_G The Reported Crystal System is Inconsistent with        R-3 Check

PLAT152_ALERT_1_G The Supplied and Calc. Volume s.u. Differ by ...          6 Units

PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K)        293 Check

PLAT200_ALERT_1_G Reported   _diffrn_ambient_temperature ..... (K)        293 Check

PLAT232_ALERT_2_G Hirshfeld Test Diff (M-X)  Cd1    --  Ow1     ..       10.0 s.u.

PLAT605_ALERT_4_G Largest Solvent Accessible VOID in the Structure        464 A**3

PLAT720_ALERT_4_G Number of Unusual/Non-Standard Labels ..........          1 Note

PLAT869_ALERT_4_G ALERTS Related to the use of SQUEEZE Suppressed           ! Info

PLAT899_ALERT_4_G SHELXL97   is Deprecated and Succeeded by SHELXL       2014 Note

Datablock: 3

| Bond precision: | C-C = 0.0111 A | Wavelength=0.71073 |
| --- | --- | --- |

| Cell: | a=11.001(2) | b=25.507(5) | c=17.270(4) |
| --- | --- | --- | --- |
|  | alpha=90 | beta=93.56(3) | gamma=90 |
| Temperature: | 293 K |  |  |

|  | Calculated | Reported |
| --- | --- | --- |
| Volume | 4836.7(17) | 4836.6(17) |
| Space group | C 2/c | C2/c |
| Hall group | -C 2yc | ? |
| Moiety formula | C24 H12 N6 O7 Zn [+ solvent] | ? |
| Sum formula | C24 H12 N6 O7 Zn [+ solvent] | C24 H14 N6 O7 Zn |
| Mr | 561.79 | 563.78 |
| Dx,g cm-3 | 1.543 | 1.549 |
| Z | 8 | 8 |
| Mu (mm-1) | 1.073 | 1.073 |
| F000 | 2272.0 | 2288.0 |
| F000' | 2275.26 |  |
| h,k,lmax | 14,33,22 | 14,33,22 |
| Nref | 5534 | 5512 |
| Tmin,Tmax | 0.870,0.898 | 0.870,0.898 |
| Tmin' | 0.870 |  |

| Correction method= # Reported T Limits: Tmin=0.870 Tmax=0.898 AbsCorr = EMPIRICAL |  |
| --- | --- |

| Data completeness= 0.996 | Theta(max)= 27.480 |
| --- | --- |

| R(reflections)= 0.1205( 3710) | wR2(reflections)= 0.3645( 5512) |
| --- | --- |

| S = 1.088 | Npar= 343 |
| --- | --- |

The following ALERTS were generated. Each ALERT has the format

test-name_ALERT_alert-type_alert-level.

Click on the hyperlinks for more details of the test.

Alert level B

PLAT084_ALERT_3_B High wR2 Value (i.e. > 0.25) ...................       0.36 Report

PLAT097_ALERT_2_B Large Reported Max.  (Positive) Residual Density       3.25 eA-3

PLAT416_ALERT_2_B Short Intra D-H..H-D       H2A    ..  H3A     ..       1.39 Ang.

PLAT430_ALERT_2_B Short Inter D...A Contact  O1     ..  Ow1     ..       2.71 Ang.

PLAT990_ALERT_1_B Deprecated RES file style based SQUEEZE job ....          ! Note

Alert level C

DIFMX02_ALERT_1_C  The maximum difference density is > 0.1*ZMAX*0.75

The relevant atom site should be identified.

PLAT082_ALERT_2_C High R1 Value ..................................       0.12 Report

PLAT094_ALERT_2_C Ratio of Maximum / Minimum Residual Density ....       3.27 Report

PLAT213_ALERT_2_C Atom O1              has ADP max/min Ratio .....        3.2 prolat

PLAT250_ALERT_2_C Large U3/U1 Ratio for Average U(i,j) Tensor ....        2.4 Note

PLAT341_ALERT_3_C Low Bond Precision on  C-C Bonds ...............    0.01112 Ang.

PLAT430_ALERT_2_C Short Inter D...A Contact  Ow1    ..  O5      ..       2.89 Ang.

Alert level G

FORMU01_ALERT_2_G  There is a discrepancy between the atom counts in the

_chemical_formula_sum and the formula from the _atom_site* data.

Atom count from _chemical_formula_sum:C24 H14 N6 O7 Zn1

Atom count from the _atom_site data:  C24 H12 N6 O7 Zn1

CELLZ01_ALERT_1_G Difference between formula and atom_site contents detected.

CELLZ01_ALERT_1_G WARNING: H atoms missing from atom site list. Is this intentional?

From the CIF: _cell_formula_units_Z    8

From the CIF: _chemical_formula_sum  C24 H14 N6 O7 Zn

TEST: Compare cell contents of formula and atom_site data

atom    Z*formula  cif sites diff

C        192.00    192.00    0.00

H        112.00     96.00   16.00

N         48.00     48.00    0.00

O         56.00     56.00    0.00

Zn         8.00      8.00    0.00

PLAT004_ALERT_5_G Polymeric Structure Found with Maximum Dimension          3 Info

PLAT005_ALERT_5_G No Embedded Refinement Details found  in the CIF     Please Do !

PLAT007_ALERT_5_G Number of Unrefined Donor-H Atoms ..............          4 Report

PLAT041_ALERT_1_G Calc. and Reported SumFormula    Strings  Differ     Please Check

PLAT066_ALERT_1_G Predicted and Reported Tmin&Tmax Range Identical          ? Check

PLAT068_ALERT_1_G Reported F000 Differs from Calcd (or Missing)...     Please Check

PLAT072_ALERT_2_G SHELXL First  Parameter in WGHT  Unusually Large       0.18 Report

PLAT083_ALERT_2_G SHELXL Second Parameter in WGHT  Unusually Large      75.35 Why ?

PLAT199_ALERT_1_G Reported _cell_measurement_temperature ..... (K)        293 Check

PLAT200_ALERT_1_G Reported   _diffrn_ambient_temperature ..... (K)        293 Check

PLAT605_ALERT_4_G Largest Solvent Accessible VOID in the Structure        245 A**3

PLAT720_ALERT_4_G Number of Unusual/Non-Standard Labels ..........          1 Note

PLAT869_ALERT_4_G ALERTS Related to the use of SQUEEZE Suppressed           ! Info

PLAT899_ALERT_4_G SHELXL97   is Deprecated and Succeeded by SHELXL       2014 Note