data_1

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'C9 H6 N4 O3 Zn'

_chemical_formula_weight          283.55

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'C'  'C'   0.0033   0.0016

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'N'  'N'   0.0061   0.0033

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Zn'  'Zn'   0.2839   1.4301

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            RHOMBOHEDRAL

_symmetry_space_group_name_H-M    R-3

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-y, x-y, z'

'-x+y, -x, z'

'x+2/3, y+1/3, z+1/3'

'-y+2/3, x-y+1/3, z+1/3'

'-x+y+2/3, -x+1/3, z+1/3'

'x+1/3, y+2/3, z+2/3'

'-y+1/3, x-y+2/3, z+2/3'

'-x+y+1/3, -x+2/3, z+2/3'

'-x, -y, -z'

'y, -x+y, -z'

'x-y, x, -z'

'-x+2/3, -y+1/3, -z+1/3'

'y+2/3, -x+y+1/3, -z+1/3'

'x-y+2/3, x+1/3, -z+1/3'

'-x+1/3, -y+2/3, -z+2/3'

'y+1/3, -x+y+2/3, -z+2/3'

'x-y+1/3, x+2/3, -z+2/3'

_cell_length_a                    24.192(3)

_cell_length_b                    24.192(3)

_cell_length_c                    9.6003(19)

_cell_angle_alpha                 90.00

_cell_angle_beta                  90.00

_cell_angle_gamma                 120.00

_cell_volume                      4865.7(14)

_cell_formula_units_Z             18

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     13484

_cell_measurement_theta_min       3.335

_cell_measurement_theta_max       27.5

_exptl_crystal_description        clomnar

_exptl_crystal_colour             colorless

_exptl_crystal_size_max           0.13

_exptl_crystal_size_mid           0.12

_exptl_crystal_size_min           0.12

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     1.742

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              2556

_exptl_absorpt_coefficient_mu     2.273

_exptl_absorpt_correction_type    empirical

_exptl_absorpt_correction_T_min   0.752

_exptl_absorpt_correction_T_max   0.761

_exptl_absorpt_process_details    'Process-auto'

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   'Rigaku RAXIS-RAPID'

_diffrn_measurement_method        omega-scan

_diffrn_detector_area_resol_mean  '10.0'

_diffrn_standards_number          0

_diffrn_standards_interval_count  0

_diffrn_standards_interval_time   0

_diffrn_standards_decay_%         0

_diffrn_reflns_number             15879

_diffrn_reflns_av_R_equivalents   0.0392

_diffrn_reflns_av_sigmaI/netI     0.0244

_diffrn_reflns_limit_h_min        -31

_diffrn_reflns_limit_h_max        31

_diffrn_reflns_limit_k_min        -31

_diffrn_reflns_limit_k_max        31

_diffrn_reflns_limit_l_min        -12

_diffrn_reflns_limit_l_max        11

_diffrn_reflns_theta_min          3.33

_diffrn_reflns_theta_max          27.48

_reflns_number_total              2481

_reflns_number_gt                 2210

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        'Process-auto'

_computing_cell_refinement        'Process-auto'

_computing_data_reduction         'Process-auto'

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.0852P)^2^+41.2380P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     constr

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          2481

_refine_ls_number_parameters      155

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.0529

_refine_ls_R_factor_gt            0.0475

_refine_ls_wR_factor_ref          0.1527

_refine_ls_wR_factor_gt           0.1489

_refine_ls_goodness_of_fit_ref    1.135

_refine_ls_restrained_S_all       1.135

_refine_ls_shift/su_max           0.000

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

Zn1 Zn 0.24861(2) 0.07017(2) -0.85638(4) 0.01855(19) Uani 1 1 d . . .

O1 O 0.22544(15) 0.15284(15) -0.6532(3) 0.0249(6) Uani 1 1 d . . .

O2 O 0.32230(14) 0.02429(14) -0.3909(3) 0.0200(6) Uani 1 1 d . . .

N1 N 0.26654(16) 0.08840(16) -0.6541(3) 0.0171(6) Uani 1 1 d . . .

N2 N 0.29316(16) 0.05773(16) -0.5806(3) 0.0177(6) Uani 1 1 d . . .

H2A H 0.3087 0.0389 -0.6294 0.021 Uiso 1 1 calc R . .

N3 N 0.23875(16) 0.12296(15) -0.0009(3) 0.0176(6) Uani 1 1 d . . .

N4 N 0.20534(17) 0.18293(16) -0.1153(3) 0.0187(7) Uani 1 1 d . . .

C1 C 0.24654(18) 0.11756(17) -0.1434(4) 0.0148(7) Uani 1 1 d . . .

C2 C 0.22405(18) 0.15379(18) -0.2142(4) 0.0159(7) Uani 1 1 d . . .

C3 C 0.22239(19) 0.15480(18) -0.3592(4) 0.0179(7) Uani 1 1 d . . .

H3B H 0.2058 0.1770 -0.4061 0.021 Uiso 1 1 calc R . .

C4 C 0.24642(18) 0.12144(17) -0.4315(4) 0.0154(7) Uani 1 1 d . . .

C5 C 0.27123(18) 0.08740(17) -0.3600(4) 0.0147(7) Uani 1 1 d . . .

C6 C 0.27129(19) 0.08449(18) -0.2148(4) 0.0168(7) Uani 1 1 d . . .

H6A H 0.2871 0.0616 -0.1679 0.020 Uiso 1 1 calc R . .

C7 C 0.24557(18) 0.12142(18) -0.5848(4) 0.0164(7) Uani 1 1 d . . .

C8 C 0.29720(17) 0.05446(17) -0.4418(4) 0.0143(7) Uani 1 1 d . . .

C9 C 0.21452(19) 0.16173(18) 0.0066(4) 0.0186(8) Uani 1 1 d . . .

H9A H 0.2046 0.1734 0.0913 0.022 Uiso 1 1 calc R . .

OW1 O 0.33638(15) 0.08162(15) -0.9002(3) 0.0262(7) Uani 1 1 d . . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

Zn1 0.0304(3) 0.0149(3) 0.0084(3) 0.00004(15) -0.00243(16) 0.0099(2)

O1 0.0366(17) 0.0352(16) 0.0136(13) 0.0059(12) 0.0015(12) 0.0261(14)

O2 0.0229(14) 0.0248(14) 0.0180(13) 0.0007(11) -0.0016(11) 0.0163(12)

N1 0.0242(16) 0.0208(15) 0.0088(14) -0.0004(12) -0.0014(12) 0.0130(13)

N2 0.0247(16) 0.0241(16) 0.0115(14) -0.0014(12) -0.0006(12) 0.0176(14)

N3 0.0280(17) 0.0185(15) 0.0095(14) 0.0022(11) 0.0028(12) 0.0140(14)

N4 0.0278(17) 0.0224(16) 0.0117(14) -0.0004(12) 0.0009(12) 0.0170(14)

C1 0.0213(17) 0.0151(16) 0.0082(15) 0.0022(12) 0.0007(13) 0.0093(14)

C2 0.0205(17) 0.0173(17) 0.0117(16) 0.0001(13) 0.0012(13) 0.0109(15)

C3 0.0266(19) 0.0202(18) 0.0107(16) 0.0011(13) 0.0005(14) 0.0146(16)

C4 0.0187(17) 0.0161(16) 0.0109(16) 0.0015(13) 0.0007(13) 0.0083(14)

C5 0.0181(17) 0.0145(16) 0.0115(17) 0.0009(13) 0.0006(13) 0.0082(14)

C6 0.0232(18) 0.0172(17) 0.0127(17) 0.0019(13) -0.0002(14) 0.0120(15)

C7 0.0196(17) 0.0179(17) 0.0106(16) 0.0004(13) 0.0001(13) 0.0085(14)

C8 0.0164(16) 0.0133(16) 0.0124(16) -0.0005(12) -0.0011(13) 0.0068(14)

C9 0.027(2) 0.0218(19) 0.0099(16) 0.0003(14) 0.0021(14) 0.0139(16)

OW1 0.0293(16) 0.0267(15) 0.0262(15) 0.0021(12) 0.0060(12) 0.0168(13)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Zn1 N3 1.979(3) 1_554 ?

Zn1 N1 1.990(3) . ?

Zn1 N4 2.014(3) 11_554 ?

Zn1 OW1 2.043(3) . ?

O1 C7 1.271(5) . ?

O2 C8 1.258(5) . ?

N1 C7 1.321(5) . ?

N1 N2 1.394(4) . ?

N2 C8 1.341(5) . ?

N3 C9 1.333(5) . ?

N3 C1 1.396(4) . ?

N3 Zn1 1.979(3) 1_556 ?

N4 C9 1.341(5) . ?

N4 C2 1.386(5) . ?

N4 Zn1 2.014(3) 12_554 ?

C1 C6 1.395(5) . ?

C1 C2 1.415(5) . ?

C2 C3 1.393(5) . ?

C3 C4 1.393(5) . ?

C4 C5 1.416(5) . ?

C4 C7 1.471(5) . ?

C5 C6 1.396(5) . ?

C5 C8 1.465(5) . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

N3 Zn1 N1 128.62(13) 1_554 . ?

N3 Zn1 N4 109.90(14) 1_554 11_554 ?

N1 Zn1 N4 109.95(13) . 11_554 ?

N3 Zn1 OW1 102.74(13) 1_554 . ?

N1 Zn1 OW1 94.26(13) . . ?

N4 Zn1 OW1 108.15(13) 11_554 . ?

C7 N1 N2 119.1(3) . . ?

C7 N1 Zn1 121.3(3) . . ?

N2 N1 Zn1 118.9(2) . . ?

C8 N2 N1 127.0(3) . . ?

C9 N3 C1 104.3(3) . . ?

C9 N3 Zn1 130.8(3) . 1_556 ?

C1 N3 Zn1 124.1(2) . 1_556 ?

C9 N4 C2 104.2(3) . . ?

C9 N4 Zn1 126.9(3) . 12_554 ?

C2 N4 Zn1 128.7(3) . 12_554 ?

C6 C1 N3 130.7(3) . . ?

C6 C1 C2 121.8(3) . . ?

N3 C1 C2 107.5(3) . . ?

N4 C2 C3 131.0(3) . . ?

N4 C2 C1 108.1(3) . . ?

C3 C2 C1 120.9(3) . . ?

C4 C3 C2 117.6(3) . . ?

C3 C4 C5 121.1(3) . . ?

C3 C4 C7 119.3(3) . . ?

C5 C4 C7 119.7(3) . . ?

C6 C5 C4 121.7(3) . . ?

C6 C5 C8 119.7(3) . . ?

C4 C5 C8 118.6(3) . . ?

C1 C6 C5 116.8(3) . . ?

O1 C7 N1 118.6(3) . . ?

O1 C7 C4 121.7(3) . . ?

N1 C7 C4 119.7(3) . . ?

O2 C8 N2 119.4(3) . . ?

O2 C8 C5 124.8(3) . . ?

N2 C8 C5 115.9(3) . . ?

N3 C9 N4 115.9(3) . . ?

_diffrn_measured_fraction_theta_max    0.998

_diffrn_reflns_theta_full              27.48

_diffrn_measured_fraction_theta_full   0.998

_refine_diff_density_max    1.647

_refine_diff_density_min   -0.872

_refine_diff_density_rms    0.159

# SQUEEZE RESULTS (APPEND TO CIF)

loop_

_platon_squeeze_void_nr

_platon_squeeze_void_average_x

_platon_squeeze_void_average_y

_platon_squeeze_void_average_z

_platon_squeeze_void_volume

_platon_squeeze_void_count_electrons

1     0.000     0.000    -0.030     346.5       1.1

2     0.333     0.667    -0.006     353.8       0.3

3     0.667     0.333    -0.041     353.8       0.2

_platon_squeeze_details

;

;

data_2

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'C9 H6 Cd N4 O3'

_chemical_formula_weight          330.59

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'C'  'C'   0.0033   0.0016

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Cd'  'Cd'  -0.8075   1.2024

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'N'  'N'   0.0061   0.0033

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            RHOMBOHEDRAL

_symmetry_space_group_name_H-M    R-3

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-y, x-y, z'

'-x+y, -x, z'

'x+2/3, y+1/3, z+1/3'

'-y+2/3, x-y+1/3, z+1/3'

'-x+y+2/3, -x+1/3, z+1/3'

'x+1/3, y+2/3, z+2/3'

'-y+1/3, x-y+2/3, z+2/3'

'-x+y+1/3, -x+2/3, z+2/3'

'-x, -y, -z'

'y, -x+y, -z'

'x-y, x, -z'

'-x+2/3, -y+1/3, -z+1/3'

'y+2/3, -x+y+1/3, -z+1/3'

'x-y+2/3, x+1/3, -z+1/3'

'-x+1/3, -y+2/3, -z+2/3'

'y+1/3, -x+y+2/3, -z+2/3'

'x-y+1/3, x+2/3, -z+2/3'

_cell_length_a                    25.002(3)

_cell_length_b                    25.002(3)

_cell_length_c                    9.968(2)

_cell_angle_alpha                 90.00

_cell_angle_beta                  90.00

_cell_angle_gamma                 120.00

_cell_volume                      5396.2(14)

_cell_formula_units_Z             18

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     15841

_cell_measurement_theta_min       3.22

_cell_measurement_theta_max       27.545

_exptl_crystal_description        COLUMNAR

_exptl_crystal_colour             COLORLESS

_exptl_crystal_size_max           0.13

_exptl_crystal_size_mid           0.12

_exptl_crystal_size_min           0.11

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     1.831

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              2879

_exptl_absorpt_coefficient_mu     1.822

_exptl_absorpt_correction_type    EMPIRICAL

_exptl_absorpt_correction_T_min   0.789

_exptl_absorpt_correction_T_max   0.818

_exptl_absorpt_process_details    'Process-auto'

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   'Rigaku RAXIS-RAPID'

_diffrn_measurement_method        omega-scan

_diffrn_detector_area_resol_mean  '10.0'

_diffrn_standards_number          0

_diffrn_standards_interval_count  0

_diffrn_standards_interval_time   0

_diffrn_standards_decay_%         0

_diffrn_reflns_number             17056

_diffrn_reflns_av_R_equivalents   0.0329

_diffrn_reflns_av_sigmaI/netI     0.0225

_diffrn_reflns_limit_h_min        -32

_diffrn_reflns_limit_h_max        32

_diffrn_reflns_limit_k_min        -32

_diffrn_reflns_limit_k_max        32

_diffrn_reflns_limit_l_min        -12

_diffrn_reflns_limit_l_max        11

_diffrn_reflns_theta_min          3.22

_diffrn_reflns_theta_max          27.48

_reflns_number_total              2753

_reflns_number_gt                 2514

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        'Process-auto'

_computing_cell_refinement        'Process-auto'

_computing_data_reduction         'Process-auto'

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.0968P)^2^+56.9849P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     CONSTR

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          2753

_refine_ls_number_parameters      155

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.0533

_refine_ls_R_factor_gt            0.0502

_refine_ls_wR_factor_ref          0.1700

_refine_ls_wR_factor_gt           0.1682

_refine_ls_goodness_of_fit_ref    1.175

_refine_ls_restrained_S_all       1.175

_refine_ls_shift/su_max           0.001

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

Cd1 Cd 0.24565(2) 0.070144(18) 0.66255(4) 0.0363(2) Uani 1 1 d . . .

O1 O 0.32153(18) 0.02293(17) 0.1375(4) 0.0298(8) Uani 1 1 d . . .

O2 O 0.2336(2) 0.1475(2) -0.1342(4) 0.0362(9) Uani 1 1 d . . .

N1 N 0.2432(2) 0.1261(2) 0.4982(4) 0.0308(9) Uani 1 1 d . . .

N2 N 0.2139(2) 0.1853(2) 0.3805(5) 0.0323(10) Uani 1 1 d . . .

N3 N 0.2924(2) 0.0513(2) -0.0490(4) 0.0273(9) Uani 1 1 d . . .

H3A H 0.3046 0.0298 -0.0932 0.033 Uiso 1 1 calc R . .

N4 N 0.2691(2) 0.0820(2) -0.1240(4) 0.0273(8) Uani 1 1 d . . .

C1 C 0.2530(2) 0.1206(2) 0.0850(5) 0.0231(9) Uani 1 1 d . . .

C2 C 0.2744(2) 0.0860(2) 0.1587(5) 0.0222(9) Uani 1 1 d . . .

C3 C 0.2735(2) 0.0847(2) 0.2982(5) 0.0243(9) Uani 1 1 d . . .

H3B H 0.2875 0.0623 0.3464 0.029 Uiso 1 1 calc R . .

C4 C 0.2505(2) 0.1188(2) 0.3627(5) 0.0258(10) Uani 1 1 d . . .

C5 C 0.2319(2) 0.1550(2) 0.2896(5) 0.0260(10) Uani 1 1 d . . .

C6 C 0.2323(2) 0.1556(2) 0.1503(5) 0.0271(10) Uani 1 1 d . . .

H6A H 0.2190 0.1788 0.1025 0.033 Uiso 1 1 calc R . .

C7 C 0.2979(2) 0.0517(2) 0.0840(5) 0.0228(9) Uani 1 1 d . . .

C8 C 0.2523(2) 0.1175(2) -0.0621(5) 0.0257(10) Uani 1 1 d . . .

C9 C 0.2213(3) 0.1653(3) 0.5005(5) 0.0347(12) Uani 1 1 d . . .

H9A H 0.2118 0.1779 0.5804 0.042 Uiso 1 1 calc R . .

OW1 O 0.3430(2) 0.0891(2) 0.6071(5) 0.0432(10) Uani 1 1 d . . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

Cd1 0.0647(3) 0.0279(3) 0.0123(3) 0.00045(12) -0.00311(15) 0.0201(2)

O1 0.0342(19) 0.0348(19) 0.0258(18) -0.0024(15) -0.0048(15) 0.0214(16)

O2 0.047(2) 0.048(2) 0.0211(18) 0.0123(16) 0.0033(16) 0.0292(19)

N1 0.049(3) 0.033(2) 0.014(2) 0.0001(16) 0.0029(18) 0.023(2)

N2 0.050(3) 0.034(2) 0.021(2) 0.0009(17) 0.0042(19) 0.027(2)

N3 0.037(2) 0.034(2) 0.018(2) -0.0051(16) -0.0021(16) 0.0228(19)

N4 0.034(2) 0.034(2) 0.0138(19) -0.0023(16) -0.0020(16) 0.0168(18)

C1 0.030(2) 0.025(2) 0.013(2) 0.0007(17) 0.0000(17) 0.0130(19)

C2 0.028(2) 0.021(2) 0.016(2) -0.0011(16) -0.0015(17) 0.0112(18)

C3 0.033(2) 0.025(2) 0.015(2) 0.0011(17) -0.0014(18) 0.0148(19)

C4 0.035(2) 0.028(2) 0.013(2) 0.0000(17) 0.0021(18) 0.014(2)

C5 0.035(2) 0.026(2) 0.019(2) 0.0004(17) 0.0053(19) 0.016(2)

C6 0.036(3) 0.029(2) 0.020(2) 0.0043(18) 0.0030(19) 0.019(2)

C7 0.025(2) 0.024(2) 0.018(2) -0.0021(17) -0.0011(17) 0.0112(18)

C8 0.030(2) 0.028(2) 0.016(2) 0.0024(18) 0.0013(18) 0.0121(19)

C9 0.054(3) 0.037(3) 0.017(2) -0.001(2) 0.005(2) 0.026(3)

OW1 0.053(3) 0.038(2) 0.040(2) 0.0036(18) 0.009(2) 0.024(2)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Cd1 N1 2.175(4) . ?

Cd1 N4 2.187(4) 1_556 ?

Cd1 N2 2.197(5) 11_556 ?

Cd1 OW1 2.303(5) . ?

O1 C7 1.255(6) . ?

O2 C8 1.285(6) . ?

N1 C9 1.341(7) . ?

N1 C4 1.387(6) . ?

N2 C9 1.345(7) . ?

N2 C5 1.391(6) . ?

N2 Cd1 2.197(5) 12_556 ?

N3 C7 1.332(6) . ?

N3 N4 1.390(6) . ?

N3 H3A 0.8600 . ?

N4 C8 1.312(7) . ?

N4 Cd1 2.187(4) 1_554 ?

C1 C6 1.383(7) . ?

C1 C2 1.428(6) . ?

C1 C8 1.467(6) . ?

C2 C3 1.391(6) . ?

C2 C7 1.463(6) . ?

C3 C4 1.397(7) . ?

C3 H3B 0.9300 . ?

C4 C5 1.412(7) . ?

C5 C6 1.389(7) . ?

C6 H6A 0.9300 . ?

C9 H9A 0.9300 . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

N1 Cd1 N4 137.52(16) . 1_556 ?

N1 Cd1 N2 110.57(18) . 11_556 ?

N4 Cd1 N2 109.19(17) 1_556 11_556 ?

N1 Cd1 OW1 93.07(18) . . ?

N4 Cd1 OW1 91.21(17) 1_556 . ?

N2 Cd1 OW1 104.21(17) 11_556 . ?

C9 N1 C4 104.1(4) . . ?

C9 N1 Cd1 127.6(4) . . ?

C4 N1 Cd1 126.9(3) . . ?

C9 N2 C5 103.6(4) . . ?

C9 N2 Cd1 128.1(4) . 12_556 ?

C5 N2 Cd1 128.1(4) . 12_556 ?

C7 N3 N4 126.9(4) . . ?

C7 N3 H3A 116.5 . . ?

N4 N3 H3A 116.5 . . ?

C8 N4 N3 119.0(4) . . ?

C8 N4 Cd1 113.2(3) . 1_554 ?

N3 N4 Cd1 127.3(3) . 1_554 ?

C6 C1 C2 120.9(4) . . ?

C6 C1 C8 120.4(4) . . ?

C2 C1 C8 118.7(4) . . ?

C3 C2 C1 121.4(4) . . ?

C3 C2 C7 120.2(4) . . ?

C1 C2 C7 118.4(4) . . ?

C2 C3 C4 117.0(4) . . ?

C2 C3 H3B 121.5 . . ?

C4 C3 H3B 121.5 . . ?

N1 C4 C3 130.6(5) . . ?

N1 C4 C5 108.0(4) . . ?

C3 C4 C5 121.4(4) . . ?

C6 C5 N2 130.3(5) . . ?

C6 C5 C4 121.3(4) . . ?

N2 C5 C4 108.3(4) . . ?

C1 C6 C5 117.8(4) . . ?

C1 C6 H6A 121.1 . . ?

C5 C6 H6A 121.1 . . ?

O1 C7 N3 119.6(4) . . ?

O1 C7 C2 124.2(4) . . ?

N3 C7 C2 116.2(4) . . ?

O2 C8 N4 117.8(5) . . ?

O2 C8 C1 121.7(5) . . ?

N4 C8 C1 120.5(5) . . ?

N1 C9 N2 116.0(5) . . ?

N1 C9 H9A 122.0 . . ?

N2 C9 H9A 122.0 . . ?

_diffrn_measured_fraction_theta_max    0.998

_diffrn_reflns_theta_full              27.48

_diffrn_measured_fraction_theta_full   0.998

_refine_diff_density_max    3.265

_refine_diff_density_min   -0.586

_refine_diff_density_rms    0.231

# SQUEEZE RESULTS (APPEND TO CIF)

loop_

_platon_squeeze_void_nr

_platon_squeeze_void_average_x

_platon_squeeze_void_average_y

_platon_squeeze_void_average_z

_platon_squeeze_void_volume

_platon_squeeze_void_count_electrons

1     0.000     0.000    -0.019     420.4       6.9

2     0.333     0.667    -0.045     429.8       5.4

3     0.667     0.333    -0.006     429.8       5.4

_platon_squeeze_details

;

;

data_3

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'C24 H14 N6 O7 Zn'

_chemical_formula_weight          563.78

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'C'  'C'   0.0033   0.0016

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'N'  'N'   0.0061   0.0033

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Zn'  'Zn'   0.2839   1.4301

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            monoclinic

_symmetry_space_group_name_H-M    C2/c

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, y, -z+1/2'

'x+1/2, y+1/2, z'

'-x+1/2, y+1/2, -z+1/2'

'-x, -y, -z'

'x, -y, z-1/2'

'-x+1/2, -y+1/2, -z'

'x+1/2, -y+1/2, z-1/2'

_cell_length_a                    11.001(2)

_cell_length_b                    25.507(5)

_cell_length_c                    17.270(4)

_cell_angle_alpha                 90.00

_cell_angle_beta                  93.56(3)

_cell_angle_gamma                 90.00

_cell_volume                      4836.6(17)

_cell_formula_units_Z             8

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     16374

_cell_measurement_theta_min       3.02

_cell_measurement_theta_max       27.53

_exptl_crystal_description        columnar

_exptl_crystal_colour             yellow

_exptl_crystal_size_max           0.13

_exptl_crystal_size_mid           0.11

_exptl_crystal_size_min           0.10

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     1.549

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              2288

_exptl_absorpt_coefficient_mu     1.073

_exptl_absorpt_correction_type    empirical

_exptl_absorpt_correction_T_min   0.870

_exptl_absorpt_correction_T_max   0.898

_exptl_absorpt_process_details    'Process-auto'

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   'Rigaku RAXIS-RAPID'

_diffrn_measurement_method        omega-scan

_diffrn_detector_area_resol_mean  '10.0'

_diffrn_standards_number          0

_diffrn_standards_interval_count  0

_diffrn_standards_interval_time   0

_diffrn_standards_decay_%         0

_diffrn_reflns_number             23380

_diffrn_reflns_av_R_equivalents   0.0755

_diffrn_reflns_av_sigmaI/netI     0.0612

_diffrn_reflns_limit_h_min        -14

_diffrn_reflns_limit_h_max        14

_diffrn_reflns_limit_k_min        -32

_diffrn_reflns_limit_k_max        33

_diffrn_reflns_limit_l_min        -22

_diffrn_reflns_limit_l_max        22

_diffrn_reflns_theta_min          3.02

_diffrn_reflns_theta_max          27.48

_reflns_number_total              5512

_reflns_number_gt                 3710

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        'Process-auto'

_computing_cell_refinement        'Process-auto'

_computing_data_reduction         'Process-auto'

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.1822P)^2^+75.3472P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     constr

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          5512

_refine_ls_number_parameters      343

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.1553

_refine_ls_R_factor_gt            0.1205

_refine_ls_wR_factor_ref          0.3645

_refine_ls_wR_factor_gt           0.3421

_refine_ls_goodness_of_fit_ref    1.088

_refine_ls_restrained_S_all       1.088

_refine_ls_shift/su_max           0.000

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

Zn1 Zn 0.09240(9) 0.09031(4) 0.04886(7) 0.0465(4) Uani 1 1 d . . .

O1 O 0.0189(8) 0.0121(4) -0.0905(5) 0.083(3) Uani 1 1 d . . .

O2 O -0.2591(7) 0.1822(3) -0.1116(5) 0.065(2) Uani 1 1 d . . .

O3 O -0.5244(6) 0.2964(2) -0.4432(5) 0.057(2) Uani 1 1 d . . .

H3A H -0.5438 0.3272 -0.4503 0.086 Uiso 1 1 calc R . .

O4 O -0.0413(6) 0.2889(3) -0.3839(6) 0.072(3) Uani 1 1 d . . .

O5 O -0.7316(6) 0.0751(2) -0.5719(4) 0.0448(15) Uani 1 1 d . . .

O6 O -0.6481(6) -0.0733(2) -0.3562(4) 0.0488(17) Uani 1 1 d . . .

N1 N -0.0250(6) 0.0912(3) -0.0484(4) 0.0411(17) Uani 1 1 d . . .

N2 N -0.1034(7) 0.1346(3) -0.0576(5) 0.0456(18) Uani 1 1 d . . .

H2A H -0.0921 0.1593 -0.0240 0.055 Uiso 1 1 calc R . .

N3 N -0.3426(7) 0.3362(3) -0.4265(4) 0.0410(17) Uani 1 1 d . . .

N4 N -0.2172(7) 0.3317(3) -0.4099(5) 0.0438(18) Uani 1 1 d . . .

H4A H -0.1761 0.3604 -0.4079 0.053 Uiso 1 1 calc R . .

N5 N -0.7742(6) -0.0002(2) -0.5125(4) 0.0337(15) Uani 1 1 d . . .

H5A H -0.8328 -0.0042 -0.5474 0.040 Uiso 1 1 calc R . .

N6 N -0.7625(6) -0.0398(2) -0.4566(4) 0.0336(15) Uani 1 1 d . . .

C1 C -0.1501(8) 0.0152(4) -0.2150(5) 0.043(2) Uani 1 1 d . . .

H1A H -0.0991 -0.0139 -0.2104 0.051 Uiso 1 1 calc R . .

C2 C -0.2395(8) 0.0180(3) -0.2738(5) 0.0385(19) Uani 1 1 d . . .

H2B H -0.2481 -0.0093 -0.3094 0.046 Uiso 1 1 calc R . .

C3 C -0.3188(7) 0.0613(3) -0.2814(4) 0.0304(16) Uani 1 1 d . . .

C4 C -0.3057(7) 0.1018(3) -0.2301(5) 0.0329(16) Uani 1 1 d . . .

H4B H -0.3583 0.1304 -0.2346 0.040 Uiso 1 1 calc R . .

C5 C -0.2116(7) 0.1006(3) -0.1695(5) 0.0318(16) Uani 1 1 d . . .

C6 C -0.1363(7) 0.0562(3) -0.1626(5) 0.0356(17) Uani 1 1 d . . .

C7 C -0.0427(8) 0.0530(4) -0.0979(5) 0.043(2) Uani 1 1 d . . .

C8 C -0.1938(8) 0.1423(3) -0.1126(6) 0.041(2) Uani 1 1 d . . .

C9 C -0.1691(8) 0.1913(3) -0.3890(6) 0.042(2) Uani 1 1 d . . .

H9A H -0.0847 0.1893 -0.3821 0.050 Uiso 1 1 calc R . .

C10 C -0.2386(7) 0.1462(3) -0.3896(5) 0.0380(18) Uani 1 1 d . . .

H10A H -0.2003 0.1139 -0.3833 0.046 Uiso 1 1 calc R . .

C11 C -0.3647(7) 0.1483(3) -0.3993(4) 0.0303(16) Uani 1 1 d . . .

C12 C -0.4207(7) 0.1964(3) -0.4105(5) 0.0356(18) Uani 1 1 d . . .

H12A H -0.5051 0.1982 -0.4176 0.043 Uiso 1 1 calc R . .

C13 C -0.3513(7) 0.2427(3) -0.4113(5) 0.0362(18) Uani 1 1 d . . .

C14 C -0.2263(7) 0.2397(3) -0.3989(5) 0.0388(19) Uani 1 1 d . . .

C15 C -0.4109(8) 0.2935(3) -0.4269(6) 0.044(2) Uani 1 1 d . . .

C16 C -0.1544(8) 0.2875(4) -0.3969(6) 0.047(2) Uani 1 1 d . . .

C17 C -0.5313(7) 0.0933(3) -0.4569(5) 0.0319(16) Uani 1 1 d . . .

H17A H -0.5449 0.1196 -0.4936 0.038 Uiso 1 1 calc R . .

C18 C -0.4393(7) 0.0996(3) -0.4002(4) 0.0290(15) Uani 1 1 d . . .

C19 C -0.4159(6) 0.0584(3) -0.3454(4) 0.0287(15) Uani 1 1 d . . .

C20 C -0.4871(7) 0.0138(3) -0.3504(4) 0.0299(16) Uani 1 1 d . . .

H20A H -0.4707 -0.0134 -0.3155 0.036 Uiso 1 1 calc R . .

C21 C -0.5841(6) 0.0086(3) -0.4073(4) 0.0282(15) Uani 1 1 d . . .

C22 C -0.6055(7) 0.0484(3) -0.4613(4) 0.0290(15) Uani 1 1 d . . .

C23 C -0.7074(7) 0.0423(3) -0.5191(5) 0.0334(17) Uani 1 1 d . . .

C24 C -0.6659(7) -0.0380(3) -0.4061(5) 0.0326(17) Uani 1 1 d . . .

OW1 O -0.0216(8) 0.0894(3) 0.1359(5) 0.071(2) Uani 1 1 d . . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

Zn1 0.0364(6) 0.0470(7) 0.0533(7) -0.0172(5) -0.0205(5) 0.0133(4)

O1 0.068(5) 0.086(6) 0.088(6) -0.039(5) -0.057(5) 0.042(5)

O2 0.066(5) 0.033(3) 0.091(6) -0.014(4) -0.033(4) 0.008(3)

O3 0.039(3) 0.031(3) 0.100(6) 0.024(3) -0.018(4) -0.004(3)

O4 0.036(4) 0.045(4) 0.130(7) 0.020(4) -0.023(4) -0.013(3)

O5 0.045(3) 0.038(3) 0.048(3) 0.010(3) -0.021(3) -0.003(3)

O6 0.057(4) 0.025(3) 0.060(4) 0.007(3) -0.028(3) -0.009(3)

N1 0.031(3) 0.043(4) 0.046(4) -0.010(3) -0.019(3) 0.001(3)

N2 0.036(4) 0.042(4) 0.056(5) -0.008(3) -0.016(3) -0.001(3)

N3 0.037(4) 0.033(4) 0.050(4) 0.017(3) -0.016(3) -0.005(3)

N4 0.036(4) 0.030(3) 0.063(5) 0.012(3) -0.012(3) -0.010(3)

N5 0.033(3) 0.027(3) 0.039(4) -0.001(3) -0.017(3) -0.003(3)

N6 0.036(3) 0.020(3) 0.043(4) -0.001(3) -0.011(3) -0.001(3)

C1 0.032(4) 0.045(5) 0.049(5) -0.006(4) -0.010(4) 0.014(4)

C2 0.038(4) 0.030(4) 0.045(5) -0.009(3) -0.015(4) 0.003(3)

C3 0.025(3) 0.029(4) 0.035(4) 0.005(3) -0.013(3) -0.007(3)

C4 0.031(4) 0.025(3) 0.041(4) 0.001(3) -0.009(3) -0.007(3)

C5 0.025(3) 0.024(3) 0.045(4) 0.002(3) -0.007(3) -0.010(3)

C6 0.027(4) 0.039(4) 0.039(4) -0.005(3) -0.010(3) -0.002(3)

C7 0.032(4) 0.045(5) 0.050(5) -0.007(4) -0.015(4) 0.007(4)

C8 0.032(4) 0.032(4) 0.058(5) 0.001(4) -0.011(4) -0.003(3)

C9 0.031(4) 0.036(4) 0.057(5) 0.003(4) -0.005(4) -0.004(3)

C10 0.030(4) 0.038(4) 0.046(5) 0.002(4) 0.001(3) -0.003(3)

C11 0.032(4) 0.025(4) 0.033(4) 0.005(3) -0.005(3) -0.006(3)

C12 0.030(4) 0.033(4) 0.041(4) 0.008(3) -0.011(3) -0.005(3)

C13 0.034(4) 0.029(4) 0.045(4) 0.005(3) -0.009(3) -0.005(3)

C14 0.031(4) 0.034(4) 0.050(5) 0.008(4) -0.007(4) -0.014(3)

C15 0.042(5) 0.030(4) 0.057(5) 0.013(4) -0.011(4) -0.003(4)

C16 0.031(4) 0.036(5) 0.070(6) 0.009(4) -0.013(4) -0.011(4)

C17 0.031(4) 0.027(4) 0.035(4) 0.008(3) -0.012(3) -0.003(3)

C18 0.025(3) 0.025(3) 0.037(4) 0.001(3) -0.002(3) -0.005(3)

C19 0.026(3) 0.027(3) 0.032(4) -0.002(3) -0.010(3) 0.002(3)

C20 0.033(4) 0.022(3) 0.033(4) -0.001(3) -0.013(3) -0.003(3)

C21 0.021(3) 0.025(3) 0.037(4) -0.007(3) -0.009(3) -0.001(3)

C22 0.029(4) 0.028(4) 0.029(3) -0.004(3) -0.009(3) 0.000(3)

C23 0.030(4) 0.034(4) 0.035(4) -0.001(3) -0.011(3) 0.002(3)

C24 0.033(4) 0.028(4) 0.035(4) -0.003(3) -0.012(3) 0.004(3)

OW1 0.067(5) 0.064(5) 0.081(6) 0.001(4) -0.009(4) -0.016(4)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Zn1 OW1 2.016(10) . ?

Zn1 N3 2.040(7) 8_556 ?

Zn1 N1 2.055(7) . ?

Zn1 N6 2.059(7) 6_656 ?

O1 C7 1.247(12) . ?

O2 C8 1.246(11) . ?

O3 C15 1.266(11) . ?

O4 C16 1.252(11) . ?

O5 C23 1.253(10) . ?

O6 C24 1.253(10) . ?

N1 C7 1.302(11) . ?

N1 N2 1.407(10) . ?

N2 C8 1.346(11) . ?

N3 C15 1.324(11) . ?

N3 N4 1.396(10) . ?

N3 Zn1 2.040(7) 8_455 ?

N4 C16 1.332(12) . ?

N5 C23 1.320(10) . ?

N5 N6 1.397(9) . ?

N6 C24 1.333(9) . ?

N6 Zn1 2.059(7) 6_455 ?

C1 C2 1.371(11) . ?

C1 C6 1.385(12) . ?

C2 C3 1.409(11) . ?

C3 C4 1.363(11) . ?

C3 C19 1.491(9) . ?

C4 C5 1.426(10) . ?

C5 C6 1.404(11) . ?

C5 C8 1.455(12) . ?

C6 C7 1.473(10) . ?

C9 C10 1.380(12) . ?

C9 C14 1.391(12) . ?

C10 C11 1.387(11) . ?

C11 C12 1.381(11) . ?

C11 C18 1.490(10) . ?

C12 C13 1.407(11) . ?

C13 C14 1.380(11) . ?

C13 C15 1.469(12) . ?

C14 C16 1.454(11) . ?

C17 C18 1.373(10) . ?

C17 C22 1.405(10) . ?

C18 C19 1.425(10) . ?

C19 C20 1.381(10) . ?

C20 C21 1.412(9) . ?

C21 C22 1.388(11) . ?

C21 C24 1.492(11) . ?

C22 C23 1.463(9) . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

OW1 Zn1 N3 94.7(3) . 8_556 ?

OW1 Zn1 N1 102.7(3) . . ?

N3 Zn1 N1 110.8(3) 8_556 . ?

OW1 Zn1 N6 123.2(3) . 6_656 ?

N3 Zn1 N6 108.8(3) 8_556 6_656 ?

N1 Zn1 N6 114.8(3) . 6_656 ?

C7 N1 N2 116.7(7) . . ?

C7 N1 Zn1 126.1(6) . . ?

N2 N1 Zn1 116.8(5) . . ?

C8 N2 N1 128.0(7) . . ?

C15 N3 N4 119.0(7) . . ?

C15 N3 Zn1 124.3(6) . 8_455 ?

N4 N3 Zn1 116.7(5) . 8_455 ?

C16 N4 N3 126.9(7) . . ?

C23 N5 N6 128.7(6) . . ?

C24 N6 N5 117.6(6) . . ?

C24 N6 Zn1 125.5(6) . 6_455 ?

N5 N6 Zn1 116.4(4) . 6_455 ?

C2 C1 C6 119.3(8) . . ?

C1 C2 C3 121.4(7) . . ?

C4 C3 C2 119.7(7) . . ?

C4 C3 C19 124.1(7) . . ?

C2 C3 C19 116.2(7) . . ?

C3 C4 C5 120.1(7) . . ?

C6 C5 C4 118.6(7) . . ?

C6 C5 C8 118.6(7) . . ?

C4 C5 C8 122.7(7) . . ?

C1 C6 C5 120.9(7) . . ?

C1 C6 C7 119.8(8) . . ?

C5 C6 C7 119.3(7) . . ?

O1 C7 N1 120.0(8) . . ?

O1 C7 C6 118.3(8) . . ?

N1 C7 C6 121.7(8) . . ?

O2 C8 N2 120.8(8) . . ?

O2 C8 C5 123.6(8) . . ?

N2 C8 C5 115.6(7) . . ?

C10 C9 C14 119.4(8) . . ?

C9 C10 C11 121.2(8) . . ?

C12 C11 C10 119.0(7) . . ?

C12 C11 C18 119.9(7) . . ?

C10 C11 C18 121.0(7) . . ?

C11 C12 C13 120.6(7) . . ?

C14 C13 C12 119.2(8) . . ?

C14 C13 C15 120.4(7) . . ?

C12 C13 C15 120.4(7) . . ?

C13 C14 C9 120.5(7) . . ?

C13 C14 C16 119.4(8) . . ?

C9 C14 C16 120.1(8) . . ?

O3 C15 N3 120.3(8) . . ?

O3 C15 C13 121.1(8) . . ?

N3 C15 C13 118.6(8) . . ?

O4 C16 N4 120.4(8) . . ?

O4 C16 C14 124.2(9) . . ?

N4 C16 C14 115.5(7) . . ?

C18 C17 C22 122.3(7) . . ?

C17 C18 C19 118.8(6) . . ?

C17 C18 C11 119.1(7) . . ?

C19 C18 C11 122.1(6) . . ?

C20 C19 C18 119.2(6) . . ?

C20 C19 C3 117.6(6) . . ?

C18 C19 C3 123.2(6) . . ?

C19 C20 C21 121.5(7) . . ?

C22 C21 C20 119.2(7) . . ?

C22 C21 C24 121.0(6) . . ?

C20 C21 C24 119.7(7) . . ?

C21 C22 C17 119.1(6) . . ?

C21 C22 C23 118.2(7) . . ?

C17 C22 C23 122.7(7) . . ?

O5 C23 N5 121.2(7) . . ?

O5 C23 C22 123.1(7) . . ?

N5 C23 C22 115.8(7) . . ?

O6 C24 N6 120.6(7) . . ?

O6 C24 C21 120.9(6) . . ?

N6 C24 C21 118.3(7) . . ?

_diffrn_measured_fraction_theta_max    0.996

_diffrn_reflns_theta_full              27.48

_diffrn_measured_fraction_theta_full   0.996

_refine_diff_density_max    3.252

_refine_diff_density_min   -0.996

_refine_diff_density_rms    0.202

# SQUEEZE RESULTS (APPEND TO CIF)

loop_

_platon_squeeze_void_nr

_platon_squeeze_void_average_x

_platon_squeeze_void_average_y

_platon_squeeze_void_average_z

_platon_squeeze_void_volume

_platon_squeeze_void_count_electrons

1    -0.020     0.202     0.250     242.6      21.2

2    -0.010     0.702     0.250     242.6      21.2

3    -0.026     0.799     0.750     242.8      22.2

4    -0.009     0.299     0.750     242.8      22.2

_platon_squeeze_details

;

;