S1 The relationship between [Co2+] / [Ni2+] ratios in the baths and Co content in (a) C.R.L.,  the Ni-Co alloys deposited from (b)Ni-Co1, Ni-Co4 and Ni-Co7 alloys (free IL), (c) Ni-Co2, Ni-Co5 and Ni-Co8 alloys (with 1×10-5 M [MOFIM]I), (d) Ni-Co3, Ni-Co6 and Ni-Co9 alloys (with 1×10-5 M [FPIM]Br), i = 20 mA cm-2,     t = 10 min., T = 25oC.

- Ni-Co1

| Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- |
| 0.33 | 59.54 | 38.03 |

(a') NiCo2

| [MOFIM]I M | Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- | --- |
| 1×10-5 | 0.21 | 63.23 | 35.55 |

| [FPIM]Br M | Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- | --- |
| 0 | 0.20 | 58.76 | 38.96 |

(a") NiCo3

(b) NiCo4

| Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- |
| 0.76 | 37.68 | 59.80 |

| [MOFIM]I M | Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- | --- |
| 1×10-5 | 0.76 | 31.84 | 65.65 |

(b') NiCo5

(b") NiCo6

| [FPIM]Br M | Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- | --- |
| 1×10-5 | 0.33 | 36.11 | 60.76 |

(c) NiCo7

| Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- |
| 0.34 | 14.55 | 79.09 |

| [MOFIM]I M | Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- | --- |
| 1×10-5 | 0.63 | 11.48 | 85.33 |

(c') NiCo8

(c") NiCo9

| [FPIM]Br M | Cu fraction % | Ni fraction % | Co fraction % |
| --- | --- | --- | --- |
| 1×10-5 | 0.12 | 13.69 | 83.62 |

S2. EDS spectra and SEM-EDS elemental mapping images of  Cu, Co, Ni, and C,N,O, F elements of [MOFIM]I and [FPIM]Br compositions obtained from the Ni-Co alloys electrodeposited in (a),(b),(c) free ILs, (a'),(b'),(c') 1×10-5M  [MOFIM]I, (a"),(b"),(c") 1×10-5M  [FPIM]Br.