Simultaneous non-steroidal anti-inflammatory drug electro-detection on nitrogen doped carbon nanodots and nanosized cobalt phthalLocyanine nanoparticles conjugate modified gassy carbon electrode.

Nyaradzai Dondo1,Munyaradzi Shumba1,Mambo Moyo1, Stephen Nyoni2,*

1. Midlands State University, Department of Chemical Technology, P. Bag 9055, Senga Road, Gweru, Zimbabwe.

2. Chinhoyi University of Technology, Chemistry department, P. Bag 7724, Chinhoyi, Zimbabwe.

Supplementary information

Fig.S1. FTIR spectra of the electrode modifiers

Fig S2 Electrochemical characterisation by (A) CVs, Scan rate 100 mV/s ((B) Nyquist plots and (C) Bode plots for  a) CNDs-GCE, (b) NCNDs-GCE, (c) Bare-GCE, (d) CoTAPhPcNPs-GCE (e) CoTAPhPcNPs-CNDs-GCE (f) CoTAPhPcNPs-NDCNDs-GCE in Fe(CN)63-/4- in  0.1 M KCl,

Current/au

Current/au

Current/au

Fig S3: Optimization of pH for each analyte in PBS. Scan rate 100mV/s

Current/au

Current/au

Current/au

Fig. S4. Voltammetric evolutions for CoTAPhPcNP-NDCNDs-GCEin 1 mm Drug for ASA, IBU and INDO. At scan rates 50-400 mV/s with corresponding plots of root of scan rate versus anodic current and log of scan rate versus detection potential.

Fig S5.Twenty successive cyclic voltammetric evolutions for (A) ASA, (B) IBU and (C) INDO for1 mM drug in PBS at CoTAPhPcNPs-NCNDs-GCE.Scan rate = 100 mV/s

Fig S6: Linear sweep voltammograms and Langmuir adsorption isotherm plot for CoTAPhPcNPs-NDCNDs-GCE (10 μM, 20 μM, 30 μM, 40 μM, 50 μM, 60 μM) of ASA, IBU and INDO concentrations in PBS.

Fig S7. Cyclic voltammograms of (A) ASA, (B) IBU and (C) INDO in PBS at regenerated CoTAPhPcNPs-NDCNDs-GCE. Scan rate 100mV/s

Table S1. Electrochemical parameters for CoTAPhPcNP-NDCNDs-GCE

| Modified GCE | Electrode characterisation inFe(CN)63-/4- (0.1 M KCl) |  |  | E/V drug oxidation pH 7 buffer |  |  | Background corrected currents/µA drug oxidation |  |  | RCT values for drug oxidation |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ∆E/V | RCT/kΩ | Kapp/10-7 | ASA pH 4 | INDO pH 6 | IBU pH 5 | ASA pH 4 | INDO pH 6 | IBU pH 5 | ASA pH 4 | INDO pH 6 | IBU pH 5 |
| Bare GCE | - | 8.3 | - | - | - | - | - | - | - | - | - | - |
| CNDs-GCE | 0.0836 | 22.603 | 1.44 | - | - | - | - | - | - | - | - | - |
| # NDCNDs-GCE | # 0.0989 | # 9.14 | 2.94 | # - | # - | # - | # - | # - | # - | # - | # - | # - |
| # CoTAPhPcNPs-GCE | # 0.1305 | # 5.61 | # 3.63 | # 0.847 | # 1.045 | # 1.331 | # 283 | # 256 | # 67 | # 3.388 | # 3.764 | # 3.461 |
| # CoTAPhPcNPs-CNDs-GCE | # 0.1327 | # 1.51 | # 13.3 | # 0.832 | # 1.035 | # 1.322 | # 306 | # 306 | # 84 | # 1.645 | # 1.742 | # 1.528 |
| # CoTAPhPcNPs-NDCNDs-GCE | # 0.1373 | # 1.36 | # 14.3 | # 0.816 | # 1.003 | # 1.318 | # 411 | # 368 | # 229 | # 1.328 | # 1.355 | # 1.273 |

Table S2. Limits of detection and catalytic rate constants for different drugs

| Modified GCE | Drug | Technique | LOD/nM | k(103 M-1s-1) | Ref |
| --- | --- | --- | --- | --- | --- |
| CoTAPhPcNP-NDCNDs-GCE | ASA | DPV | 9.66 | 1.66 | This work |
|  | INDO | DPV | 7.23 | 0.195 | This work |
|  | IBU | DPV | 4.19 | 1.42 | This work |
| Gr-NiO-GCE | INDO | DPV | 54 | - | [3] |
| GCE/ZnO–Pd/CNTs | Levedopa | DPV | 80 | - | [2] |
|  | IBU |  | 40 | - | [2] |
| ER-GONRs/SPC | Nimesulide | Amperometry | 3.50 | - | [41] |

Table S3. Recovery values for the anodic detection of NSAIDs

| Sample | [ASA]/µM |  |  | [IBU]/µM |  |  | [INDO]/µM |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tape water | Added | Observed | Recovery | Added | Observed | Recovery | Added | Observed | Recovery |
|  | 2 | 2.033 | 101.5±0.2 | 2 | 1.926 | 96.3 | 2 | 1.894 | 94.7±0.1 |
|  | 4 | 4.071 | 101.8±0.1 | 4 | 3.743 | 93.6 | 4 | 3.751 | 93.8±0.3 |
|  | 6 | 6.025 | 100.4±0.3 | 6 | 5.471 | 91.2 | 6 | 5.437 | 90.6±0.1 |