**Table 1S.** The BET analysis of the prepared CFYM and CFYM/GO.

|  |  |  |  |
| --- | --- | --- | --- |
| Compounds | BET surface area (m2 g–1) | Total pore volume (cm3 g–1) | Mean pore diameter (nm) |
| CFYM | **3.485** | **0.0078** | **8.692** |
| CFYM/GO | **21.413** | **0.2586** | **3.638** |