Fractal evolution of dual pH- and temperature-responsive P(NIPAM-co-AA)@BMMs with bimodal mesoporous silica core and coated-copolymer shell during drug delivery procedure via SAXS characterization

# Jiayu Maa, Jihong Suna*, Li Fanb*, Shiyang Baia, Hamida Panezaia, Yuwen Jiaob

a Beijing Key Laboratory for Green Catalysis and Separation, Department of Chemistry and Chemical Engineering, Beijing University of Technology, Beijing, 100124, China

b Department of Pharmaceutical chemistry and analysis, School of Pharmacy, The Fourth Military Medical University, Xi’an, 7100032, Shaanxi Province, China

Electronic Supporting Information

Lists of Figures and Tables captions:

Figure S1. The calibrated curve of IBU concentration through HPLC analysis.

Figure S2. The calibrated curve of IBU concentration generated through UV analysis under different releasing media in pH value of (A) pH 2.0 and (B) pH 7.4.

Figure S3. TG curves of pre and after copolymer-coated samples (A), as well as drug-loaded samples (B). (a) BMMs, (b) BMMs-MPS, (c) P@BMMs(1), (d) P@BMMs(2), (e) P@BMMs(4), (f) P@BMMs(7), (g) I/P@BMMs(1)-48, (h) I/P@BMMs(2)-48, (i) I/P@BMMs(4)-48, and (j) I/P@BMMs(7)-48.

Figure S4. FT-IR spectra of (a) BMMs, (b) BMMs-MPS, (c) P@BMMs(7), (d) I/P@BMMs(7)-48, (e) I/P@BMMs(7)-48-24 obtained after release at 37 oC in pH 2.0, (f) I/P@BMMs(7)-48-24 obtained after release at 37 oC in pH 7.4, and (g) IBU.

Figure S5. A: SAXS patterns of I/P@BMMs(1)-48-24 and corresponding Dm values (inset); B: r-p(r) chart of I/P@BMMs(1)-48-24 under different conditions of drug releasing. (a) 25 oC, pH 2.0, (b) 25 oC, pH 7.4, (c) 37 oC, pH 2.0, (d) 37 oC, pH 7.4.

Figure S6. A: SAXS patterns of I/P@BMMs(2)-48-24 and corresponding Dm values (inset); B: r-p(r) chart of I/P@BMMs(2)-48-24 under different conditions of drug releasing. (a) 25 oC, pH 2.0, (b) 25 oC, pH 7.4, (c) 37 oC, pH 2.0, (d) 37 oC, pH 7.4.

Figure S7. A: SAXS patterns of I/P@BMMs(7)-48-24 and corresponding Dm values (inset); B: r-p(r) chart of I/P@BMMs(7)-48-24 under different conditions of drug releasing. (a) 25 oC, pH 2.0, (b) 25 oC, pH 7.4, (c) 37 oC, pH 2.0, (d) 37 oC, pH 7.4.

Table S1. Elemental composition of all related samples.

Table S2. The textural parameters of all related samples.

Figure S1.

Figure S1. The calibrated curve of IBU concentration through HPLC analysis

Figure S2.

Figure S2. The calibrated curve of IBU concentration generated through UV analysis under different releasing media in pH value of (A) pH 2.0 and (B) pH 7.4

Figure S3.

Figure S3. TG curves of pre and after copolymer-coated samples (A), as well as drug-loaded samples (B). (a) BMMs, (b) BMMs-MPS, (c) P@BMMs(1), (d) P@BMMs(2), (e) P@BMMs(4), (f) P@BMMs(7), (g) I/P@BMMs(1)-48, (h) I/P@BMMs(2)-48, (i) I/P@BMMs(4)-48, and (j) I/P@BMMs(7)-48

Figure S4.

Figure S4. FT-IR spectra of (a) BMMs, (b) BMMs-MPS, (c) P@BMMs(7), (d) I/P@BMMs(7)-48, (e) I/P@BMMs(7)-48-24 obtained after release at 37 oC in pH 2.0, (f) I/P@BMMs(7)-48-24 obtained after release at 37 oC in pH 7.4, and (g) IBU

Figure S5.

Figure S5. A: SAXS patterns of I/P@BMMs(1)-48-24 and corresponding Dm values (inset); B: r-p(r) chart of I/P@BMMs(1)-48-24 under different conditions of drug releasing. (a) 25 oC, pH 2.0, (b) 25 oC, pH 7.4, (c) 37 oC, pH 2.0, (d) 37 oC, pH 7.4

Figure S6.

Figure S6. A: SAXS patterns of I/P@BMMs(2)-48-24 and corresponding Dm values (inset); B: r-p(r) chart of I/P@BMMs(2)-48-24 under different conditions of drug releasing. (a) 25 oC, pH 2.0, (b) 25 oC, pH 7.4, (c) 37 oC, pH 2.0, (d) 37 oC, pH 7.4

Figure S7.

Figure S7. A: SAXS patterns of I/P@BMMs(7)-48-24 and corresponding Dm values (inset); B: r-p(r) chart of I/P@BMMs(7)-48-24 under different conditions of drug releasing. (a) 25 oC, pH 2.0, (b) 25 oC, pH 7.4, (c) 37 oC, pH 2.0, (d) 37 oC, pH 7.4

Table S1.

Table S1. Elemental composition of all related samples

| Samples | N content (wt%) | C content (wt%) | H content (wt%) | N/C (molar ratio) |
| --- | --- | --- | --- | --- |
| BMMs | 0 | 3.43 | 1.01 |  |
| BMMs-MPS | 0 | 11.65 | 5.7 |  |
| P@BMMs(1) | 1.58 | 11.67 | 5.83 | 0.12 |
| P@BMMs(2) | 2.34 | 13.18 | 7.96 | 0.15 |
| P@BMMs(7) | 4.35 | 27.36 | 10.82 | 0.14 |
| I/P@BMMs(1)-48 | 0.09 | 10.9 | 2.04 |  |
| I/P@BMMs(2)-48 | 0.14 | 10.32 | 2.26 |  |
| I/P@BMMs(4)-48 | 1.44 | 13.16 | 2.49 |  |
| I/P@BMMs(7)-48 | 1.43 | 20.42 | 3.49 |  |

Table S2.

Table S2. The textural parameters of all related samples

| Samples | SBET (m2/g) | Vp(cm3/g)a | Small mean pore (nm)b | Large mean pore (nm)b |
| --- | --- | --- | --- | --- |
| BMMs | 1073 | 1.74 | 3.04 | 19.9 |
| BMMs-MPS | 1043 | 1.74 | 3.19 | 21.1 |
| P@BMMs(1) | 1019 | 1.64 | 3.16 | 20.9 |
| P@BMMs(2) | 988 | 1.44 | 3.26 | 20.3 |
| P@BMMs(4) | 926 | 1.53 | 3.19 | 20.1 |
| P@BMMs(7) | 554 | 1.12 | 3.02 | 18.5 |
| I/P@BMMs(1)-48 | 669 | 1.29 | 2.54 | 27.7 |
| I/P@BMMs(2)-48 | 295 | 0.65 | 2.66 | 28.6 |
| I/P@BMMs(4)-48 | 587 | 1.05 | 2.52 | 33.2 |
| I/P@BMMs(7)-48 | 385 | 0.69 | 2.27 | 40.1 |

SBET: BET surface area. VP: pore volume.

a. Estimated from the amount adsorbed at a relative pressure (P/P0) of 0.99.

b. The pore size distribution was calculated from N2 adsorption branch of isotherm using BJH method.