Supporting information for

**Enhanced visible light photocatalytic activity of CeO2@Zn0.5Cd0.5S by facile Ce(IV)/Ce(III) cycle**

Zain Ul Abideen1, Fei Teng,1\* Wenhao Gu1, Zhicheng Yang,1 An Zhang1, Fangdi Zhao1,2

Abid Hussain Shah1

*1Jiangsu Engineering and Technology Research Centre of Environmental Cleaning Materials (ECM) , Collaborative Innovation Centre of Atmospheric Environment and Equipment Technology (CICAEET), Jiangsu Key Laboratory of Atmospheric Environment Monitoring and Pollution Control (AEMPC) , School of Environmental Science and Engineering, School of Chemistry and Materials, Nanjing University of Information Science and Technology，219 Ningliu Road, Nanjing 210044, China. Corresponding author. tfwd@163.com*

*2 Nanjing Fangzheng Construction Quality Testing Co., Ltd, 10-5 Wanshi, Zhenjiang Road, Nanjing 210003, China.*

**Experimental**

***Synthesis of CeO2;*** CeO2sample was synthesized by a simple hydrothermal method. Typically, 1 g of Ce(NO3)3.6H2O was dissolved in 35 mL of double distilled water under stirring. Then, 5 mL of 2M NaOH solution was added drop wise into the solution under vigorous stirring and stirred for 30 min. Subsequently solution was transferred into a 50 mL Teflon cup stainless steel autoclave and processed at 180o C for 12h. After reaction for 8 h, the autoclave was cooled to room temperature naturally; the solid was washed with distilled water and ethanol several times, respectively; and collected *via* centrifugation. Finally, the solid was dried at 60ο C in an oven overnight.

### Fig. S1



**(f)**

 ***h+***

 ***e-***

O2/O2•- = -0.28 V

**0**

**-2**

**-1**

**1**

**2**

•OH /H2O = 2.38 V

 **CB -0.29 V**

 **CeO2 3.10 eV**

 **VB 2.81 V**

Potential (V) *vs.* SHE

**Fig. S1** (a) XRD pattern; **(b)** SEM image; **(c)** UV-DRS spectrum; **(d)** Tauc plot;

**(e)** Mott–Schottky plot; **(f)** Energy band potentials of CeO2

**Figure S2**



**Figure S2** XPS survey spectra of the sample