Supplementary Material

FigureS1. (a) HR-TEM image of Graphene (inset : SAED pattern), (b),(c ) HR-TEM images of aerogel with different magnification.

FigureS2.(a) MPMS analysis of 3D-MPBRGO  and its attraction by external magnet (b).

FigureS3.(a) TGA analysis of 3D-MPBRGO

(a)

Figure S4. a) N2 adsorption/desorption isotherm and (b) BJH (Barret-Joyner-Halenda) pore size distribution curves for 3D-MPBRGO aerogel analysis.

Table S1.  BET and pore size values from BET and BJH plot

| BET plot |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Vm |  |  | 92.52 | [cm3(STP) g-1] |  |  |
| as, BET |  |  | 402.68 | [m2 g-1] |  |  |
| Total pore volume (p/p0=0.990) |  |  | 0.44 | [cm3 g-1] |  |  |
| Mean pore diameter |  |  | 4.34 | [nm] |  |  |
| BJH plot |  |  |  |  |  |  |
| Vp |  |  | 0.37 | [cm3 g-1] |  |  |
| dp,peak |  |  | 7.2 | [nm] |  |  |

Figure S5. HR-TEM EDX surface analysis of aerogel before Cesium ion adsorption

Figure S6. HR-TEM EDX surface analysis of aerogel after Cesium ion adsorption

Figure S7. Adsorption isotherm study (a) Langmuir (b) Freundlich (c)  Tempkin isotherm