Supporting information

Graphdiyne-actinyl complexes as potential catalytic materials: a DFT perspective from their structural, bonding, electronic and redox properties

Raza ullah shah Bacha,† Ting-Ting Lin,† Jun Yao‡ and Qing-Jiang Pan*,†

† Key Laboratory of Functional Inorganic Material Chemistry (Ministry of Education), School of Chemistry and Materials Science, Heilongjiang University, Harbin, 150080, China

‡ Inner Mongolia Key Laboratory of Carbon Nanomaterials, College of Chemistry and Chemical Engineering, Inner Mongolia University for Nationalities (IMUN), Tongliao 028000, China

Corresponding Authors:

panqjitc@163.com (QJPan)

ORCID: 0000-0003-2763-6976 (QJP)

Figure S1. Theoretically simulated IR spectra of GDY-(AnVO2)+ complexes

Figure S2. Summary of ADF calculated atomic charges of U, Np and Pu in GDY-(AnmO2)n+ complexes.

Figure S3. Density of states (DOS) of α-spin orbitals of GDY-(NpVIO2)2+ (left) and Orbital structures (right). (The Isosurface value of 0.03 au is used in this and rest of the MO figures)

Figure S4. Density of states (DOS) of α-spin orbitals of GDY-(PuVIO2)2+ (left) and Orbital structures (right).

Figure S5. Density of states (DOS) of α-spin orbitals of GDY-(UVO2)+ complex.

Figure S6. Orbital structures of highest occupied molecular orbitals (HOMO) and lowest unoccupied molecular orbitals (LUMO) of GDY-(UVO2)+ complex.

Figure S7. Density of states (DOS) of α-spin orbitals of GDY-(NpVO2)+ complex.

Figure S8. Orbital structures of highest occupied molecular orbitals (HOMO) and lowest unoccupied molecular orbitals of GDY-(NpVO2)+ complex.

Figure S9. Density of states (DOS) of α-spin orbitals of GDY-(PuVO2)+ complex.

Figure S10. Orbital structures of highest occupied molecular orbitals (HOMO) and lowest unoccupied molecular orbitals (LUMO) of GDY-(PuVO2)+ complex.

Figure S11. Energy level diagram α-spin orbitals of GDY-(AnVO2)+ and free GDY, where orbitals of π(GDY) and π*(GDY) are correlated.

Table S1. Calculated relative energies (eV) of GDY-(AnmO2)n+ complexes in various electron-spin states (ESS)..

| An complexes | ESS | ΔE | ΔE0 | ΔH | ΔG |
| --- | --- | --- | --- | --- | --- |
| GDY-(NpVO2)+ | Triplet | 0.000 | 0.000 | 0.000 | 0.000 |
|  | Singlet | 0.586 | 0.587 | 0.571 | 0.645 |
| GDY-(PuVO2)+ | Quartet | 0.000 | 0.000 | 0.000 | 0.000 |
|  | Doublet | 0.643 | 0.637 | 0.640 | 0.634 |
| GDY-(PuVIO2)2+ | Triplet | 0.000 | 0.000 | 0.000 | 0.000 |
|  | Singlet | 1.369 | 1.364 | 1.376 | 1.285 |

Table S2. QTAIM analysis showing (ρ), (2ρ), H(r), V(r), G(r), -G(r)/V(r), ɛ, and δ in (a.u.) and Eint in (eV) of GDY-(NpmO2)n+ complexes.a

| GDY-(NpVIO2)2+ |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bonds | ρ(r) | 2ρ(r) | H(r) | V(r) | G(r) | -G(r)/V(r) | ɛ | δ | Eint |
| An=O1 | 0.339 | 0.303 | -0.347 | -0.770 | 0.423 | 0.549 | 0.001 | 2.126 | -10.476 |
| An=O2 | 0.339 | 0.306 | -0.347 | -0.770 | 0.423 | 0.550 | 0.000 | 2.134 | -10.472 |
| An–C | 0.033 | 0.097 | -0.002 | -0.027 | 0.026 | 0.942 | 0.604 | 0.202 | -0.373 |
| C1≡C2 | 0.388 | -1.011 | -0.513 | -0.756 | 0.242 | 0.321 | 0.003 | 2.221 | -10.279 |
| C-C1 | 0.293 | -0.753 | -0.284 | -0.381 | 0.162 | 0.424 | 0.103 | 1.202 | -5.177 |
| C2-C3 | 0.317 | -0.827 | -0.329 | -0.450 | 0.122 | 0.270 | 0.033 | 1.380 | -6.125 |
| GDY-(NpVO2)+ |  |  |  |  |  |  |  |  |  |
| Bonds | ρ(r) | 2ρ(r) | H(r) | V(r) | G(r) | -G(r)/V(r) | ɛ | δ | Eint |
| An=O1 | 0.336 | 0.285 | -0.342 | -0.755 | 0.413 | 0.547 | 0.001 | 2.077 | -10.270 |
| An=O2 | 0.335 | 0.288 | -0.341 | -0.754 | 0.413 | 0.548 | 0.000 | 2.087 | -10.264 |
| An–C | 0.032 | 0.101 | -0.001 | -0.027 | 0.026 | 0.963 | 0.522 | 0.146 | -0.370 |
| C1≡C2 | 0.387 | -1.011 | -0.510 | -0.755 | 0.245 | 0.324 | 0.005 | 2.251 | -10.270 |
| C-C1 | 0.293 | -0.751 | -0.282 | -0.377 | 0.095 | 0.251 | 0.099 | 1.195 | -5.129 |
| C2-C3 | 0.317 | -0.829 | -0.329 | -0.450 | 0.121 | 0.270 | 0.024 | 1.375 | -6.123 |

a The density and laplacian for C≡C in GDY were 0.38262 and -0.10022, respectively.

| GDY-(PuVIO2)2+ |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bonds | ρ(r) | 2ρ(r) | H(r) | V(r) | G(r) | -G(r)/V(r) | ɛ | δ | Eint |
| An=O1 | 0.331 | 0.310 | -0.328 | -0.733 | 0.405 | 0.553 | 0.000 | 2.143 | -9.969 |
| An=O2 | 0.331 | 0.312 | -0.327 | -0.733 | 0.405 | 0.553 | 0.001 | 2.150 | -9.968 |
| An–C | 0.031 | 0.097 | -0.001 | -0.026 | 0.025 | 0.973 | 0.528 | 0.157 | -0.350 |
| C1≡C2 | 0.388 | -1.108 | -0.512 | -0.755 | 0.242 | 0.321 | 0.007 | 2.228 | -10.270 |
| C-C1 | 0.293 | -0.753 | -0.283 | -0.378 | 0.095 | 0.251 | 0.100 | 1.203 | -5.147 |
| C2-C3 | 0.317 | -0.833 | -0.329 | -0.451 | 0.121 | 0.269 | 0.031 | 1.381 | -6.129 |
| GDY-(PuVO2)+ |  |  |  |  |  |  |  |  |  |
| Bonds | ρ(r) | 2ρ(r) | H(r) | V(r) | G(r) | -G(r)/V(r) | ɛ | δ | Eint |
| An=O1 | 0.329 | 0.297 | -0.324 | -0.723 | 0.398 | 0.551 | 0.000 | 2.107 | -9.834 |
| An=O2 | 0.329 | 0.299 | -0.324 | -0.723 | 0.399 | 0.552 | 0.000 | 2.114 | -9.834 |
| An–C | 0.031 | 0.099 | 0.000 | -0.026 | 0.252 | 9.852 | 0.491 | 0.137 | -0.348 |
| C1≡C2 | 0.387 | -1.106 | -0.511 | -0.755 | 0.245 | 0.324 | 0.005 | 2.257 | -10.276 |
| C-C1 | 0.293 | -0.752 | -0.283 | -0.377 | 0.095 | 0.251 | 0.099 | 1.195 | -5.133 |
| C2-C3 | 0.317 | -0.833 | -0.329 | -0.450 | 0.121 | 0.269 | 0.027 | 1.374 | -6.127 |

Table S3. QTAIM analysis showing (ρ), (2ρ), H(r), V(r), G(r), -G(r)/V(r), ɛ, and δ in (a.u) and Eint in (eV) of GDY-(PumO2)n+ complexes.

a The density and laplacian for C≡C in GDY were 0.38262 and -0.10022, respectively.

Table S4. Calculated atomic charge analysis of GDY-(AnmO2)n+ complexes, calculated at ADF; PBE/TZP/water.

|  | Mulliken |  | Hirshfeld |  | Voronoi |  | MDC |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | U(VI) | O | U(VI) | O | U(VI) | O | U(VI) | O |
| Charge | 1.201 | -0.536 | 0.821 | -0.248 | 3.150 | -1.032 | 2.344 | -0.772 |
| Spin | 0 | 0 | — | — | — | — | — | — |
|  | U(V) | O | U(V) | O | U(V) | O | U(V) | O |
| Charge | 1.191 | -0.633 | 0.676 | -0.336 | 3.050 | -1.002 | 2.005 | -0.831 |
| Spin | 0.896 | -0.033 | — | — | — | — | — | — |
|  | Np(VI) | O | Np(VI) | O | Np(VI) | O | Np(VI) | O |
| Charge | 1.201 | -0.536 | 0.714 | -0.235 | 3.037 | -1.007 | 1.218 | -2.078 |
| Spin | 1.623 | -0.077 | — | — | — | — | — | — |
|  | Np(V) | O | Np(V) | O | Np(V) | O | Np(V) | O |
| Charge | 1.182 | -0.618 | 0.606 | -0.315 | 2.973 | -0.990 | 3.256 | -1.965 |
| Spin | 2.124 | -0.093 | — | — | — | — | — | — |
|  | Pu(VI) | O | Pu(VI) | O | Pu(VI) | O | Pu(VI) | O |
| Charge | 1.231 | -0.541 | 0.795 | -0.274 | 2.678 | -0.924 | 3.522 | -1.659 |
| Spin | 3.040 | -0.152 | — | — | — | — | — | — |
|  | Pu(V) | O | Pu(V) | O | Pu(V) | O | Pu(V) | O |
| Charge | 1.221 | -0.601 | 0.720 | -0.331 | 2.639 | -0.911 | 1.430 | -0.160 |
| Spin | 3.308 | -0.157 | — | — | — | — | — | — |

Table S5. Contribution (%) of molecular orbitals of GDY-(UVIO2)2+ complex. a

| Orbitals | Energy | % |  |  | Assignment |
| --- | --- | --- | --- | --- | --- |
|  | eV | U | GDY | Composition |  |
| L+4 | -4.290 | 1.35 | 90.74 | 90.74 C(pz), 1.35 U(fxyz) | π(GDY) |
| L+3 | -6.016 | 91.46 | — | 79.26 U(fz), 9.25 U(fx), 2.95 U(fxyz) | U(5f) |
| L+2 | -6.019 | 92.21 | — | 89.67 U(fxyz), 2.54 U(fz) | U(5f) |
| L+1 | -6.042 | 86.99 | 6.64 | 74.46 U(fxyz), 10.94 U(fz),1.59 U(fx) 3.13 C(py), 3.51 C(px) | U(5f) |
| LUMO | -6.389 | 90.04 | 2.23 | 90.04 U(fy), 2.23 C(py) | U(5f) |
| HOMO | -6.607 | 3.17 | 87.94 | 87.94 C(pz), 3.17 U(fz) | π(GDY) |
| H-1 | -6.608 | 3.19 | 82.18 | 82.18 C(pz), 3.19 U(fxyz) | π(GDY) |
| H-2 | -6.989 | — | 89.47 | 89.47 C(pz) | π(GDY) |
| H-3 | -7.729 | — | 87.53 | 87.53 C(pz) | π(GDY) |

a fx, fy and fz are used to denote fx(x2-3y2), fy(3x2-y2) and fz(x2-y2), respectively.

Table S6. Contribution (%) of molecular orbitals of GDY-(NpVIO2)2+ complex.

| Orbitals | Energy | % |  |  | Assignment |
| --- | --- | --- | --- | --- | --- |
|  | eV | Np | GDY | Composition |  |
| L+5 | -4.263 | — | 89.12 | 89.12 C(pz) | π(GDY) |
| L+4 | -4.528 | 95.29 | — | 39.41 Np(5fz2y), 28.50 Np (5fz2x), 15.41 O(py), 11.57 O(px) | Np(5f) |
| L+3 | -4.529 | 95.70 | — | 39.20 Np(fz2x), 28.50 Np(fz2x), 14.26 O(py), 13.06 O(py) | Np(5f) |
| L+2 | -5.727 | 88.80 | 5.95 | 88.80 Np(fx), 5.95 C(px) | Np(5f) |
| L+1 | -6.362 | 75.57 | 14.62 | 61.63 Np(fxyz), 13.94 Np(fz), 14.62 C(pz) | Np(5f)+ π(GDY) |
| LUMO | -6.376 | 72.53 | 17.72 | 59.01 Np(fz), 13.52 Np(fxyz), 17.72 C(pz) | Np(5f)+ π(GDY) |
| HOMO | -6.593 | 21.84 | 69.01 | 69.01 C(pz), 18.24 Np(fxyz), 3.60 Np(fz) | π(GDY)+ Np(5f) |
| H-1 | -6.598 | 24.89 | 67.28 | 67.28 C(pz), 20.87 Np(fz), 4.02 Np(fxyz) | π(GDY)+Np(5f) |
| H-2 | -6.753 | 93.81 | 0.71 | 93.81 Np(fy), 0.71 C(py) | Np(5f) |
| H-3 | -6.968 | — | 90.25 | 90.25 C(pz) | π(GDY) |

Table S7. Contribution (%) of molecular orbitals of GDY-(PuVIO2)2+ complex.

| Orbitals | Energy |  | % |  |  | Assignment |
| --- | --- | --- | --- | --- | --- | --- |
|  | eV | Pu |  | GDY | Composition |  |
| L+4 | -4.315 | — |  | 92.52 | 92.52 C(pz) | π(GDY) |
| L+3 | -4.644 | 66.74 |  | 28.12 | 66.74 Pu(fz2y), 28.12 C(py) | Pu(5f)+ π(GDY) |
| L+2 | -4.649 | 66.10 |  | 28.77 | 66.10 Pu(fz2x), 28.77 C(px) | Pu(5f)+ π(GDY) |
| L+1 | -5.927 | 89.78 |  | 4.92 | 88.05 Pu(fx), 1.73 Pu(fx), 4.92 C(py) | Pu(5f) |
| LUMO | -6.449 | 29.09 |  | 60.21 | 29.09 Pu(fxyz), 60.21 C(pz) | Pu(5f)+π*(GDY) |
| HOMO | -6.513 | 10.12 |  | 81.52 | 10.12 Pu(fz), 81.52 C(pz) | π(GDY) |
| H-1 | -6.651 | 68.06 |  | 24.16 | 68.06 Pu(fxyz), 24.16 C(pz) | Pu(5f)+ π(GDY) |
| H-2 | -6.742 | 86.81 |  | 4.54 | 86.81 Pu(fz), 4.54 C(pz) | Pu(5f) |
| H-3 | -6.879 | 94.60 |  | 0.55 | 94.60 Pu(fy), 0.55 C(py) | Pu(5f) |
| H-4 | -6.971 | — |  | 90.36 | 90.36 C(pz) | π(GDY) |

Table S8. Contribution % of molecular orbitals of GDY-(UVO2)+ complex.

| Orbitals | Energy | % |  |  | Assignment |
| --- | --- | --- | --- | --- | --- |
|  | eV | U | GDY | Composition |  |
| L+4 | -3.789 | 11.75 | 81.67 | 81.67 C(pz), 11.75 U(fz), | π(GDY) |
| L+3 | -3.789 | 11.74 | 84.16 | 84.16 C(pz), 11.74 U(fxyz) | π(GDY) |
| L+2 | -3.868 | 93.26 | 0.80 | 93.26 U(fx), 0.80 C(py) | U(5f) |
| L+1 | -4.393 | 86.38 | 3.89 | 60.29 U(fz), 26.07 U(fxyz), 3.89 C(pz) | U(5f) |
| LUMO | -4.394 | 86.41 | 3.21 | 60.31 U(fxyz), 26.09 U(fz), 3.21 C(pz) | U(5f) |
| HOMO | -4.977 | 78.63 | 11.97 | 78.63 U(fy), 6.75 C(py), 5.22 C(px) | U(5f)+ π(GDY) |
| H-1 | -6.176 | — | 91.53 | 91.53 C(pz) | π(GDY) |
| H-2 | -6.176 | — | 90.96 | 90.96 C(pz) | π(GDY) |
| H-3 | -6.630 | — | 91.38 | 91.38 C(pz) | π(GDY) |

Table S9. Contribution % of molecular orbitals of GDY-(NpVO2)+ complex.

| Orbitals | Energy | % |  |  | Assignment |
| --- | --- | --- | --- | --- | --- |
|  | eV | Np | GDY | Composition |  |
| L+4 | -3.323 | 36.49 | 34.09 | 25.10 Np(fz2y), 11.39 Np(fz2x), 2.47 (dx2-y2), 1.82 (dxy), 34.09 C(py), 13.52 O(py) | Np(5f) +π(GDY) |
| L+3 | -3.830 | 3.29 | 90.52 | 90.52 C(py), 3.29 Np(fxyz) | π(GDY) |
| L+2 | -3.838 | 1.42 | 93.93 | 93.93 C(pz), 1.42 Np(fz) | π(GDY) |
| L+1 | -4.423 | 92.36 | 1.08 | 92.36 Np(fx), 1.08 C(py) | Np(5f) |
| LUMO | -4.800 | 94.68 | — | 89.02 Np(fxyz), 5.66 Np(fz) | Np(5f) |
| HOMO | -5.279 | 96.00 | — | 90.25 Np(fz), 5.75 Np(fxyz) | Np(5f) |
| H-1 | -5.423 | 89.28 | 2.22 | 89.28 Np(fy), 2.22 C(py) | Np(5f) |
| H-2 | -6.171 | — | 89.58 | 89.58 C(pz) | π(GDY) |
| H-3 | -6.178 | 1.12 | 91.17 | 91.17 C(pz), 1.12 Np(fz) | π(GDY) |

Table S10. Contribution % of molecular orbitals of GDY-(PuVO2)+ complex.

| Orbitals | Energy | % |  |  | Assignment |
| --- | --- | --- | --- | --- | --- |
|  | eV | Pu | GDY | Composition |  |
| L+5 | -3.227 | 6.55 | 88.54 | 88.54 C(pz), 6.55 Pu(fx) | π(GDY) |
| L+4 | -3.770 | 66.87 | 26.54 | 66.87 Pu(fz2x), 26.54 C(px) | Pu(5f),π(GDY) |
| L+3 | -3.771 | 67.51 | 26.25 | 67.51 Pu(fz2y), 26.25 C(py) | Pu(5f)+π(GDY) |
| L+2 | -3.842 | — | 93.64 | 93.64 C(pz) | π(GDY) |
| L+1 | -3.843 | — | 94.21 | 94.21 C(pz) | π(GDY) |
| LUMO | -4.947 | 93.16 | — | 93.16 Pu(fx) | Pu(5f) |
| HOMO | -5.646 | 94.90 | — | 60.50 Pu(fz), 34.40 Pu(fxyz) | Pu(5f) |
| H-1 | -5.647 | 94.87 | — | 60.60 Pu(fxyz), 34.27 Pu(fz) | Pu(5f) |
| H-2 | -5.895 | 93.67 | 0.74 | 93.67 Pu(fy), 0.74 C(py) | Pu(5f) |
| H-3 | -6.174 | 2.69 | 89.84 | 2.69 Pu(fxyz), 89.84 C(pz) | π(GDY) |