Supplementary Information

Fluorescent pH indicators for alkaline pH range based on perylene tetra-(alkoxycarbonyl) derivatives

Fengxia Zhang a, Wenyao Dong c, Yongshan Ma a*, Tianyi Jiang a, Bing Liu a,b, Xuemei Li a, Yuanyuan Shao a and Junsen Wu a

a School of Municipal and Environmental Engineering, Shandong Jianzhu University, Jinan 250101，Shandong，China.

b Resources and Environment Innovation Research Institute，Jinan，250101，Shandong，China.

c the First Clinical Medical College of Shandong University of Chinese Medicine.* Corresponding author. E-mail: mlosh@sdjzu.edu.cn (Y. Ma). Tel.: +86 531 86361570.

Table of contents

1. Synthesis protocols

2. Samples characteriaztions profiles

- Synthesis protocols

Scheme S1. The synthesis route of probes 1a-b

General procedure for the synthesis of 3a

Fuming nitric acid (3.0mL) was added dropwise into a solution containing compound 2a (2.0g, 3.0 mmol）and dichloromethane (200mL). The mixture was stirred at room temperature for 3h. Sodium bicarbonate solution (20%, 100 mL) was added in the resulting mixture. The organic phase was washed with water 3 times (100 ml×3) and dried with anhydrous MgSO4. Then the solvent was evaporated on a rotary evaporator until dry. The solid was purified on silica gel chromatographyeluted with dichloromethane/petroleum ether (2:1, v/v). After evaporated the eluent, it afford target red solid (0.9g, 86%). Characterization data: 1H-NMR(300 MHz, CDCl3, δ ppm): 8.40 (s, 1H), 8.37 (m, 2H), 8.26 (d, 1H), 8.14 (d, 1H, J=6 Hz), 7.97 (d, 1H, J=6 Hz), 7.93 (d, 1H, J=9 Hz), 4.37 (m, 8H), 1.82 (m, 8H), 1.55 (m, 8H), 1.03 (m, 12H). 13C NMR (75 MHz, CDCl3, δ ppm) : 168.06, 167.86, 167.79, 166.60, 146.32, 133.91, 132.53, 131.96, 131.61, 130.83, 130.51, 130.38, 130.00, 129.15, 128.73, 128.48, 127.92, 127.40, 126.63, 125.62, 123.13, 122.61, 66.02, 65.64, 65.58, 30.60, 19.23, 13.74. FT-IR (KBr, cm-1): v = 2959, 2871, 1711, 1589, 1529, 1460, 1394, 1353, 1274, 1249, 1163, 1108, 1062, 1021, 959, 899, 846, 801, 736, 702, 604, 506, 434. HRMS (APCI): m/z = 697.2913 (M + Na+).

General procedure for the synthesis of 1a.

A mixture of 3a (1.0 g, 1.5 mmol), ammonium chloride (0.8 g, 16.0 mmol) and zinc powder (0.5 g, 8.0 mmol) was stirred in tetrahydrofuran (80 mL) at room temperature for 3 h. The ammonium chloride and zinc powder were filtered. After evaporated the eluent, the crude product was purified on silica gel column chromatography with dichloromethane/ethyl acetate (20:1, V/V), affording dark brown solid (378.5 mg, 80%). Characterization data: 1HNMR (400 MHz, CDCl3, δ ppm): 8.08 (d, 1H, J=6 Hz), 8.06 (d, 1H, J=6 Hz), 7.94 (d, 1H, J=9 Hz), 7.80 (d, 1H, J=9 Hz), 7.70 (s, 1H), 7.33 (s, 1H), 4.57 (s, 1H), 4.32-4.34 (m, 8H), 3.83 (s, 2H), 1.72-1.84 (m, 8H), 1.46-1.53 (m, 8H), 0.96-1.04 (m,12H).13C-NMR (75 MHz, CDCl3,ppm): δ=169.03, 168.94, 167.96, 167.78, 155.68, 143.19, 133.47, 131.99, 131.80, 131.61, 129.97, 129.76, 128.87, 128.78, 127.42, 127.01, 126.20, 125.83, 125.57, 123.54, 122.18, 120.58, 90.57, 65.27, 65.19, 62.15, 31.06, 30.70, 30.60, 27.44, 19.28, 19.20, 13.79. FT-IR (KBr, cm-1): v = 3361, 3265, 3179, 2968, 2863, 1689, 1583, 1449, 1373, 1249, 1201, 1154, 1039, 857, 781, 752, 695. HRMS (APCI): m/z = 682.3004 [M-H]-.

General procedure for the synthesis of 2b.

Compound 3a (120 mg, 0.2 mmol) was dissolved in N-methylpyrrolidone (NMP, 10 ml). The resulting solution was stirred at 130℃ under O2 for 4 h until the starting material could not be detected by TLC, and then poured into 100 ml of 2 M HCl. The precipitate was collected by vacuum filtration and washed with water. After solvent was removed under vacuum, the crude product was purified by silica gel column chromatography with eluent dichloromethane/petroleum ether (5/2, V/V). After solvent was removed, a yellow solid of 34 mg (30%) 2b was obtained. 1H NMR (CDCl3, 400 MHz, ppm): 8.88 (d, 2H), 8.73 (s, 1H), 8.38 (d, 2H), 4.40-4.44 (m, 8), 1.82 (m, 8H), 1.50-1.55 (m, 8H), 0.89-1.04 (m, 12H). 13C NMR (100 MHz, CDCl3, δ ppm): 168.56, 168.50, 135.71, 132.40, 130.98, 130.13, 129.55, 129.33, 126.27, 125.96, 125.60, 121.80, 65.58, 65.47, 30.70, 19.29, 13.77. FT-IR (KBr, cm-1): v = 2921, 2846, 1692, 1652, 1612, 1416, 1344, 1308, 1258, 1178, 1000, 893, 852, 803, 736, 628, 578. MS (APCI-TOF) m/z = 666.2817 (M+)。

General procedure for the synthesis of 3b.

The compound 3b was synthesized according to the procedure of 3a, Briefly, Compound 2b (280 mg, 0.4 mmol) and fuming nitric acid (2.5 mL) reacted for 3 h in dichloromethane at room temperature to yield 3a (252mg, 87%). Characterization data: 1HNMR (400 MHz, CDCl3, δ ppm): 8.86 (s, 1H), 8.77 (s, 1H), 8.44 (d, 2H), 8.40 (s, 1H), 8.31 (d, 1H), 4.40-4.46 (m, 8), 1.81-1.89 (m, 8H), 1.52-1.57 (m, 8H), 1.00-1.04 (m, 12H). 13C NMR (100 MHz, CDCl3, δ ppm): 168.09, 167.91, 167.82, 166.55, 145.48, 136.24, 136.10, 132.05, 130.91, 130.50, 130.00, 129.27, 127.77, 127.36, 126.68, 126.52, 126.06, 125.82, 125.45, 123.81, 122.88, 66.16, 65.92, 65.80, 65.73, 30.65, 30.58, 19.25, 13.74. HRMS (APCI): m/z = 711.2732 (M + Na+).

General procedure for the synthesis of 1b.

Potassium carbonate (150 mg, 1.0 mmol) was added into a solution containing compound 3b (150mg, 0.2mmol) and N-methylpyrrolidone (15ml). Under N2, the resulting solution was stirred at 60℃ for 5h. After cooling to room temperature, the mixture was poured into HCl (100ml, 2 M). The mixture is filtered, and the granular precipitate is washed thoroughly with water and dried under vacuum condition. The residue was purified by gel column chromatography with dichloromethane /ethyl acetate (20/1) as eluent to afford red solid 1b (136mg, 86%). Characterization data: 1H-NMR (CDCl3, 300 MHz, δ ppm): 11.09 (s, 1H), 9.73 (d, J = 9.0 Hz, 1H), 8.71 (s, 1H), 8.55 (s, 1H), 8.33 (s, 1H), 8.11 (d, 1H), 4.34-4.43 (m, 8), 1.74 (m, 8H), 1.48 (m, 8H), 0.88-0.99 (m, 12H). 13C NMR (75 MHz, CDCl3, δ ppm): 169.59, 169.20, 168.81, 153.19, 129.87, 129.08, 128.16, 127.77, 126.94, 126.77, 125.43, 124.15, 123.01, 122.27, 119.10, 116.71, 65.71, 65.61, 65.42, 30.81, 29.67, 19.34, 13.84. FT-IR (KBr, cm−1): v = 3365, 3189, 2922, 2854, 1651, 1462, 1410, 1067, 873, 732, 661, 586, 528, 486, 437. HRMS (APCI): m/z = 682.2869 (M+ -H).

- Sample characterizations profiles

Figure S1. 1H NMR spectrum of compound 3a.

Figure S2. 13 C NMR spectrum of compound 3a.

Figure S3. FT-IR profile of compound 3a.

Figure S4. HRMS profile of compound 3a.

Figure S5. 1H NMR spectrum of compound 1a.

Figure S6. 13 C NMR spectrum of compound 1a.

Figure S7. FT-IR profile of compound 1a.

Figure S8. HRMS profile of compound 1a.

Figure S9. 1H NMR spectrum of compound 2b.

Figure S10. 13C NMR spectrum of compound 2b.

Figure S11. FT-IR profile of compound 2b.

Figure S12. HRMS profile of compound 2b.

Figure S13. 1H NMR spectrum of compound 3b.

Figure Figure S14. 13 C NMR spectrum of compound 3b.

Figure S15. HRMS profile of compound 3b.

Figure S16. 1H NMR spectrum of compound 1b.

Figure S17. 13 C NMR spectrum of compound 1b.

Figure S18. FT-IR profile of compound 1b.

Figure S19. HRMS profile of compound 1b.