Electronic Supplementary Information

High-efficiency electrodeposition of polyindole nanocomposite using MoS2 nanosheets as electrolytes and their capacitive performance

Liming Xua, §, Danqin Lia, §, Weiqiang Zhoua, b, *, Yongbo Dinga, Yanli Wua, Jingkun Xua,*, Xuemin Duana

a Flexible Electronics Innovation Institute (FEII), Jiangxi Science and Technology Normal University, Nanchang 330013, PR China

b Jiangxi Engineering Laboratory of Waterborne Coatings, Jiangxi Science and Technology Normal University, Nanchang 330013, PR China

* Corresponding author: Fax: +86-791-83823320, Tel.: +86-791-88537967, E-mail: zhouwqh@163.com; xujingkun@tsinghua.org.cn.

§ Liming Xu and Danqin Li contributed equally to this work.

Calculation of the specific capacitance

According to the literature, it is more appropriate to use the area specific capacitance to characterize the electrode material capacity than mass specific capacitance (Horng et al., 2010; Liu et al., 2012). Therefore, the area specific capacitance was calculated from CV (Eq. 1) and GCD (Eq. 2):

Cs=idV /2S×∆V×v         (1)

Cs=I∆tS∆V                     (2)

where Cs is the area capacitance (mF cm-2), idV is the integrated area of the CV curve, S is the surface area of active materials in the single electrode (cm2), ∆V is the potential window (V), v is the scan rate (mV s-1), I is the current density (A), and ∆t is the discharge time (s).

Calculation of the effective surface areas

The effective surface areas of PIn and PIn/MoS2 electrodes were tested by CV with 5 mM K3Fe(CN)6 as a probe at different scan rates (T = 298 K). For a reversible process, the following Eq. 3 applies (Wang et al., 2007; Yang et al., 2009):

ip = 2.69 × 105 An3/2DR1/2Cov1/2        (3)

where ip refers to the peak current (A) and A is the electrode area (cm2). For 5 mM K3Fe(CN)6, n = 1, DR = 7.6 × 10-6 cm2 s-1 (0.1 M KCl), Co is the concentration of K3Fe(CN)6 (M), v is the scan rate (V s-1), then the effective surface areas was calculated from the slope (k) of the ip versus v1/2 plot (Fig. S3) to be 0.11 cm2 for PIn electrode and 0.23 cm2 for PIn/MoS2 electrode.

Fig. S1 Digital photo of MoS2 ACN solution.

Fig. S2 AFM images and corresponding data of exfoliated MoS2.

Fig. S3 The peak current of PIn and PIn/MoS2 electrodes in 5 mM K3Fe(CN)6 containing 0.1 M KCl as a function of the square root of scan rates.

Fig. S4 EDX spectral of PIn/MoS2.

Fig. S5 Survey scan X-ray photoelectron spectrum of PIn/MoS2.

Fig. S6 The CVs of MoS2 at different scan rates (A) and the specific capacitance as a function scan rate (B).

Fig. S7 The peak current densities of PIn/MoS2 as a function of scan rates (A) and square root of scan rates (B), respectively. jp, jp,a, jp,c are deﬁned as the peak current densities, the anodic peak current densities at about 0.5 V, and the cathodic peak current densities at about 0.4 V, respectively.

References

Horng, Y., Lu, Y., Hsu, Y., Chen, C., Chen, L., Chen, K., 2010. Flexible supercapacitor based on polyaniline nanowires/carbon cloth with both high gravimetric and area-normalized capacitance. J. Power Sources 195, 4418-4422.

Liu, J., Jiang, J., Bosman, M., Fan. H., 2012. Three-dimensional tubular arrays of MnO2-NiO nanoflakes with high areal pseudocapacitance. J. Mater. Chem. 22, 2419-2426.

Wang, S., Xie, F., Hu, F., 2007. Electrochemical study of brucine on an electrode modified with magnetic carbon-coated nickel nanoparticles. Anal. Bioanal. Chem. 387, 933-939.

Yang, L., Tang, C., Xiong, H., Zhang, X., Wang, S., 2009. Electrochemical properties of catechin at a single-walled carbon nanotubes-cetylramethylammonium bromide modiﬁed electrode. Bioelectrochemistry 75, 158-162.