Substituent effect on the catalytic activity of dinuclear Zn(II) and Cu(II), 3- and 4-pyridinyl Schiff complexes in the ring-opening polymerization of cyclic esters

Damilola C. Akintayo1, Wisdom A. Munzeiwa2, Bernard Omondi3*, Sreekantha B. Jonnalagadda1

1School of Chemistry & Physics, University of KwaZulu-Natal, Westville Campus, Private Bag X54001, Durban, 4000, South Africa.

2Chemistry Department, Bindura University of Science Education, Private Bag 1020, Bindura Zimbabwe.

3School of Chemistry & Physics, University of KwaZulu-Natal, Pietermaritzburg Campus, Private Bag X01, Scottville, 3209, South Africa

*Corresponding author: owaga@ukzn.ac.za

Supplementary information

Table of Contents

1H NMR SPECTRA OF L1 – L10	4

Figure S1: (E)-N-(p-tolyl)-1-(pyridin-4-yl)methanimine L1	4

Figure S2: (E)-N-(2,6-diisopropylphenyl)-1-(pyridin-4-yl)methanimine L2	5

Figure S3: (E)-N-(4-chlorophenyl)-1-(pyridin-4-yl)methanimine L3	6

Figure S4: (E)-N-(2,6-dimethylphenyl)-1-(pyridin-4-yl)methanimine L4	7

Figure S5: (E)-N-phenyl-1-(pyridin-4-yl)methanimine L5	8

Figure S6: (E)-1-(pyridin-3-yl)-N-(p-tolyl)methanimine L6	9

Figure S7: (E)-N-(2,6-diisopropylphenyl)-1-(pyridin-3-yl)methanimine L7	10

Figure S8: (E)-N-(4-chlorophenyl)-1-(pyridin-3-yl)methanimine L8	11

Figure S9: (E)-N-(2,6-dimethylphenyl)-1-(pyridin-3-yl)methanimine L9	12

Figure S10: (E)-N-phenyl-1-(pyridin-3-yl)methanimine L10	13

13C NMR spectra of L1 – L10	14

Figure S11: (E)-N-(p-tolyl)-1-(pyridin-4-yl)methanimine L1	14

Figure S12: (E)-N-(2,6-diisopropylphenyl)-1-(pyridin-4-yl)methanimine L2	15

Figure S13: (E)-N-(4-chlorophenyl)-1-(pyridin-4-yl)methanimine L3	16

Figure S14: (E)-N-(2,6-dimethylphenyl)-1-(pyridin-4-yl)methanimine L4	17

Figure S15: (E)-N-phenyl-1-(pyridin-4-yl)methanimine L5	18

Figure S16: (E)-1-(pyridin-3-yl)-N-(p-tolyl)methanimine L6	19

Figure S17: (E)-N-(2,6-diisopropylphenyl)-1-(pyridin-3-yl)methanimine L7	20

Figure S18: (E)-N-(4-chlorophenyl)-1-(pyridin-3-yl)methanimine L8	21

Figure S19: (E)-N-(2,6-dimethylphenyl)-1-(pyridin-3-yl)methanimine L9	22

Figure S20: (E)-N-phenyl-1-(pyridin-3-yl)methanimine L10	23

1H NMR spectra of complexes 1, 3 and 5	24

Figure S21: 1H NMR spectrum of complex 1 in CDCl3 at room temperature	24

Figure S22: 1H NMR spectrum of complex 3 in CDCl3 at room temperature	25

Figure S23: 1H NMR spectrum of complex 5 in CDCl3 at room temperature	26

13C NMR spectra of complexes 1, 3 and 5	27

Figure S24: 13C NMR spectrum of complex 1 in CDCl3 at room temperature.	27

Figure S25: 13C NMR spectrum of complex 3 in CDCl3 at room temperature.	28

Figure S26: 13C NMR spectrum of complex 5 in CDCl3 at room temperature.	29

Figure S27: An overlay of complex 9 (blue) and complex 11 (red)	32

Figure S28: Packing diagram of complexes 9 as viewed down the crystallographic a-axis direction. Hydrogen atoms have been omitted for clarity.	33

Figure S29: Packing diagram of complexes 11 as viewed down the crystallographic a-axis direction. Hydrogen atoms have been omitted for clarity.	34

Figure S30: Pseudo-first-order logarithmic plot for the polymerization of rac-LA and L-LA in toluene at 110 °C by complex 5.	35

Figure S31: Pseudo-first-order logarithmic plot for the bulk polymerization of CL at 110 °C by complexes 2, 4, 6, 7 and 8.	36

Figure S32: Pseudo-first-order logarithmic plot for the bulk polymerization of CL at 110 °C by complexes 9, 10, 11, 12 and 13.	37

Figure S33: The 1H-NMR spectrum of poly(ε-CL) initiated by complex 7 in different alcohol at room temperature in CDCl3 (400 MHz). Reaction conditions: [CL] 0 :[I]0:[ROH]0  = 200:1, bulk, T = 110 °C	38

Figure S34: The 1H-NMR spectrum of poly(L-LA) initiated by complex 5 at room temperature in CDCl3 (400 MHz). Reaction conditions: [LA] 0 :[I]0 = 200:1, bulk, T = 110 °C.	39

Figure S35: ESI-MS spectrum of poly(L-LA) initiated by complex 5. Reaction conditions: [LA]0 :[I]0 = 200:1, bulk, T = 110 °C.	40

Figure S36: 13C NMR spectrum of the methine and carbonyl region of PLA obtained by complex 5 in CDCl3 at room temperature.	41

MASS SPECTRA OF CARBOXYLATE COMPLEXES	42

Figure S37: ESI-MS spectrum of complex 1	42

Figure S38: ESI-MS spectrum of complex 10	43

MASS SPECTRA OF POLYMERS	44

Figure S39: ESI-MS spectrum of PCL obtained from complex 7	44

Figure S40: ESI-MS spectrum of PCL obtained from complex 7 in benzyl alcohol	45

Figure S41: ESI-MS spectrum of PCL obtained from complex 7 in isopropyl alcohol	46

Figure S42: ESI-MS spectrum of poly(rac-lA) obtained from complex 5	47

# 1H NMR SPECTRA OF L1 – L10

## Figure S1: (E)-N-(p-tolyl)-1-(pyridin-4-yl)methanimine L1

## Figure S2: (E)-N-(2,6-diisopropylphenyl)-1-(pyridin-4-yl)methanimine L2

## Figure S3: (E)-N-(4-chlorophenyl)-1-(pyridin-4-yl)methanimine L3

## Figure S4: (E)-N-(2,6-dimethylphenyl)-1-(pyridin-4-yl)methanimine L4

## Figure S5: (E)-N-phenyl-1-(pyridin-4-yl)methanimine L5

## Figure S6: (E)-1-(pyridin-3-yl)-N-(p-tolyl)methanimine L6

## Figure S7: (E)-N-(2,6-diisopropylphenyl)-1-(pyridin-3-yl)methanimine L7

## Figure S8: (E)-N-(4-chlorophenyl)-1-(pyridin-3-yl)methanimine L8

## Figure S9: (E)-N-(2,6-dimethylphenyl)-1-(pyridin-3-yl)methanimine L9

## Figure S10: (E)-N-phenyl-1-(pyridin-3-yl)methanimine L10

# 13C NMR spectra of L1 – L10

## Figure S11: (E)-N-(p-tolyl)-1-(pyridin-4-yl)methanimine L1

## Figure S12: (E)-N-(2,6-diisopropylphenyl)-1-(pyridin-4-yl)methanimine L2

## Figure S13: (E)-N-(4-chlorophenyl)-1-(pyridin-4-yl)methanimine L3

## Figure S14: (E)-N-(2,6-dimethylphenyl)-1-(pyridin-4-yl)methanimine L4

## Figure S15: (E)-N-phenyl-1-(pyridin-4-yl)methanimine L5

## Figure S16: (E)-1-(pyridin-3-yl)-N-(p-tolyl)methanimine L6

## Figure S17: (E)-N-(2,6-diisopropylphenyl)-1-(pyridin-3-yl)methanimine L7

## Figure S18: (E)-N-(4-chlorophenyl)-1-(pyridin-3-yl)methanimine L8

## Figure S19: (E)-N-(2,6-dimethylphenyl)-1-(pyridin-3-yl)methanimine L9

## Figure S20: (E)-N-phenyl-1-(pyridin-3-yl)methanimine L10

# 1H NMR spectra of complexes 1, 3 and 5

## Figure S21: 1H NMR spectrum of complex 1 in CDCl3 at room temperature

## Figure S22: 1H NMR spectrum of complex 3 in CDCl3 at room temperature

## Figure S23: 1H NMR spectrum of complex 5 in CDCl3 at room temperature

# 13C NMR spectra of complexes 1, 3 and 5

## Figure S24: 13C NMR spectrum of complex 1 in CDCl3 at room temperature.

## Figure S25: 13C NMR spectrum of complex 3 in CDCl3 at room temperature.

## Figure S26: 13C NMR spectrum of complex 5 in CDCl3 at room temperature.

Table S1: Summarized wavelengths and transitions of complexes 1 – 13

| Complex | Wavelength | Transition |
| --- | --- | --- |
| 1 | 241, 270, 332 | π-π*, n-π* |
| 2 | 234, 266, 334 | π-π*, n-π* |
| 3 | 241, 357 | π-π*, n-π* |
| 4 | 236, 346 | π-π*, n-π* |
| 5 | 241, 267, 330 | π-π*, n-π* |
| 6 | 234, 262, 325 | π-π*, n-π* |
| 7 | 234, 341 | π-π*, n-π* |
| 8 | 231, 260, 324 | π-π*, n-π* |
| 9 | 241, 325 | π-π*, n-π* |
| 10 | 246, 346 | π-π*, n-π* |
| 11 | 250, 325 | π-π* π-π*, |
| 12 | 241, 343 | π-π*, n-π* |
| 13 | 253, 325 | π-π*, n-π* |

Table S2: Shift in the proton of ligands and complexes

| Entry | Complexes | NMR |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | d, py 2H |  | Δυ | d, py 2H |  | Δυ |
|  |  | Ligand | Complex |  | Ligand | Complex |  |
| 1 | 1 | 8.73 | 8.84 | 0.11 | 7.73 | 7.90 | 0.17 |
| 2 | 3 | 8.78 | 8.88 | 0.10 | 7.77 | 7.92 | 0.15 |
| 3 | 5 | 8.80 | 8.84 | 0.04 | 7.79 | 7.89 | 0.10 |

## Figure S27: An overlay of complex 9 (blue) and complex 11 (red)

## Figure S28: Packing diagram of complexes 9 as viewed down the crystallographic a-axis direction. Hydrogen atoms have been omitted for clarity.

## Figure S29: Packing diagram of complexes 11 as viewed down the crystallographic a-axis direction. Hydrogen atoms have been omitted for clarity.

## Figure S30: Pseudo-first-order logarithmic plot for the polymerization of rac-LA and L-LA in toluene at 110 °C by complex 5.

## Figure S31: Pseudo-first-order logarithmic plot for the bulk polymerization of CL at 110 °C by complexes 2, 4, 6, 7 and 8.

## Figure S32: Pseudo-first-order logarithmic plot for the bulk polymerization of CL at 110 °C by complexes 9, 10, 11, 12 and 13.

## Figure S33: The 1H-NMR spectrum of poly(ε-CL) initiated by complex 7 in different alcohol at room temperature in CDCl3 (400 MHz). Reaction conditions: [CL] 0 :[I]0:[ROH]0  = 200:1, bulk, T = 110 °C

## Figure S34: The 1H-NMR spectrum of poly(L-LA) initiated by complex 5 at room temperature in CDCl3 (400 MHz). Reaction conditions: [LA] 0 :[I]0 = 200:1, bulk, T = 110 °C.

## Figure S35: ESI-MS spectrum of poly(L-LA) initiated by complex 5. Reaction conditions: [LA]0 :[I]0 = 200:1, bulk, T = 110 °C.

## Figure S36: 13C NMR spectrum of the methine and carbonyl region of PLA obtained by complex 5 in CDCl3 at room temperature.

# MASS SPECTRA OF CARBOXYLATE COMPLEXES

## Figure S37: ESI-MS spectrum of complex 1

## Figure S38: ESI-MS spectrum of complex 10

# MASS SPECTRA OF POLYMERS

## Figure S39: ESI-MS spectrum of PCL obtained from complex 7

## Figure S40: ESI-MS spectrum of PCL obtained from complex 7 in benzyl alcohol

## Figure S41: ESI-MS spectrum of PCL obtained from complex 7 in isopropyl alcohol

## Figure S42: ESI-MS spectrum of poly(rac-lA) obtained from complex 5