Supplementary Material

Eco Friendly Synthesis of Fluorescent Carbon Dots for the Sensitive Detection of Ferric Ions and Cell Imaging

Jiankang Deng*a,b, Jing Hub, Juanjuan Zhaob, Nan Anb, Kuijing Lianga,b, Qinghua Wanga,b, Zhiqiang Zhangb, Rongrong Wua,b, Fuyuan Zhang*c

(a. Hebei Key Laboratory of Wetland Ecology and Conservation, Hengshui053000, China;

b. College of Life Science, Hengshui University, Hengshui053000, China;

c. College of Food Science and Technology, Hebei Agricultural University, Baoding071001, China.)

Corresponding author：*Jiankang Deng, phone number: +86 03186016590, Email: dengjk1989@163.com. Address: No.1088 Heping Road, Taocheng District, Hengshui, China.

*Fuyuan Zhang, phone number: +86 18322112260, Email: zhang.fuyuan@hotmail.com. Address: No.2596 Lekai South Street, Lianchi District, Baoding, China.

Fig. S1 Effects of ultraviolet irradiation time on the fluorescence intensity of CDs.

Fig. S2 Effects of storage time on the fluorescence spectra of the CDs (blue line: 0 month, pink line: 6 months).

Fig. S3 XRD spectra of the synthesized CDs.

Fig. S4 Digital photo images of the aqueous solution of the CDs (0.3 mg/mL) and in presence of Fe3+ (6 mM) under UV light (365nm).

Fig. S5. Stern-Volmer plots describes the dependency of the fluorescence intensities on the Fe3+ concentration over the range of 0.3-7 μM.

Fig. S6 The fluorescence lifetime decay curves of the CDs and CDs-Fe3+.

Fig. S7 Absorption spectrum of CDs, Fe3+, CDs-Fe3+ system and sum absorption of CDs with Fe3+.

Fig. S8 Fluorescence spectra of CDs solutions(30 μg/mL) in the absence and presence of other components: 1 mM Fe3+,1 mM Fe3++1 mM EDTA.

Fig. S9  Effects of incubation time on the fluorescence of CDs (30 μg/mL) in the presence of 1 mM Fe3+.

Fig. S10 The fluorescence spectra of CDs in PB buffer of different pH levels.

Fig. S11 Relative fluorescence intensity of CDs co-exist with different metal ion (the concentration of Fe3+ 1 mM, the concentration of each metal ions was 10 times larger than that of Fe3+, from left to right: blank, control, Ag+, Cu2+, Co2+, Cr3+, Cd2+, Hg2+, Mn2+, Fe2+, Sn2+, Pb2+, Zn2+, Ca2+, Mg2+, Na+, K+, Ni2+.

Fig. S12 Cytotoxicity test of CDs on Hela cells viability. The values represent percentage cell viability (mean%±SD, n=3).

Table S1. The comparison between our assay and previous’ CD based assays.

| Materials | Starting materials | Synthetic methods | Analyte | Limit of detection | Linear Range | References |
| --- | --- | --- | --- | --- | --- | --- |
| N-CDs | Chitosan and tartaric acid | hydrothermal | Fe3+ | 0 μM- 2000 μM | 1.15 μM | (Lv et al., 2020) |
| B-CDs | Glucose and boric acid | hydrothermal | Fe3+ | 0 μM- 16 μM | 242 nM | (Wang et al., 2016) |
| CDs | 1,2,4-triaminobenzene and formamide | solvothermal | Fe3+ | 1 μM- 60 μM | 0.28 μM | (Xu et al., 2019) |
| CDs | Fish scale | hydrothermal | Fe3+ | 1 μM- 78 μM | 0.54 μM | (Zhang et al., 2019) |
| CDs | Cranberry beans | hydrothermal | Fe3+ | 30 μM- 600 μM | 9.55 μM | (Zulfajri et al., 2019) |
| N-CDs | Citric acid and allylamine hydrochloride | hydrothermal | Fe3+ | 0.05 μM- 30 μM | 13.5 nM | (Zhou et al., 2019) |
| N-CDs | Prunus avium fruit extract | hydrothermal | Fe3+ | 0 μM- 100 μM | 0.96 μM | (Edison et al., 2016) |
| CDs | Goose feathers | microwave | Fe3+ | 0 μM- 10 μM | 0.196 μM | (Liu et al., 2015). |

References:

Edison, T. N. J. I., Atchudan, R., Shim, J., Kalimuthu, S., Ahn, B. & Lee, Y. R. 2016. Turn-off fluorescence sensor for the detection of ferric ion in water using green synthesized N-doped carbon dots and its bio-imaging. J. Photochem. Photobiol. 158:235-42. https://doi.org/10.1016/j.jphotobiol.2016.03.010.

Liu, R., Zhang, J., Gao, M., Li, Z., Chen, J., Wu, D. & Liu, P. 2015. A facile microwave-hydrothermal approach towards highly photoluminescent carbon dots from goose feathers. RSC Adv. 5:4428-33. https://doi.org/10.1039/c4ra12077a.

Lv, X., Man, H., Dong, L., Huang, J., & Wang, X. 2020. Preparation of highly crystalline nitrogen-doped carbon dots and their application in sequential fluorescent detection of Fe3+ and ascorbic acid. Food Chem. 326:126935. https://doi.org/10.1016/j.foodchem.2020.126935.

Wang, F., Hao, Q., Zhang, Y., Xu, Y., & Lei, W. 2016. Fluorescence quenchometric method for determination of ferric ion using boron-doped carbon dots. Microchim. Acta. 183(1):273-279. https://doi.org/10.1007/s00604-015-1650-1.

Zhang, Y., Gao, Z., Yang, X., Chang, J., Liu, Z., & Jiang, K. 2019. Fish-scale-derived carbon dots as efficient fluorescent nanoprobes for detection of ferric ions. RSC Adv. 9(2):940-949. https://doi.org/10.1039/c8ra09471c.

Zhou, X., Zhao, G., Tan, X., Qian, X., Zhang, T., Gui, J., Yang, L., & Xie, X. 2019. Nitrogen-doped carbon dots with high quantum yield for colorimetric and fluorometric detection of ferric ions and in a fluorescent ink. Microchim. Acta.  186(2):67. https://doi.org/10.1007/s00604-018-3176-9.

Zulfajri, M., Gedda, G., Chang, C., Chang, Y., & Huang, G. G. 2019. Cranberry beans derived carbon dots as a potential fluorescence sensor for selective detection of Fe3+ ions in aqueous solution. ACS Omega. 4(13):15382-15392. https://doi.org/10.1021/acsomega.9b01333.