# **Chemical deposition and exfoliation from liquid crystal template: Nickel/nickel (II) hydroxide nanoflakes electrocatalyst for a non-enzymatic glucose oxidation reaction**

Etab M. Almutairi,a Mohamed A. Ghanem,a,b\* Abdulrhman Al-Warthan,a Mohammed R. Shaik,a Syed F. Adil, Adibah M. Almutairia

*a Chemistry Department, King Saud University, 11451 Riyadh, Saudi Arabia.*

*b Electrochemical Sciences Research Chair (ESRC), College of Science, King Saud University, Riyadh 11451, Saudi Arabia.*

*\* Corresponding author Email: mghanem@ksu.edu.sa; Tel: +966 114670405; Fax: +96614675992,*

*ORCID 0000-0003-2866-9016*

**Supporting information**

Fig. S1 SEM image and X-ray diffraction of the *bare*-Ni(OH)2.



Fig. S2 EDX analysis of nickel/nickel hydroxides nanoflakes (Ni/Ni(OH)2−NFs)



keV

Fig. S2 The SEM elemental composition mapping annalysis of the Ni/Ni(OH)2-NFs catalyst

 



Table S1 EDX composition elemental analysis of the Ni/Ni(OH)2-NFs catalyst.

|  |  |  |
| --- | --- | --- |
| Element  | Wt. % | Atomic % |
| Ni k | 60.67 | 29.60 |
| O k | 39.33 | 70.40 |