Zeolite framework silicon allotropes with direct band gap

Yanxing Song*1, Changchun Chai1, Qingyang Fan*2, Wei Zhang1 and Yintang Yang1

1State Key Discipline Laboratory of Wide BandGap Semiconductor Technology, School of Microelectronics, Xidian University, Xi’an, People’s Republic of China.

2School of Information and Control Engineering, Xi’an University of Architecture and Technology, Xi’an, People’s Republic of China.

Table S1. The structural parameters of the new silicon allotropes

| Structure | Wyckoff position |
| --- | --- |
| ACO | Si1: 16f (0.16000, -0.16000, 0.16000) |
| AEI | Si1: 16h (0.11507, -0.04262, 0.33406) |
|  | Si2: 16h (0.61319, -0.26326, -0.43848) |
|  | Si3: 16h (0.27489, -0.40488, 0.44662) |
| AFX | Si1: 24l (0.99807, 0.22648, 0.08053) |
|  | Si2: 24l (0.33484, 0.44070, 0.16905) |
| ANA | Si1: 48g (-1.12500, 0.15784, -0.09216) |
| BOZ | Si1: 16h (0.25732, -0.36622, -0.14207) |
|  | Si2: 16h (0.10476, -0.04163, -0.14126) |
|  | Si3: 16h (0.24545, -0.07851, -0.01285) |
|  | Si4: 16h (0.10525, -0.36601, -0.99072) |
|  | Si5: 8f (0.00000, -0.68267, -0.14153) |
|  | Si6: 8g (0.39466, -0.32089, -0.25000) |
|  | Si7: 4c (0.00000, -0.75187, -0.25000) |
|  | Si8: 8e (0.22315, 0.00000, 0.00000) |
| BPH | Si1: 12l (0.86441, 0.35154, 0.73930) |
|  | Si2: 12l (0.13542, 0.69175, 0.61885) |
|  | Si3: 4h (0.33333, 0.66667, 0.88252) |
| EDI | Si1: 4j (0.27997, 0.00000, 0.12472) |
|  | Si2: 1d (0.00000, 0.00000, 0.50000) |
| ETR | Si1: 12d (0.74463, 0.10733, 0.01595) |
|  | Si2: 12d (0.66790, 0.18737, 0.16048) |
|  | Si3: 12d (0.63517, 0.97157, 0.21897) |
|  | Si4: 12d (0.61013, 0.07651, 0.43260) |
| GME | Si1: 24l (0.43856, 0.10667, 0.09011) |
| LEV | Si1: 36i (0.99831, 0.23982, 0.06760) |
|  | Si2: 18g (0.23961, -0.00000, 0.50000) |
| LIT | Si1: 8d (-0.49425, 0.07153, 0.16069) |
|  | Si2: 8d (-0.32716, 0.57306, 0.67342) |
|  | Si3: 8d (-0.33447, 0.57312, 0.31725) |
| MEL | Si1: 16j (0.18924, 0.12267, -0.14384) |
|  | Si2: 16j (0.22128, 0.07697, -0.35650) |
|  | Si3: 16j (0.18849, 0.27861, -0.14100) |
|  | Si4: 16j (0.57727, 0.80883, -0.48988) |
|  | Si5: 16j (0.37667, 0.07752, -0.35359) |
|  | Si6: 8g (0.07770, 0.07770, 0.00000) |
|  | Si7: 8g (0.69177, 0.69176, -0.00000) |
| RWR | Si1: 16h (-0.00000, 0.30464, 0.17870) |
|  | Si2: 16g (0.70236, 0.70236, 1.00000) |
| SAT | Si1: 36i (-0.75620, -0.00171, -0.29414) |
|  | Si2: 36i (-0.57730, 0.33554, -0.21724) |
| SGT | Si1: 16h (-0.00000, 0.71354, 0.75450) |
|  | Si2: 16h (-0.00000, -0.14848, 0.67737) |
|  | Si3: 16h (-0.00000, -0.15269, 0.83578) |
|  | Si4: 16f (0.27722, -0.25000, 0.12500) |

Figure S1. Phonon spectra for the zeolite framework silicon allotropes.

Figure S2. Three-dimensional contour plots of electron effective masses for zeolite framework silicon allotropes with higher minimum electronic effective mass than diamond silicon.

Figure S3. Three-dimensional contour plots of hole effective masses for zeolite framework silicon allotropes with higher minimum hole effective mass than diamond silicon.