**Supporting information**

**Hyper-branched Multifunctional Carbon Nanotubes Carrier for Targeted Liver**

**Cancer Therapy**

**Yadong Zhoua, Kandasamy Vinothinib\*, Fafu Doua, Yan Jinga, Anil A Chuturgoonc, Thilona Arumugamc, Mariappan Rajanb**

aDepartment of Gastrointestinal surgery, 3201 Hospital, Hanzhong, 723000, China

bBiomaterials in Medicinal Chemistry Laboratory, Department of Natural Products Chemistry, School of Chemistry, Madurai Kamaraj University, Madurai 625021, Tamil Nadu, India.

cDiscipline of Medical Biochemistry and Chemical Pathology, Faculty of Health Sciences, University of KwaZulu-Natal, Durban,4041, South Africa.

\*Corresponding author: **Kandasamy Vinothini,** Biomaterials in Medicinal Chemistry Laboratory, Department of Natural Products Chemistry, School of Chemistry, Madurai Kamaraj University, Madurai 625021, Tamil Nadu, India. Email: vinothini81094@gmail.com

**Supporting information**

**1. Characterizations**

**1.1. Fourier Transformed Infrared Spectroscopy (FT-IR)**

The FT-IR spectroscopy used to analyze the structural elucidation of MWCNT-COOH, MWCNT-PEG, MWCNT-PEG-AA, MWCNT-PEG-AA-HBPLL-FA, and DOX/MWCNT-PEG-AA-HBPLL-FA were performed using hydraulic pressure compressed KBr pellet method in FT-IR spectrophotometer, Spectrum GX-1, Perkin Elmer, USA. The scanning ranges from 400-4000 cm-1.

**1.2. X-ray diffraction (XRD)**

XRD analysis of MWCNT-COOH, MWCNT-PEG, MWCNT-PEG-AA, MWCNT-PEG-AA-HBPLL-FA, and DOX/MWCNT-PEG-AA-HBPLL-FA carrier crystalline phase identifications was analyzed by Philips 1710 X-ray diffractometer (Philips Electronic Instruments, Inc., Mahwah, NJ).

**1.3. Scanning Electron Microscopy (SEM)**

For the surface morphology of MWCNT-COOH, MWCNT-PEG, MWCNT-PEG-AA-HBPLL-FA, and DOX/MWCNT-PEG-AA-HBPLL-FA carriers’ solution were ultra-sonicated for 10 min. The solution was drop cast onto a sample holder, air-dried, and subjected to a Carl Zeiss Ultra Plus Field emission scanning electron microscope (FE-SEM).

**1.4. Transmission electron microscope (HR-TEM)**

The MWCNT-COOH, MWCNT-PEG, MWCNT-PEG-AA-HBPLL-FA, and DOX/MWCNT-PEG-AA-HBPLL-FA carriers (1 µL) solution was placed for particle size and shape on formvar coated grids, air-dried, and viewed at 100 kV to conduct transmission electron microscopy (JEOL 1010 TEM using a Mega view III camera and TEM software) studies. The JEM-2100 is a multipurpose, 200 kV analytical electron microscope.

**1.5. Thermogravimetric Analysis (TGA)**

Thermal gravimetric analysis (TGA) was measured on Shimadzu-TA 60 instrument with a heating rate of 25 °C min-1 using crucibles of aluminum under N2 atmosphere.

**1.6. Particles size measurements analysis**

The hydrodynamic particle size and surface charge of the MWCNT-PEG-AA-HBPLL- FA and DOX/MWCNT-PEG-AA-HBPLL-FA were studied at 25℃ in a Zetasizer (Malvern instruments DTS Ver.4.10) equipped with He-Ne laser (633 nm) as a light source at room temperature.