Searching for high performance asymmetrically substituted teterazine energetic materials based on 3-hydrazino-6-(1H-1,2,3,4-tetrazol-5-ylimino)-s-tetrazine

Xiang Chena, Cong Zhanga, Wenli Caob, Zhaoqi Guoa*, Jianguo Zhangb, Haixia Maa

aSchool of Chemical Engineering / Xi'an Key Laboratory of Special Energy Materials, Northwest University, Xi'an 710069, Shaanxi, P. R. China.

bState Key Laboratory of Explosion Science and Technology, Beijing Institute of Technology, Beijing 100081, P. R. China

Table of Contents

1. Materials and methods.

2. Crystallographic data and crystal structures.

3. DSC curves.

4. Computational details.

5. NMR spectra.

6. References.

1. Materials and methods

All of the reagents were purchased from commercial sources and used without further purification. IR were performed on Shimadzu IRAﬃnity-1S FTIR spectrophotometer (KBr pellets). Elemental analyses were recorded on a VarioEL III elemental analyzer (Elementar Co., Germany). 1H (500 MHz) and 13C (125 MHz) NMR spectra were performed on BRUKER AVANCE III HD. Single-crystal X-ray diﬀraction were performed on a Bruker D8 Venture diﬀractometer outfitted with a PHOTON-100 CMOS detector with highly oriented graphite crystal monochromated Mo-K radiation ( =0.071073 nm). All the non-hydrogen atoms were refined anisotropically. The hydrogen atoms were refined using a riding model.

2. Crystallographic data and crystal structures

Table S1 Crystallographic data for 6·CH3OH, 7·2H2O, 9·4/3DMF, 12·5/2H2O

| Compound | 6·CH3OH | 7·2H2O | 9·4/3DMF | 12·5/2H2O |
| --- | --- | --- | --- | --- |
| Empirical formula | C4H9N11O | C3H10N12O5 | C24H40N40O4 | C10H28N30O5 |
| Temperature/K | 296(2) | 173 | 296(2) | 296(2) |
| Crystal system | monoclinic | monoclinic | triclinic | triclinic |
| Space group | P21/c | P21/n | P-1 | P-1 |
| α/° | 90 | 90 | 92.329(5) | 74.715(9) |
| β/° | 84.897(12) | 90.861(10) | 94.879(5) | 83.332(8) |
| γ/° | 90 | 90 | 96.746(5) | 86.715(8) |
| a/Å | 4.793(3) | 4.7674(15) | 7.4873(19) | 7.752(4) |
| b/Å | 11.213(7) | 11.521(4) | 11.912(3) | 12.315(6) |
| c/Å | 18.222(11) | 20.980(6) | 24.315(6) | 14.879(7) |
| Volume/Å3 | 975.5(10) | 1152.3(6) | 2143.1(9) | 1360.5(11) |
| Z | 4 | 4 | 2 | 2 |
| μ/mm-1 | 0.123 | 0.152 | 0.113 | 0.13 |
| F(000) | 472 | 608 | 992 | 676 |
| Density/g·cm-3 | 1.547 | 1.696 | 1.477 | 1.583 |
| 2 range/° | 4.27 to 50.054 | 3.884 to 50.052 | 3.366 to 50.052 | 3.852 to 50.194 |
| Data/restraints/parameters | 1732/18/169 | 2030/1/196 | 7448/0/614 | 4768/0/421 |
| Reflections collected | 4800 | 7957 | 10737 | 6713 |
| Independent reflections | 1732 | 2030 | 7448 | 4768 |
| GOOF | 0.897 | 1.024 | 0.988 | 0.918 |
| Final R indexes [I>=2σ(I)] | R1 = 0.0582, wR2 = 0.0983 | R1 = 0.0565, wR2 = 0.1212 | R1 = 0.0664, wR2 = 0.1551 | R1 = 0.0561, wR2 = 0.1076 |
| Final R indexes [all data] | R1 = 0.1934, wR2 = 0.1425 | R1 = 0.1045, wR2 = 0.1436 | R1 = 0.1252, wR2 = 0.1891 | R1 = 0.1168, wR2 = 0.1323 |
| Recrystallization solvent | methanol | water | DMF | water |
| CCDC | 1827108 | 2128375 | 1556002 | 2128377 |

Table S2 Crystallographic data for 13·3/2H2O, Na2·14H2O and 18·2DMSO·CH3OH

| Compound | 13·3/2H2O | Na2·14·4H2O | 18·2DMSO·2CH3OH |
| --- | --- | --- | --- |
| Empirical formula | C10H28N34O3 | C4H9N13O6Na2 | C14H24N24O4S2 |
| Temperature/K | 296(2) | 273(2) | 296(2) |
| Crystal system | triclinic | triclinic | triclinic |
| Space group | P-1 | P-1 | P-1 |
| α/° | 98.876(5) | 103.137(9) | 111.135(12) |
| β/° | 96.670(5) | 91.652(10) | 100.035(14) |
| γ/° | 93.770(5) | 111.827(9) | 96.405(14) |
| a/Å | 10.461(3) | 8.178(6) | 5.860(3) |
| b/Å | 10.594(3) | 9.423(7) | 10.563(4) |
| c/Å | 12.613(3) | 10.212(7) | 12.709(4) |
| Volume /Å3 | 1366.7(6) | 705.8(9) | 709.4(5) |
| Z | 2 | 2 | 1 |
| μ/mm-1 | 0.131 | 0.208 | 0.259 |
| F(000) | 700 | 388 | 340 |
| 2 range/° | 3.296 to 50.054 | 5.408 to 54.968 | 4.21 to 50.682 |
| Density/g·cm-3 | 1.635 | 1.794 | 1.537 |
| Data/restraints/parameters | 4805/0/437 | 3133/0/226 | 2535/0/204 |
| Reflections collected | 6909 | 6116 | 2535 |
| Independent reflections | 4805 | 3133 | 2535 |
| GOOF | 0.905 | 1.054 | 1.077 |
| Final R indexes [I>=2σ(I)] | R1 = 0.0714, wR2 = 0.1432 | R1 = 0.0483, wR2 = 0.1377 | R1 = 0.1043, wR2 = 0.3042 |
| Final R indexes [all data] | R1 = 0.2383, wR2 = 0.2152 | R1 = 0.0664, wR2 = 0.1531 | R1 = 0.1430, wR2 = 0.3272 |
| Recrystallization solvent | water | water | DMSO and methanol |
| CCDC | 2128381 | 2128382 | 2128383 |

Fig. S1 The asymmetric unit of 8·1/2HClO4·7/2H2O.

Fig. S2 The packing diagram of 8·1/2HClO4·7/2H2O.

3. DSC curves

Fig. S3 The DSC curve of compound 6.

Fig. S4 The DSC curve of compound 7.

Fig. S5 The DSC curve of compound 8.

Fig. S6 The DSC curve of compound 9.

Fig. S7 The DSC curve of compound 10.

Fig. S8 The DSC curve of compound 12.

Fig. S9 The DSC curve of compound 13.

Fig. S10 The DSC curve of compound 14.

Fig. S11 The DSC curve of compound 15.

Fig. S12 The DSC curve of compound 16.

Fig. S13 The DSC curve of compound 17.

Fig. S14 The DSC curve of compound 18.

Table S3 The Te and Tp at different heating rates.

| Compound | (oC·min-1) | Te (oC) | Tp (oC) |
| --- | --- | --- | --- |
| 6 | 5 | 179.02 | 183.98 |
|  | 10 | 183.68 | 187.68 |
|  | 15 | 186.16 | 190.34 |
|  | 20 | 189.18 | 191.89 |
| 12 | 5 | 279.07 | 280.11 |
|  | 10 | 284.24 | 285.41 |
|  | 15 | 288.65 | 289.36 |
|  | 20 | 291.87 | 292.95 |
| 13 | 5 | 221.14 | 222.35 |
|  | 10 | 225.81 | 229.84 |
|  | 15 | 232.38 | 234.10 |
|  | 20 | 234.35 | 236.46 |
| 15 | 5 | 166.75 | 182.34 |
|  | 10 | 173.60 | 188.71 |
|  | 15 | 179.02 | 191.47 |
|  | 20 | 182.23 | 192.89 |
| 16 | 5 | 207.12 | 236.71 |
|  | 10 | 212.28 | 241.97 |
|  | 15 | 218.60 | 247.73 |
|  | 20 | 220.60 | 249.24 |
| 17 | 5 | 178.90 | 195.54 |
|  | 10 | 184.77 | 200.03 |
|  | 15 | 186.99 | 205.19 |
|  | 20 | 191.21 | 207.15 |

4. Computational details

The theoretical calculations were carried out by using Gaussian 16 program (Revision C.01). Geometric optimization and frequency analyses of the structures were performed at the level of B3LYP/6-31+G**. Besides, single-point energies were calculated at MP2/6-311++G** level.1 Atomization energies were calculated by using G2 ab initio method based on atomization reaction and NIST WebBook.2,3 All of the optimized structures were determined to be true local energy minima without imaginary frequencies. The heat of formation (HOF) of all the compounds were obtained using isodesmic reactions (Scheme S1). The calculation results of the gas-phase species were list in Table S4.

Scheme S1 The isodesmic reactions of obtained compounds.

Table S4 Calculated HOF of the gas-phase species

| Compound | ∆Hf° (kJ·mol-1) | Compound | ∆Hf° (kJ·mol-1) |
| --- | --- | --- | --- |
| 1 | 1603.85 | 2 | 478.70 |
| 3 | 318.08 | 4 | 998.59 |
| 5 | 682.59 | 6 | 804.94 |
| 7 | 1011.01 | 8 | 980.59 |
| 9 | 2273.61 | CH4 | -74.87 |
| NH3 | -45.90 | CH3NH2 | -22.50 |
| NH2NO2 | -6.11 | NH2NH2+ | 770.00 |
| NH=NH | 200.40 | NHNO2- | -6.74 |

For neutral compounds, the solid-phase HOF can be calculated by subtracting the heat of sublimation (∆Hsub) from the gas-phase HOF. Based on Trouton’s rule, the solid-phase HOF were calculated by equation 1, where T denotes either the melting point or the decomposition temperature when no melting occurs before the decomposition.4

∆Hfs=∆Hfg-∆Hsub=∆Hfg-188J∙mol∙K-1 × T (1)

For energetic salts, the solid-phase HOF can be obtained on the basis of Born-Haber energy cycle, which is shown in Scheme S2. The calculation equation is simplified by using equation 2.

Scheme S2 Born-Haber energy cycle for the formation of energetic salts.

∆Hfosalt,298 K=∆Hfocation,298 K+∆Hfoanion,298 K-∆HL  (2)

In equation 2, ∆HL represents the lattice energy of the ionic salts which can be obtained by using equation 3 that suggested by Jenkins, et al.5

∆HL=Upot+[pnM2-2+q(nX2-2)]RT  (3)

In equation 3, the values of nM and nX depend on the nature of the ions ( Mq+and XP-), which equal to 3 for monatomic ions, 5 for linear polyatomic ions, and 6 for nonlinear polyatomic ions. Upot represents the lattice potential energy that can be calculated from equation 4:

UpotkJ∙mol-1=γ(ρm/Mm)1/3+δ  (4)

where ρm equals to the density of the energetic salt and Mm denotes the chemical formula mass of the compound. The values of coefficients γ (kJ∙mol-1∙cm) and δ (kJ∙mol-1) can be assigned according to the literature.5

Based on the measured densities and the calculated heats of formation, the detonation velocities and detonation pressures of all the compounds were evaluated using EXPLO5 v6.04, and the results are summarized in Table 3.

5. NMR spectra

Fig. S5 1H NMR spectrum of 7.

Fig. S6 13C NMR spectrum of 7.

Fig. S7 1H NMR spectrum of 8.

Fig. S8 13C NMR spectrum of 8.

Fig. S9 1H NMR spectrum of 9.

Fig. S10 13C NMR spectrum of 9.

Fig. S11 1H NMR spectrum of 10.

Fig. S12 13C NMR spectrum of 10.

Fig. S13 1H NMR spectrum of 12.

Fig. S14 13C NMR spectrum of 12.

Fig. S15 1H NMR spectrum of 13.

Fig. S16 13C NMR spectrum of 13.

Fig. S17 1H NMR spectrum of 14.

Fig. S18 13C NMR spectrum of 14.

Fig. S19 1H NMR spectrum of 15.

Fig. S20 13C NMR spectrum of 15.

Fig. S21 1H NMR spectrum of 16.

Fig. S22 13C NMR spectrum of 16.

Fig. S23 1H NMR spectrum of 17.

Fig. S24 13C NMR spectrum of 17.

Fig. S25 1H NMR spectrum of 18.

Fig. S26 13C NMR spectrum of 18.

6. References.

- R. G. Parr and W. Yang, Density Functional Theory of Atoms and Molecules, Oxford University Press: Oxford, U.K., 1989.

- L. A. Curtiss, K. Raghavachari, G. W. Trucks and J. A. Pople, J. Chem. Phys., 1991, 94, 7221- 7230.

- NIST Chemistry WebBook, https://webbook.nist.gov/chemistry/.

- M. S. Westwell, M. S. Searle, D. J. Wales and D. H. Wiliams, J. Am. Chem. Soc., 1995, 117, 5013.

- H. D. B. Jenkins, D. Tudela and L. Glasser, Inorg. Chem., 2002, 41, 2364-2367.

Corresponding author. Email address: guozhaoqi@outlook.com; mahx@nwu.edu.cn.