Supporting information

Ultrafast 99% Polyethylene terephthalate depolymerization into value added monomers using sequential glycolysis-hydrolysis under microwave irradiation

Muhammad Azeem1, Margaret Brennan Fournet1 and Olivia A. Attallah*1,2

1 Materials Research Institute, Technological University of the Shannon Midlands Midwest, Athlone, N37 HD68, Ireland.

2 Pharmaceutical Chemistry Department, Faculty of Pharmacy, Heliopolis University, Cairo - Belbeis Desert Road, El Salam, Cairo 11777, Egypt.

*Correspondence: oadly@ait.ie

Note:

Number of Pages: 9

Number of Tables: 2

Number of Figure: 4

Table of Content

| S1 Instrumental Analysis | S3 |
| --- | --- |
| Table S1: Statistical analysis of measured responses for MW assisted glycolysis of PET using DES 1 | S4 |
| Table S2: Statistical analysis of measured responses for MW assisted glycolysis of PET using DES 2 | S5 |
| Figure S1: 3-D plots of the effect of the interaction of [a] DES volume (X1) and EG volume (X2), [b] DES volume (X1) and MW time (X3) and [c] EG volume (X2) and MW time (X3) on carbonyl index for MW assisted glycolysis of PET using DES 1 and 2 | S6 |
| Figure S2: 3-D plots of the effect of the interaction of [a] DES volume (X1) and EG volume (X2), [b] DES volume (X1) and MW time (X3) and [c] EG volume (X2) and MW time (X3) on crystallinity index for MW assisted glycolysis of PET using DES 1 and 2 | S7 |
| Figure S3: 3-D plots of the effect of the interaction of [a] DES volume (X1) and EG volume (X2), [b] DES volume (X1) and MW time (X3) and [c] EG volume (X2) and MW time (X3) on weight loss of PET (%) for MW assisted glycolysis of PET using DES 1 and 2. | S8 |
| Figure S4: HPLC chromatograms of cooled filtrate of PET samples treated via: [a] MW assisted hydrolysis, [b] MW assisted hydrolysis post MW assisted DES 1/glycolysis and [c] MW assisted hydrolysis post MW assisted DES 2/glycolysis | S9 |

S1 Instrumental Analysis

The PET samples before and after MW assisted DES pre-treatment were analysed by FTIR spectroscopy (Perkin Elmer, UK) at a spectral region of 4000-600 cm-1. Carbonyl Index was determined based on the obtained results using baseline method. Ratios of ester carbonyl peak intensity at 1713 cm-1 to that of the normal C-H bonding mode at 1408 cm-1 in PET were calculated as follows (Chelliah et al., 2017),

Carbonyl index=Absorption at 1713 cm-1Absorption at 1408 cm-1                     (1)

The thermal behaviour of the samples was evaluated by a DSC Perkin Elmer 4000 (Perkin Elmer Washington, Ma, USA) with Pyris Software (Version 13.3.1) under an inert nitrogen stream. About 10 mg of specimen was sealed in an aluminium pan and the DSC scans were recorded while heating from 30 – 275 ℃ at a heating rate of 10 ℃/min, and then cooled to 30℃. The crystallinity index was calculated according to the following Equation (Li et al., 2017),

Crystallinity index = (∆Hm/W∆Hm0) × 100         (2)

where ∆Hm (J/g) is the heat of fusion of the PET sample. ∆Hm0 is the heat of fusion for completely crystalline PET (140 J/g) (Fosse et al., 2019) and W(g) is the weight fraction of residual PET in the samples.

The percentage weight loss of PET was calculated using following equation:

PET Weight loss (%)=(W1-W2)/W1×100      (3)

where W1 was PET initial weight and W2 was the weight of PET residual after MW assisted DESs/glycolysis technique.

Soluble monomers obtained from PET depolymerization were identified and quantified by HPLC (Alliance Waters, UK) with C-18 column (NUCLEODUR, Germany 4.6*250, 5 um) at 1.2 ml/min flow rate and 10 µl injection volume at 30 ⁰C. Standard TPA, MHET and BHET in 100% methanol were used as reference in the HPLC analysis. A mobile phase of acetonitrile and 10mM sulphuric acid in ultrapure water was employed with a UV detector at 254 nm. Total run time was 18 min. Retention times were TPA 7.9 min, MHET 9.6 min, BHET 11.7 min. Quantification of TPA, MHET and BHET was performed by constructing calibration curves with standard concentrations in the range of 0.01-1 mM

Table S1: Statistical analysis of measured responses for MW assisted glycolysis of PET using DES 1

| Fitting model | Factors | Coefficient | P-value | ANOVA |
| --- | --- | --- | --- | --- |
| PET Carbonyl index (Y1) | Intercept | +3.78 |  | F = 184.91, R2 = 0.9916, Model P-value ˂0.0001, P-value of lack of fit = 0.352 |
|  | X1 | -0.092 | 0.0010 |  |
|  | X2 | +0.17 | < 0.0001 |  |
|  | X3 | -0.37 | < 0.0001 |  |
|  | X1X2 | -0.20 | 0.0001 |  |
|  | X1X3 | +0.15 | 0.0005 |  |
|  | X2X3 | -0.38 | < 0.0001 |  |
|  | X12 | -0.20 | 0.0001 |  |
|  | X22 | -0.096 | 0.0045 |  |
|  | X32 | -0.036 | 0.1253 |  |
| PET Crystallinity index (Y2) | Intercept | +28.86 |  | F = 442.16, R2 = 0.9965, Model P-value = ˂ 0.0001, P-value of lack of fit = 0.497 |
|  | X1 | +0.68 | 0.0005 |  |
|  | X2 | +0.68 | 0.0005 |  |
|  | X3 | +4.78 | < 0.0001 |  |
|  | X1X2 | +2.29 | < 0.0001 |  |
|  | X1X3 | +0.40 | 0.0212 |  |
|  | X2X3 | +0.22 | 0.1277 |  |
|  | X12 | +0.73 | 0.0021 |  |
|  | X22 | +0.52 | 0.0083 |  |
|  | X32 | +1.86 | < 0.0001 |  |
| Weight loss of PET (Y3) | Intercept | +6.57 |  | F = 214.20, R2 = 0.9928, Model P-value = ˂ 0.0001, P-value of lack of fit = 0.889 |
|  | X1 | +3.77 | < 0.0001 |  |
|  | X2 | +2.56 | 0.0002 |  |
|  | X3 | +3.85 | < 0.0001 |  |
|  | X1X2 | +5.45 | < 0.0001 |  |
|  | X1X3 | +5.44 | < 0.0001 |  |
|  | X2X3 | +1.94 | 0.0031 |  |
|  | X12 | +2.80 | 0.0007 |  |
|  | X22 | +6.43 | < 0.0001 |  |
|  | X32 | +9.81 | < 0.0001 |  |

X1: volume of DES, X2: volume of EG, X3: MW irradiation time

Table S2: Statistical analysis of measured responses for MW assisted glycolysis of PET using DES 2

| Fitting model | Factors | Coefficient | P-value | ANOVA |
| --- | --- | --- | --- | --- |
| PET Carbonyl index (Y1) | Intercept | +3.70 |  | F = 953.1, R2 = 0.9984, Model P-value ˂0.0001, P-value of lack of fit = 0.107 |
|  | X1 | -0.13 | < 0.0001 |  |
|  | X2 | +0.12 | < 0.0001 |  |
|  | X3 | -0.23 | < 0.0001 |  |
|  | X1X2 | -0.087 | < 0.0001 |  |
|  | X1X3 | +0.25 | < 0.0001 |  |
|  | X2X3 | +0.052 | 0.0006 |  |
|  | X12 | +0.38 | < 0.0001 |  |
|  | X22 | -0.087 | < 0.0001 |  |
|  | X32 | -0.052 | 0.0007 |  |
| PET Crystallinity index (Y2) | Intercept | +34.34 |  | F = 311.78, R2 = 0.9950, Model P-value = ˂ 0.0001, P-value of lack of fit = 0.518 |
|  | X1 | +0.52 | 0.0173 |  |
|  | X2 | +2.39 | < 0.0001 |  |
|  | X3 | +4.95 | < 0.0001 |  |
|  | X1X2 | -0.52 | 0.0554 |  |
|  | X1X3 | +1.36 | 0.0013 |  |
|  | X2X3 | +3.31 | < 0.0001 |  |
|  | X12 | +3.56 | < 0.0001 |  |
|  | X22 | +1.76 | 0.0005 |  |
|  | X32 | -5.84 | < 0.0001 |  |
| Weight loss of PET (Y3) | Intercept | +6.90 |  | F = 170.28, R2 = 0.9901, Model P-value = ˂ 0.0001, P-value of lack of fit = 0.134 |
|  | X1 | +0.59 | 0.1289 |  |
|  | X2 | -0.050 | 0.8839 |  |
|  | X3 | +5.25 | < 0.0001 |  |
|  | X1X2 | -3.79 | 0.1117 |  |
|  | X1X3 | +5.05 | 0.0001 |  |
|  | X2X3 | +0.89 | 0.0004 |  |
|  | X12 | -1.32 | 0.0399 |  |
|  | X22 | -0.68 | 0.2154 |  |
|  | X32 | +15.43 | < 0.0001 |  |

X1: volume of DES, X2: volume of EG, X3: MW irradiation time

| Carbonyl index (Y1) |  |  |  |
| --- | --- | --- | --- |
| DES 1 |  |  |  |
| DES 2 |  |  |  |

Figure S1: 3-D plots of the effect of the interaction of [a] DES volume (X1) and EG volume (X2), [b] DES volume (X1) and MW time (X3) and [c] EG volume (X2) and MW time (X3) on carbonyl index for MW assisted glycolysis of PET using DES 1 and 2

| Crystallinity index (Y2) |  |  |  |
| --- | --- | --- | --- |
| DES 1 |  |  |  |
| DES 2 |  |  |  |

Figure S2: 3-D plots of the effect of the interaction of [a] DES volume (X1) and EG volume (X2), [b] DES volume (X1) and MW time (X3) and [c] EG volume (X2) and MW time (X3) on crystallinity index for MW assisted glycolysis of PET using DES 1 and 2

| Weight loss (%) (Y3) |  |  |  |
| --- | --- | --- | --- |
| DES 1 |  |  |  |
| DES 2 |  |  |  |

Figure S3: 3-D plots of the effect of the interaction of [a] DES volume (X1) and EG volume (X2), [b] DES volume (X1) and MW time (X3) and [c] EG volume (X2) and MW time (X3) on weight loss of PET (%) for MW assisted glycolysis of PET using DES 1 and 2.

[a]a

[b]a

[c]

Figure S4: HPLC chromatograms of cooled filterate of PET samples treated via: [a] MW assisted hydrolysis, [b] MW assisted hydrolysis post MW assisted DES 1/glycolysis and [c] MW assisted hydrolysis post MW assisted DES 2/glycolysis

References

Chelliah, A., Subramaniam, M., Gupta, R., Gupta, A., 2017. Evaluation on the Thermo-Oxidative Degradation of PET using Prodegradant Additives. Indian J. Sci. Technol. 10, 1–5. https://doi.org/10.17485/ijst/2017/v10i6/111212

Fosse, C., Bourdet, A., Ernault, E., Esposito, A., Delpouve, N., Delbreilh, L., Thiyagarajan, S., Knoop, R.J.I., Dargent, E., 2019. Determination of the equilibrium enthalpy of melting of two-phase semi-crystalline polymers by fast scanning calorimetry. Thermochim. Acta 677, 67–78. https://doi.org/10.1016/j.tca.2019.03.035

Li, W., Zhang, C., Chi, H., Li, L., Lan, T., Han, P., Chen, H., Qin, Y., 2017. Development of antimicrobial packaging film made from poly(lactic acid) incorporating titanium dioxide and silver nanoparticles. Molecules 22. https://doi.org/10.3390/molecules22071170