**Supporting Information**

**Precise Regulation of Ultra-thin Pt Decorated Au/g-C3N4 Photocatalysts by**

**ALD for Efficient Degradation of RhB under Simulated Sunlight**

Hongfen Zhang1\*, Baiyan Zhang1, Fangmiao Liang, Yang Fang, Hong Wang, Anjia Chen,

*School of Pharmacy,* *Shanxi Medical University, Jinzhong 030619, Shanxi, China*

E-mail addresses: [zhanghf\_2007@126.com](mailto:zhanghf_2007@126.com)

****

**Fig.S1** Degradation efficiency of RhB with different catalyst dosage under sunlight irradiation



**Fig.S2.** The adsorption behaviors of C3N4-Au/10Pt for RhB

The adsorption behaviors of C3N4-Au/10Pt for RhB was investigated. The experiment results showed that the adsorption and desorption of RhB by the C3N4-Au/10Pt reached equilibrium after 20 min.



**Fig.S3.** Photodegradation of RhB in the presence of C3N4-Au/10Pt at different pH values (The pH of acidic, neutral and alkaline RhB reaction solutions is 1.5, 7.0 and 11.0, respectively).

In order to deeply investigate the excellent photocatalytic activity of C3N4-Au/10Pt at different pH values, the photocatalytic performance of C3N4-Au/10Pt under different pH values were studied. As shown in Figure S3, for C3N4-Au/10Pt sample, the photodegradation efficiencies were ~100% (pH = 1.5, within 20 minutes), ~94.9% (pH = 11.0, within 30 minutes) and ~86.3% (pH = 7.0, within 30 minutes), respectively. The differences of degradation efficiencies at the different pH values may be ascribe to the effect of H+ or OH− on the production of the reactive species (·OH, ·HO2, ·O2− and h+), because these species involved in photocatalysis and were of great importance for photodegrade reactions (Fei et al., 2016, Qingyong et al., 2017).

**Table S1.** Comparison of photocatalytic activities for the degradation of RhB

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| catalyst | Visible  lamp | Catalyst dosage (g) | RhB (mg⋅L-1) | Solution volume (L) | Degradation rate | Degradation time | Ref. |
| TCN(Ta2O5/g-C3N4) | 300 W | 0.10 | 10 | 0.1 | ~100% | 20 min | (Xin et al., 2016) |
| 0.5%CQDs/g-C3N4 | 250 W | 0.05 | 10 | 0.1 | 95.2% | 210 min | (Yuanzhi et al., 2016) |
| g-C3N4/Bi4O7 | 500 W  halogen lamp | 0.08 | 4.8 | 0.08 | ~100% | 70 min | (Meng et al., 2017) |
| Bi2WO6/g-C3N4 | 300 W | 0.05 | 20 | 0.05 | 92.51% | 50 min | (Mingjuan et al., 2019) |
| 2D/2D BiVO4/g-C3N4 | 300 W | 0.01 | 20 | 0.02 | ~100% | 60 min | (Zhichao et al., 2018) |
| Au@C/g-C3N4 | 300 W |  | 10 |  | 94.3% | 120 min | (Xixian et al., 2020) |
| Fe2O3/g-C3N4 | 65 W CFL lamp | 0.003 | 5 | 0.01 | 97.4% | 140 min | (Jasminder and Soumen 2020) |
| RTCN(N-HtiNbO5/g-C3N4) | 300 W | 0.1 | 1 | 0.2 | ~95% | 60 min | (Chao et al., 2020) |
| UCNA(ultrathin-g-C3N4/AgI) | 500 W | 0.02 | 20 | 0.03 | ~100% | 60 min | (Hao et al., 2021) |
| 2% ZnO/TiO2 | 200 W | 0.05 | 10 | 0.1 | 94% | 45 min | (Yingming et al., 2021) |
| ZnO/Ag | 300 W | 0.03 |  | 0.1 | 100% | 30 min | (Liu et al., 2021) |
| C3N4-Au/10Pt | **300 W** | **0.0015** | **10** | **0.1** | **~100%** | **65 min** | **This work** |

**References**

Chao, L., H. Zitong, F. Yue, et al., 2020. Ultrathin Z-scheme 2D/2D N-doped HTiNbO5 nanosheets/g-C3N4 porous composites for efficient photocatalytic degradation and H2 generation under visible light. Journal of Colloid and Interface Science. 583, 58-70.

Fei, C., Y. Qi, L. Xiaoming, et al., 2016. Hierarchical assembly of graphene-bridged Ag3PO4/Ag/BiVO4 (040) Z-scheme photocatalyst: An efficient, sustainable and heterogeneous catalyst with enhanced visible-light photoactivity towards tetracycline degradation under visible light irradiation. Applied Catalysis B: Environmental. 200, 330-342.

Hao, H., L. Yu-Xuan, W. Hui-Long, et al., 2021. In situ fabrication of ultrathin-g-C3N4/AgI heterojunctions with improved catalytic performance for photodegrading rhodamine B solution. Applied Surface Science. 538, 148132.

Jasminder, S. and B. Soumen, 2020. Synthesis of mesoporous magnetic Fe2O3/g-C3N4 monoliths for Rhodamine B removal. Microporous and Mesoporous Materials. 303, 110299.

Liu, Y., Q. Zhang, H. Yuan, et al., 2021. Comparative study of photocatalysis and gas sensing of ZnO/Ag nanocomposites synthesized by one- and two-step polymer-network gel processes. Journal of Alloys and Compounds. 868, 566-576.

Meng, S., W. Yu, S. Yu, et al., 2017. Fabrication of a novel Z-scheme g-C3N4/Bi4O7 heterojunction photocatalyst with enhanced visible light-driven activity toward organic pollutants. Journal of Colloid and Interface Science. 501123-501132.

Mingjuan, Z., Z. Yi, T. Lin, et al., 2019. Ultrathin Bi2WO6 nanosheets loaded g-C3N4 quantum dots: A direct Z-scheme photocatalyst with enhanced photocatalytic activity towards degradation of organic pollutants under wide spectrum light irradiation. Journal of Colloid and Interface Science. 539654-539664.

Qingyong, L., W. Fulei, H. Yuxiang, et al., 2017. Deposition-precipitation preparation of Ag/Ag3PO4/WO3 nanocomposites for efficient Visible-light degradation of rhodamine B under strongly acidic/alkaline conditions. Journal of Colloid and Interface Science. 506, 207-216.

Xin, Y., L. Zhonghua, L. Jiawen, et al., 2016. TaOC chemical bond enhancing charge separation between Ta4+ doped Ta2O5 quantum dots and cotton-like g-C3N4. Applied Catalysis B: Environmental. 205, 271-280.

Xixian, H., Z. Nengwu, M. Fulin, et al., 2020. Novel Au@C modified g-C3N4 (Au@C/g-C3N4) as efficient visible-light photocatalyst for toxic organic pollutant degradation: Synthesis, performance and mechanism insight. Separation and Purification Technology. 252, 117485.

Yingming, W., L. Xiaoxiao, G. Lin, et al., 2021. Metal organic framework-derived C-doped ZnO/TiO2 nanocomposite catalysts for enhanced photodegradation of Rhodamine B. Journal of Colloid and Interface Science. 599, 566-576.

Yuanzhi, H., M. Yadong, Z. Guangyi, et al., 2016. Facile fabrication of stable metal-free CQDs/g-C3N4 heterojunctions with efficiently enhanced visible-light photocatalytic activity. Separation and Purification Technology. 171229-171237.

Zhichao, S., Y. Zhiquan, L. Yingya, et al., 2018. Construction of 2D/2D BiVO4/g-C3N4 nanosheet heterostructures with improved photocatalytic activity. Journal of Colloid and Interface Science. 533251-533258.