Supporting Information

Flower-like CoP coated NiMoO4 nanorods as self-supported core-shell heterojunction electrode can facilitate oxygen evolution reaction at a low overpotential

Nu Wang a, Kai Huo a, Hongli Zhu b, Haoran Zi c, Yan Shan a,**, Kezheng Chen a, Xuegang Yu a,*

a Lab of Functional and Biomedical Nanomaterials, College of Materials Science and Engineering, Qingdao University of Science and Technology, Qingdao 266042, China.

b Institute 53 of China's Ordnance Industry, Jinan 250031, China.

c Chinese People's Liberation Army 32382 Unit, Beijing, 100072, China

* Corresponding authors. E-mail addresses: yuxuegang@qust.edu.cn (X. Yu), shanyan@qust.edu.cn (Y. Shan)

Material characterizations

The chemical composition and crystal structure type of the self-supported core-shell structure amorphous samples were confirmed by using an X-ray diffraction (XRD, Rigaku, D/MAX/2500PC) at a scanning rate of 5° min-1 ranging from 5° to 80°. The microstructure and morphology of the samples were characterized by using scanning electron microscope (SEM, JEOL JSM-6700F), transmission electron microscope (TEM, JEOL JEM-2100PLUS), and elemental mapping (Energy dispersive X-ray spectroscopy, EDS). The surficial chemical analysis was characterized by X-ray photoelectron spectroscopy (XPS, Thermo ESCALAB XI+).

Electrochemical measurements

All tests of electrochemical properties were performed at CHI 660E workstation (CH Instruments, Shanghai). The catalyst, carbon rod and Ag/AgCl electrode were used as working electrode, counter electrode and reference electrode, respectively. The measured potentials were converted to the reversible hydrogen electrode (RHE) on the basis of the Nernst equation: E(RHE) = E (Ag/ AgCl) + 0.2223 + 0.059 × pH. The pH value of the solution is around 14. Before measurement, we measured 200 cycles of cyclic voltammetry (CV) to obtain a stable response, which could make the data more realistic. Then, recorded the linear sweep voltammetry (LSV) date of OER at the scanning rate of 5 mV s-1 after iR drop compensation, which the compensation level was 90%. Electrochemical impedance spectroscopy (EIS) was measured at a frequency from 10-2 to 105 Hz. Then calculated the over potential (η) of OER exactly by using the equation: η(V) = E(RHE) – 1.23 V and replotted curves as η versus log current density (j) to get Tafel slopes. The estimate of the electrochemically active surface area (ECSA) was conducted by cyclic voltammetry (CV) at a non-Faradaic potential, which was ranging from 0.848 to 0.948 V vs. RHE of OER at 20, 40, 60, 80, 100 mV s-1 scan rates.

Theoretical calculations

In order to explore the changes in the electronic structure of cobalt phosphide microcrystalline supported with nickel molybdate, the researchers established three models (crystalline, amorphous, clustered) to distinguish the electrocatalytic advantages of microcrystalline cobalt phosphide. Theoretical calculations based on density functional theory (DFT) were carried out by using Vienna ab initio simulation package (VASP). During this period, various convenient data processing programs including vaspkit[1], qvasp[2], etc. were used. The generalized gradient approximation (GGA) of Perdew-Burke-Ernzerhof (PBE) exchange–correlation functional was adopted, and the interactions between electron and ion were described by the projector augmented wave (PAW) pseudopotentials. The kinetic cut-off energy of the plane-wave expansion was set to 400 eV. To consider the long-range van der Waals interactions, Grimme’s DFT-D3 correction[3] was employed, and only the Γ point was involved in Brillouin zone integration. In the process of structural optimization of the heterojunction model, the coordinates of all atoms and the lattice parameters of the model were optimized step by step to achieve a more efficient convergence progress, and the convergence thresholds of the energy change and the maximum force were set to 10-5 eV and 0.03 eV/ Å, respectively.

Fig. S1. SEM images of CoP-12/NF (a) and CoP-12@NiMoO4/NF (b).

Fig. S2. HRTEM image of NiMoO4/NF (a) and TEM image of CoP-12/NF (b).

Fig. S3. XRD pattern of CoP-12/NF.

Fig. S4. XRD pattern of CoP-12@NiMoO4/NF.

Fig. S5. XPS survey spectrum of NiMoO4/NF (a). High-resolution XPS spectra for NiMoO4/NF of Ni 2p (b), Mo 3d (c).

Fig. S6. XPS survey spectrum of CoP-12@NiMoO4/NF before 5000 cycles CV.

Fig. S7. The LSV curves of various electrodes.

Fig. S8. The CV curves of CoP-12@NiMoO4/NF.

Fig. S9. The CV curves of CoP-12/NF (a), NiMoO4/NF (b), CoP-6@NiMoO4/NF (c), CoP-9@NiMoO4/NF (d), CoP-15@NiMoO4/NF (e).

Fig. S10. The polarization curve after the water splitting process.

Fig. S11.The Chronopotentiometric curve of Ce-NiFe LDH@NiMoOxS4-x at 10, 30 and 50 mA cm-2.

Fig. S12. OER Faradic efficiency for CoP-12@NiMoO4.

Fig. S13. SEM image of CoP-12@NiMoO4/NF after 5000 cycles CV (a). TEM image of CoP-12@NiMoO4/NF after 5000 cycles CV (b).

Fig. S13. Electrostatic potential map of CoP (a) and NiMoO4 (b) along the Z axis.

Fig. S14. Electrostatic potential map of CoP-12@NiMoO4 (a)

Table S1. The element state ratio of Ni and Co between before 5000 CV cycles and after 5000 cycles CV.

| Element state ratio | Before CV cycles | After 5000 CV cycles |
| --- | --- | --- |
| Ni2+:Ni3+ | 85.54%:14.46% | 42.23%:57.77% |
| Co2+:Co3+ | 65.57%:34.43% | 60.69%:39.31% |

Table S2. Comparison of OER activity of CoP-12@NiMoO4/NF with other reported OER electrocatalysts

| Electrocatalyst | Current density (mA cm-2) | Over potential (mV) | References |
| --- | --- | --- | --- |
| CoP-12@NiMoO4/NF | 10 | 165 | This work |
| Mn-CoP | 10 | 285 | [4] |
| CoP/C | 10 | 330 | [5] |
| O-doped Co2P/CuO NWs/CF | 10 | 270 | [6] |
| CoP–TiOx | 10 | 337 | [7] |
| PrBa0.5Sr0.5Co2O5+δ/FeOOH | 10 | 390 | [8] |
| FeOOH@Ni(OH)2 | 10 | 310 | [9] |
| CoP/rGO | 10 | 340 | [10] |
| Ni2P/Ni3S2/NF | 10 | 290 | [11] |
| MnCoP/CC | 10 | 261 | [12] |
| Co3O4/NiCo2O4 | 10 | 340 | [13] |

Table S3. Comparison of over potentials and Tafel slopes of various Catalysts.

| Catalyst | η10 (mV) | η50 (mV) | Tafel slopes (mV dec-1) |
| --- | --- | --- | --- |
| CoP-12/NF | 307 | 368 | 67 |
| NiMoO4/NF | 218 | 305 | 68 |
| CoP-12@NiMoO4/NF | 165 | 229 | 45 |

Table S4. The solution resistances (Rs) and charge transfer resistance (Rct) comparison of the CoP-12/NF, NiMoO4/NF and CoP-12@NiMoO4/NF.

| Electrode | Rs | Rct |
| --- | --- | --- |
| CoP-12/NF | 1.2485 | 3.896 |
| NiMoO4/NF | 1.2635 | 2.017 |
| CoP-12@NiMoO4/NF | 1.3637 | 1.207 |

References

[1] V. Wang, N. Xu, J.C. Liu, G. Tang, W.T. Geng, VASPKIT: A user-friendly interface facilitating high-throughput computing and analysis using VASP code, Comput. Phys. Commun., 267 (2021) 19.

[2] W.C. Yi, G. Tang, X. Chen, B.C. Yang, X.B. Liu, qvasp: A flexible toolkit for VASP users in materials simulations, Comput. Phys. Commun., 257 (2020) 6.

[3] S. Grimme, J. Antony, S. Ehrlich, H. Krieg, A consistent and accurate ab initio parametrization of density functional dispersion correction (DFT-D) for the 94 elements H-Pu, J. Chem. Phys., 132 (2010) 19.

[4] S. Qin, Y.C. Yao, M. Qian, Q.H. Yang, T.Y. Chen, H.J. Xu, L. Zheng, Hierarchical Microspheres Composed of Mn-Doped CoP Nanosheets for Enhanced Oxygen Evolution, ACS Appl. Nano Mater., 3 (2020) 10702-10707.

[5] Y.J. Bai, H.J. Zhang, Y.Y. Feng, L. Fang, Y. Wang, Sandwich-like CoP/C nanocomposites as efficient and stable oxygen evolution catalysts, J. Mater. Chem. A, 4 (2016) 9072-9079.

[6] T.L.L. Doan, D.T. Tran, D.C. Nguyen, H.T. Le, N.H. Kim, J.H. Lee, Hierarchical three-dimensional framework interface assembled from oxygen-doped cobalt phosphide layer-shelled metal nanowires for efficient electrocatalytic water splitting, Appl. Catal. B-Environ., 261 (2020) 13.

[7] Z.B. Liang, W.Y. Zhou, S. Gao, R. Zhao, H. Zhang, Y.Q. Tang, J.Q. Cheng, T.J. Qiu, B.J. Zhu, C. Qu, W.H. Guo, Q. Wang, R.Q. Zou, Fabrication of Hollow CoP/TiOx Heterostructures for Enhanced Oxygen Evolution Reaction, Small, 16 (2020) 10.

[8] Z.H. Zhang, B.B. He, L.J. Chen, H.W. Wang, R. Wang, L. Zhao, Y.S. Gong, Boosting Overall Water Splitting via FeOOH Nanoflake-Decorated PrBa0.5Sr0.5Co2O5+δ Nanorods, ACS Appl. Mater. Interfaces, 10 (2018) 38032-38041.

[9] J.Y. Wang, S.M. Li, R.B. Lin, G.M. Tu, J. Wang, Z.Q. Li, MOF-derived hollow beta-FeOOH polyhedra anchored with alpha-Ni(OH)2 nanosheets as efficient electrocatalysts for oxygen evolution, Electrochim. Acta, 301 (2019) 258-266.

[10] L. Jiao, Y.X. Zhou, H.L. Jiang, Metal-organic framework-based CoP/reduced graphene oxide: high-performance bifunctional electrocatalyst for overall water splitting, Chem. Sci., 7 (2016) 1690-1695.

[11] L.Y. Zeng, K.A. Sun, X.B. Wang, Y.Q. Liu, Y. Pan, Z. Liu, D.W. Cao, Y. Song, S.H. Liu, C.G. Liu, Three-dimensional-networked Ni2P/Ni3S2 heteronanoflake arrays for highly enhanced electrochemical overall-water-splitting activity, Nano Energy, 51 (2018) 26-36.

[12] M.S. Wang, W.Y. Fu, L. Du, Y.S. Wei, P. Rao, L. Wei, X.S. Zhao, Y. Wang, S.H. Sun, Surface engineering by doping manganese into cobalt phosphide towards highly efficient bifunctional HER and OER electrocatalysis, Appl. Surf. Sci., 515 (2020) 7.

[13] H. Hu, B.Y. Guan, B.Y. Xia, X.W. Lou, Designed Formation of Co3O4/NiCo2O4 Double-Shelled Nanocages with Enhanced Pseudocapacitive and Electrocatalytic Properties, J. Am. Chem. Soc., 137 (2015) 5590-5595.