Appendix A. Supporting Information

Surface modification of pyrophyllite for optimizing properties of castor oil-based polyurethane composite and its application in controlled-release fertilizer

Shiping Wanga, Xiang Lia, Kun Rena, Rui Huanga, Ganchang Leia, Lijuan Shenb,

Yingying Zhana, *, Lilong Jianga,*

a National Engineering Research Center of Chemical Fertilizer Catalyst, Fuzhou University, Fuzhou 350002, China

b College of Environmental Science and Engineering, Fujian Normal University,

Fuzhou 350007, China

E-mail addresses: jll@fzu.edu.cn (L. Jiang), zhanyingying@fzu.edu.cn (Y. Zhan)

- Tables

Table S 1. The preparation conditions for the xMPY and their composite with PU (xMPY/PU).

|  | Preparation of xMPY |  | Preparation of xMPY/PU |  |  |
| --- | --- | --- | --- | --- | --- |
| Sample Name | PY addition | NDZ-201 emulsion solution | PY or MPY addition | CO addition | TDI addition |
| PY/PU | 10 g | 0 g | 0.24 g | 3.87 g | 1 g |
| 0.2MPY/PU | 10 g | 0.04 g | 0.24 g | 3.87 g | 1 g |
| 0.3MPY/PU | 10 g | 0.06 g | 0.24 g | 3.87 g | 1 g |
| 0.4MPY/PU(-5) | 10 g | 0.08 g | 0.24 g | 3.87 g | 1 g |
| 0.5MPY/PU | 10 g | 0.10 g | 0.24 g | 3.87 g | 1 g |
| 0.4MPY/PU-3 | 10 g | 0.08 g | 0.15 g | 3.87 g | 1 g |
| 0.4MPY/PU-7 | 10 g | 0.08 g | 0.34 g | 3.87 g | 1 g |
| 0.4MPY/PU-9 | 10 g | 0.08 g | 0.44 g | 3.87 g | 1 g |
| 0.4MPY/PU-11 | 10 g | 0.08 g | 0.54 g | 3.87 g | 1 g |

Note: The NDZ-201 emulsion solution was prepared from the mixture of isopropanol and NDZ-201 with a mass ratio of 1:1.

Table S2. The surface concentrations of Al, Si and O in the PY and different modified MPY measured by XPS.

| Sample Name | Al (at%) | Si (at%) | O (at%) | O/Al |
| --- | --- | --- | --- | --- |
| PY | 12.31 | 23.46 | 64.23 | 5.22 |
| 0.2MPY | 12.14 | 23.86 | 64.00 | 5.27 |
| 0.3MPY | 11.85 | 23.62 | 64.53 | 5.46 |
| 0.4MPY | 11.67 | 24.08 | 64.24 | 5.50 |
| 0.5MPY | 12.05 | 24.40 | 63.55 | 5.27 |

Table S3. Retention of tensile strength and elongation at break of PU, PY/PU and 0.4MPY/PU.

| Sample Name | Retention of tensile strength (%) | Retention of elongation at break (%) |
| --- | --- | --- |
| PU | 88.4 | 80.0 |
| PY/PU | 85.4 | 73.8 |
| 0.4MPY/PU | 94.0 | 91.6 |

Table S4. The nitrogen cumulative release for PCU, PY/PCU, and the xMPY/PCU at different release time.

| Sample Name | Release at 3.5d (%) | Release at 7d (%) | Release at 14d (%) | Release at 21d (%) | Release at 28d (%) | Release at 35d (%) |
| --- | --- | --- | --- | --- | --- | --- |
| PCU | 1.5 | 13.2 | 64.0 | 77.9 | 80.4 | 82.22 |
| PY/PCU | 8.3 | 40.9 | 66.1 | 79.7 | 86.6 | - |
| 0.2MPY/PCU | 6.5 | 26.1 | 65.6 | 76.2 | 79.7 | - |
| 0.3MPY/PCU | 3.6 | 18.5 | 52.4 | 74.9 | 78.8 | - |
| 0.4MPY/PCU | 1.7 | 10.4 | 43.2 | 66.2 | 76.1 | 80.5 |
| 0.5MPY/PCU | 2.2 | 16.2 | 47.9 | 68.3 | 77.6 | 81.4 |

Table S5. The nitrogen cumulative releases for 0.4MPY/PCU-y with various filling amounts of MPY.

| Sample Name | Release at 14 d (%) | Release at 21d (%) | Release at 28 d (%) | Release at 40 d (%) | Release at 56 d (%) |
| --- | --- | --- | --- | --- | --- |
| 0.4MPY/PCU-3 | 47.4 | 73.2 | 79.2 | 81.5 | 84.8 |
| 0.4MPY/PCU-5 | 43.2 | 66.2 | 76.1 | 80.9 | 83.7 |
| 0.4MPY/PCU-7 | 33.1 | 62.0 | 73.9 | 78.9 | 84.5 |
| 0.4MPY/PCU-9 | 53.9 | 74.8 | 80.6 | 83.0 | 87.2 |
| 0.4MPY/PCU-11 | 65.9 | 77.6 | 80.3 | 83.6 | 86.7 |

Table S6. The release durations of the reported polymer coatings based on natural biomass.

| Biomass-Based PU Coatings | Coating Rate | Release Duration (75%) | References |
| --- | --- | --- | --- |
| DPCU | 8.5% inner and 8.7% outer coating | 42 d | J. Agri. Food Chem. 2013, 61, 8166-8174. |
| Soybean-based PU | 2.5% 4.5% | 8 d 23 d | J. Appl. Polym. Sci. 2016, 133, 43790. |
| castor oil-based PU | 2.5% 4% | 13 d 32 d | J. Appl. Polym. Sci. 2016, 133, 43790. |
| Soybean oil, oleic acid-based PU | 3% | 28 d | J. Agri. Food Chem. 2018,66, 11265-11272. |
| Castor-oil based PU | 4% 6% 8% | 14 d 33 d 47 d | J. Clean. Prod. 2020, 249, 119329. |
| Castor-oil based PU/ Nano fumed silica | 2% 3% | 105 d 137 d | J. Clean. Prod. 2020, 249, 119329. |
| Castor oil-base PU/Soy-protein microcapsules | 3% | 45 d | Mater. Today Chem. 2021, 20, 100413 |
| Castor-oil based PU/Halloysite | 3% | 30-38 d | Prog. Org. Coat. 2022, 165, 106756 |
| Wheat straw-derived PU | 3% | 32 d | Chem. Eng. J. 2022, 435, 134985 |

- Figures

Figure S1. The chemical structure of the NDZ-201 coupling agent.

Figure S2. TG curves of PY and 0.4MPY with a NDZ-201 addition amount of 0.4 wt%.

Figure S3. (a) and (b) SEM images the ball-milled PY (0.2MPY) with the NDZ-201 addition amount of 0.2 wt%, (c) and (d) the ball-milled PY (0.3MPY) with the NDZ-201 addition amount of 0.3 wt%, (e) and (f) the ball-milled PY (0.4MPY) with the NDZ-201 addition amount of 0.4 wt%, and the ball-milled PY (0.5MPY) with the NDZ-201 addition amount of 0.5wt% (g, h).

Figure S4. The water absorbency of the PU, PY/PU, and xMPY/PU, corresponding to the XMP modified by various addition amount of NDZ-201.

Figure S5. SEM images of 0.4MPY/PU-3 (a1, a2), 0.4MPY/PU-5 (b1, b2),  0.4MPY/PU-7 (c1, c2), 0.4MPY/PU-9 (d1, d2), and 0.4MPY/PU-11 (e1, e2), which were corresponded to the MPY/PU composites with various filling amount of MPY.

Figure S6. Mechanical properties of 0.4MPY/PU-y samples corresponded to the MPY/PU composites with different filling amounts of MPY.

Figure S7. Water absorbency of 0.4MPY/PU-y samples corresponded to the MPY/PU composites with different filling amounts of MPY.