Supplementary material

Novel composite in situ obtained from coal gasification coarse slag and its mechanism of removing phosphate

Baoguo Yang a,b, Yilian Li *a, Fenglan Han *c, Yadong Bai *b, Yonghong Zhang b, Jinhao Yu a, Zhongbiao Fu a

a Hubei Key Laboratory of Yangtze River Basin Environmental Aquatic Science, School of Environmental Studies, China University of Geosciences, NO. 68 Jincheng Street, East Lake High-Tech Development Zone, Wuhan, 430078, P. R. China

b Ningxia Institute of Geophysical and Geochemical Survey, Yinchuan 750001, China

c School of Materials Science and Engineering, North Minzu University, Yinchuan 750021, China

*Corresponding author

E-mail address: 625477897@qq.com (F. Han), yl.li@cug.edu.cn (Y. Li), byd1975@163.com (Y. Bai)

Text S1: Phosphate species at different pH solution

H3PO4, H2PO4-, HPO42- and PO43- are the main forms of the phosphate at different pH solution, which can be illustrated as follows (Abdellaoui et al., 2021; Xiong et al., 2017):

H3PO4 ka1  H++ H2PO4-  ka2  H++ HPO42-  ka3 PO43- + H+                               (2)

where dissociation constant pKa1, pK a2 and pK a3 are 2.15, 7.20 and 12.33, respectively.

Table S1

Chemical composition of samples (wt %).

| Sample | O | Si | Fe | Ca | Al | Ti | K | Mg | Cl | Na | Others |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CGCS | 40.23 | 16.27 | 14.50 | 13.38 | 7.59 | 0.75 | 1.92 | 0.78 | 0.77 | 0.97 | 2.85 |
| CGCS-H-W | 50.81 | 40.41 | 2.22 | 2.55 | 1.88 | 0.29 | 0.50 | 0.17 | 0.59 | 0.22 | 0.40 |
| HSMC | 43.72 | 23.05 | 6.33 | 5.71 | 11.47 | 0.84 | 0.96 | 1.62 | 5.2 | 0.42 | 0.68 |

Fig. S1. (a) N2 adsorption–desorption isotherms and (b) pore size distribution of HSMC and CGCS.

Table S2

BET specific surface area and BJH pore parameters of CGCS and HSMC.

| Sample | BET specific surface area (m2/g) | BJH average pore diameter (nm） | BJH cumulative volume of pores (cm3/g) |
| --- | --- | --- | --- |
| CGCS | 3.6 | 6.53 | 0.0094 |
| HSMC | 66.95 | 7.35 | 0.1651 |

Table S3

Adsorption isotherm parameters. Adsorption conditions: oscillation rate, 150 rpm; reaction time, 24 h; sorbent dose, 1 g/L; initial phosphate concentration, 5-80 mg/L.

| Langmuir |  |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| qm (mg/g) | kL (L/mg) | R2 |  | 1/n | KF ((mg/g)/(mg/L) 1/n) | R2 |
| 28.618 | 0.126 | 0.997 |  | 0.366 | 6.185 | 0.961 |

Table S4

Comparison of the adsorption capacity of HSMC and adsorbents given in literatures for phosphate.

| Adsorbent | Initial concentration (mg/L) | pH | Temperature (°C) | Sorption capacity (mg/g) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Zr/Al-Mt | 20–50 | 5.0 | 25 | 17.2 | (Huang et al., 2015) |
| Iron oxide tailings | 5-150 | 6.6-6.8 | 20-21 | 8.2 | (Zeng et al., 2004) |
| BFSs | 50-500 | 7.0 | 20 | 18.9 | (Kostura et al., 2005) |
| ACF-LaOH | 10-70 | / | 25 | 15.3 | (Zhang et al., 2012) |
| La-Ves | 1.02-5.03 | 7.1 | 25 | 6.7 | (Li et al., 2009) |
| La-Z | 5-60 | 6.0 | 40 | 17.2 | (He et al., 2017) |
| La-FACC | 10-200 | / | 25 | 24.9 | (Asaoka et al., 2021) |
| MKC | 0-160 | 7.5 | 25 | 11.92 | (Deng and Shi, 2015) |
| HSMC | 5-80 | 6 | 25 | 28.62 | This study |

Table S5

Adsorption kinetic parameters of HSMC to phosphate.

| Kinetic models and Experimental results | Plot parameters |  | Values |
| --- | --- | --- | --- |
| Experimental adsorption capacity | qe,exp (mg/g) |  | 24.22 |
| Pseudo-first-order | qe,cal (mg/g) |  | 23.346 |
|  | K1 (min-1) |  | 0.744 |
|  | R2 |  | 0.942 |
| Pseudo-second-order | qe,cal (mg/g) |  | 24.772 |
|  | K2 (min-1) |  | 0.045 |
|  | R2 |  | 0.996 |
| Intraparticle diffusion | Kid1 (mg/g min1/2) |  | 9.138 |
|  | C |  | 3.420 |
|  | R2 | 0.996 |  |
|  | Kid2 (mg/g min1/2) | 1.932 |  |
|  | C | 16.246 |  |
|  | R2 | 0.984 |  |
|  | Kid3 (mg/g min1/2) | 0.131 |  |
|  | C | 23.332 |  |
|  | R2 | 0.979 |  |

Table S6

Comparison of leaching results of calcium, aluminum and iron from HSMC.

| Element | Water type | Units | Content |
| --- | --- | --- | --- |
| Ca | DI water | mg/L | 16.1 |
| Al |  | mg/L | < 0.03 |
| Fe |  | mg/L | < 0.02 |
| Ca | Phosphate solution | mg/L | 5.2 |
| Al |  | mg/L | < 0.01 |
| Fe |  | mg/L | < 0.01 |

Table S7 Main components of actual wastewater.

| Main components | Units | Content |
| --- | --- | --- |
| Ca2+ | mg/L | 57.2 |
| K+ | mg/L | 6.7 |
| Mg2+ | mg/L | 129.1 |
| Na+ | mg/L | 477.8 |
| NH4+ | mg/L | 0.1 |
| Cl- | mg/L | 465.4 |
| NO3- | mg/L | 5.3 |
| SO42- | mg/L | 660.9 |
| HCO3- | mg/L | 481.6 |
| CODMn | mg/L | 4.3 |
| PO43- | mg/L | 0.04 |

Fig. S2. 2D correlation spectra of HSMC and phosphate reaction.

References

Abdellaoui, Y., Abou Oualid, H., Hsini, A., El Ibrahimi, B., Laabd, M., El Ouardi, M., Giácoman-Vallejos, G., Gamero-Melo, P., 2021. Synthesis of zirconium-modified merlinoite from fly ash for enhanced removal of phosphate in aqueous medium: experimental studies supported by monte carlo/sa simulations. Chem. Eng. J. 404, 126600. https://10.1016/j.cej.2020.126600.

Asaoka, S., Kawakami, K., Saito, H., Ichinari, T., Nohara, H., Oikawa, T., 2021. Adsorption of phosphate onto lanthanum-doped coal fly ash—blast furnace cement composite. J. Hazard. Mater. 406, 124780. https://10.1016/j.jhazmat.2020.124780.

Deng, L., Shi, Z., 2015. Synthesis and characterization of a novel mg–al hydrotalcite-loaded kaolin clay and its adsorption properties for phosphate in aqueous solution. J. Alloy. Compd. 637, 188-196. https://10.1016/j.jallcom.2015.03.022.

He, Y., Lin, H., Dong, Y., Wang, L., 2017. Preferable adsorption of phosphate using lanthanum-incorporated porous zeolite: characteristics and mechanism. Appl. Surf. Sci. 426, 995-1004. https://10.1016/j.apsusc.2017.07.272.

Huang, W., Chen, J., He, F., Tang, J., Li, D., Zhu, Y., Zhang, Y., 2015. Effective phosphate adsorption by zr/al-pillared montmorillonite: insight into equilibrium, kinetics and thermodynamics. Appl. Clay Sci. 104, 252-260. https://10.1016/j.clay.2014.12.002.

Kostura, B., Kulveitová, H., Leško, J., 2005. Blast furnace slags as sorbents of phosphate from water solutions. Water Res. 39, 1795-1802. https://10.1016/j.watres.2005.03.010.

Li, H., Ru, J., Yin, W., Liu, X., Wang, J., Zhang, W., 2009. Removal of phosphate from polluted water by lanthanum doped vesuvianite. J. Hazard. Mater. 168, 326-330. https://10.1016/j.jhazmat.2009.02.025.

Xiong, W., Tong, J., Yang, Z., Zeng, G., Zhou, Y., Wang, D., Song, P., Xu, R., Zhang, C., Cheng, M., 2017. Adsorption of phosphate from aqueous solution using iron-zirconium modified activated carbon nanofiber: performance and mechanism. J. Colloid Interface Sci. 493, 17-23. https://10.1016/j.jcis.2017.01.024.

Zeng, L., Li, X., Liu, J., 2004. Adsorptive removal of phosphate from aqueous solutions using iron oxide tailings. Water Res. 38, 1318-1326. https://10.1016/j.watres.2003.12.009.

Zhang, L., Zhou, Q., Liu, J., Chang, N., Wan, L., Chen, J., 2012. Phosphate adsorption on lanthanum hydroxide-doped activated carbon fiber. Chem. Eng. J. 185-186, 160-167. https://10.1016/j.cej.2012.01.066.