Supporting Information for:

Enhanced superhydrophobicity of electrospun carbon nanofiber membranes by hydrothermal growth of ZnO nanorods for oil-water separation

Linzhan Bai a, Xinyan Wang b, Xichao Sun c, Jiao Li a,*, Lilan Huang a, Haibin Sun a, Xueli Gao d,*

a School of Materials Science and Engineering, Shandong University of Technology, Zibo 255000, China

b Shandong Zhaojin Motian Co., Ltd., Yantai 265400, China

c Shandong Dongyue Organic Silicon Material Co., Ltd., Zibo 255000, China

d Key Laboratory of Marine Chemistry Theory and Technology, Ministry of Education, Ocean University of China, Qingdao 266100, China

Text 1. The calculation method for the density and porosity of membrane.

The porosity (%) of the membrane was calculated by the following formula (Xu et al., 2021; Fu et al., 2021):

Porosity (%)=m2-m1ρV×100%

where m2 is the weight of the wetting membrane (g), m1 is the weight of the drying membrane (g), ρ is the density of n-butanol (0.811 g/cm3), and V is the volume of the membrane (cm3).

The formula for calculating the membrane density (ρ) was as follows:

ρ=mV

where m is the weight of the membrane (g), V is the volume of the membrane (cm3).

Text 2. Details of emulsion separation experiments.

To prepare the water-in-oil emulsion, carbon tetrachloride and water were mixed with a ratio of 99:1. Then, 0.2 mg/mL Span-80 was added as a surfactant stabilization emulsion. Finally, the mixture was mechanically stirred at 1300 rpm/min for 3h to obtain a milky emulsion. The separation efficiency (f) of emulsion was determined by the following formula (Xu et al., 2021):

f=1-cc0×100%                      (3)

where C0 and C were the water content in the emulsion and filtrate, respectively.

Xu, H., Liu, H., Huang, Y., Xiao, C., 2021. Three-dimensional structure design of tubular polyvinyl chloride hybrid nanofiber membranes for water-in-oil emulsion separation. J. Membr. Sci. 620, 118905. https://doi.org/10.1016/j.memsci.2020.118905.

Fu, Q., Zhang, W., Muhammad, I.P., Chen,X., Zeng, Y., Wang, B., Zhang, S., 2021. Coaxially electrospun PAN/HCNFs@PVDF/UiO-66 composite separator with high strength and thermal stability for lithium-ion battery. Micropor. Mesopor. Mater. 311, 110724. https://doi.org/10.1016/j.micromeso.2020.110724.

Table S1. Possible formation mechanism of ZnO nanorods.

| Chemical reaction | Order |
| --- | --- |
| C6H12N4+6H2O↔6HCHO+4NH3 | (1) |
| NH3+H2O↔NH4++OH- | (2) |
| ZnNO32↔Zn2++2NO3- | (3) |
| Zn2++ 2OH-↔2ZnOH2 | (4) |
| ZnOH2↔ZnO+H2O | (5) |

Table S2. The density and porosity of the F/ZnO/CNF-x membrane.

| Materials | Density(g/cm3) | Porosity(%) |
| --- | --- | --- |
| CNF | 0.1139 | 63% |
| F/ZnO/CNF-1 | 0.1426 | 57% |
| F/ZnO/CNF-2 | 0.1608 | 45% |
| F/ZnO/CNF-3 | 0.1923 | 37% |
| F/ZnO/CNF-4 | 0.2040 | 29% |

Table S3. Comparison of separation efficiency of the F/ZnO/CNF-3 with other membrane materials reported in the literature.

| Materials | Oil-water mixture | Efficiency (%) | Ref. |
| --- | --- | --- | --- |
| TiO2–PVA sponge | CCl4/water mixture | 97.8 | (He et al., 2022) |
| PCL/ph-LPSQ membranes | CCl4/water mixture | 99.3 | (Wang et al., 2022) |
| Biomimetic membrane | Chloroform/water mixture | 98 | (Chen et al., 2022) |
| #### Janus–CA Fiber Membrane | water-in-toluene emulsion | 98.7 | (Yu et al., 2021) |
|  | n-hexane/water mixture | 97.1 |  |
| CNF grafted PU | Hexane/water mixture | 97.8 | (Baig et al., 2019) |
| PPS membrane | Water-in-CCl4 emulsions | 99 | (Kou et al., 2021) |
| CNFM | Chloroform/water mixture | 99.4 | (Kong and Xin, 2022) |
|  | Water-in-CCl4 emulsions | 98.7 |  |
| F/ZnO/CNF | CCl4/water mixture | 99.7 | This work |
|  | Water-in-CCl4 emulsions | 99.2 |  |

He, Z., Wu, H., Shi, Z., Kong, Z., Ma, S., Sun, Y., Liu, X., 2022. Facile Preparation of Robust Superhydrophobic/Superoleophilic TiO2-Decorated Polyvinyl Alcohol Sponge for Efficient Oil/Water Separation. ACS Omega 7, 7084-7095. https://doi.org/10.1021/acsomega.1c06775.

Wang, F., Liu, K., Xi, Y., Li, Z., 2022. One-step electrospinning PCL/ph-LPSQ nanofibrous membrane with excellent self-cleaning and oil-water separation performance. Polymer 249, 124858. https://doi.org/10.1016/j.polymer.2022.124858.

Chen, Y., Quan, Z., Song, W., Wang, Z., Li, B., Mu, Z., Niu, S., Zhang, J., Han, Z., Ren, L., 2022.Hierarchically structured biomimetic membrane with mechanically/chemically durability and special wettability for highly efficient oil–water separation. Sep. Purif. Technol. 300, 121860. https://doi.org/10.1016/j.seppur.2022.121860.

Yu, X., Zhang, X., Xing, Y., Zhang, H., Jiang, W., Zhou, K., Li, Y., 2021. Development of Janus Cellulose Acetate Fiber (CA) Membranes for Highly Efficient Oil–Water Separation. Materials 14(20), 5916. https://doi.org/10.3390/ma14205916.

Baig, N., Alghunaimi, F. I., Dossary, H. S., Saleh, T. A., 2019. Superhydrophobic and superoleophilic carbon nanofiber grafted polyurethane for oil-water separation. Process Saf. Environ. 123, 327-334. https://doi.org/10.1016/j.psep.2019.01.007.

Kou, X., Han, N., Zhang, Y., Tian, S., Li, P., Wang, W., Wu, C., Li,W., Yan,X., Zhang, X., 2021. Fabrication of polyphenylene sulfide nanofibrous membrane via sacrificial templated-electrospinning for fast gravity-driven water-in-oil emulsion separation. Sep. Purif. Technol. 275, 119124. https://doi.org/10.1016/j.seppur.2021.119124.

Kong, F. and Xin, B., 2022. Three-dimensional and flexible carbon nanofiber mat by one-step electrospinning for efficient oil/water separation. Colloid. Surf. A 652, 129824. https://doi.org/10.1016/j.colsurfa.2022.129824.

Fig. S1. Schematic diagram of fluorination.

Fig. S2. The EDS result of F/ZnO/CNF-3.

Fig. S3. Strain-stress curves (a) and Young's modulus (b) of F/ZnO/CNF-x membrane at different hydrothermal time.

Fig. S4. Optical microscope images and digital photographs of the emulsion and filtrate (a), flux and separation efficiency of F/ZnO/CNF-x membranes(b), cycle separation performance of F/ZnO/CNF-3 membrane for emulsion (c).

Fig. S5. WCAs and separation efficiency (carbon tetrachloride/water mixture) of F/ZnO/CNF-3 before and after soaking in different pH solution.

* Corresponding authors.

E-mail addresses: haiyan9943@163.com (J. Li), gxl_ouc@126.com (X. Gao).