Supplementary Information

An unexpectedly stable Y2B5 compound with the fractional stoichiometry under ambient pressure

Yuanyuan Jina, Wenjie Huanga, Jinquan Zhang a, Song Lia, Shubo Chenga, Weiguo Sunb, Meng Juc, Chuanzhao Zhanga,*

a Department of Physics and Optoelectronic Engineering, Yangtze University, Jingzhou 434023, China

b College of Physics and Electronic Information, Luoyang Normal University, Luoyang 471022, China

c School of Physical Science and Technology, Southwest University, Chongqing 400715, China

* Corresponding author.

E-mail address: zcz19870517@163.com (Chuanzhao Zhang).

Fig. S1 Crystal structures of the lowest enthalpy phases of each components in the YB system. (a) PnmaY2B, (b) P4/mbmY3B2, (c) CmcmYB, (d) ImmmY3B4, (e) P63/mmcY2B3, (f) P6/mmmYB2, (g) P121/c1Y2B5, (h) R-3mYB3, (i)P4/mbmYB4, (j) Pm3mYB6 and (k) Fm3mYB12. The red and blue spheres represent Y and B atoms, respectively.

Fig. S2 Predicted Gibbs free energies of various Y-B compounds under ambient pressure with respect to -Y and -B at the temperatures of (a) 0, (b) 300, (c) 1000 and (d) 2000 K. Dashed lines connect data points, and solid lines represent the convex hull.

Fig. S3 Free energy as a function of MD time at the temperature of 300 K for (a) Cmcm-YB, (b) P6/mmm-YB2, (c) P21/c-Y2B5, (d) P4/mbm-YB4, (e) Pm-3m-YB6 and (f) Fm-3m-YB12.

Table S1 The lattice constants a, b and cÅ and the occupied positions of the lowest enthalpy phases of each components in the YB system.

|  | Structure | Lattice parameters (Å) | Positions |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Atom | x |  | y |  | z |  |  |
| Y2B | Pnma (62) | a = 6.358, b = 3.697, c = 11.424 | Y1(4c) | 0.99995 |  | 0.25000 |  | 0.75003 |  |  |
|  |  |  | Y2(4c) | 0.24994 |  | 0.25000 |  | 0.48100 |  |  |
|  |  |  | B1(4c) | 0.25011 |  | 0.25000 |  | 0.14246 |  |  |
| Y3B2 | P4/mbm (127) | a = 6.778, b = 6.778, c = 4.191 | Y1(2a) | 0.00000 |  | 0.00000 |  | 0.00000 |  |  |
|  |  |  | Y2(4h) | 0.17265 |  | 0.672658 |  | 0.50000 |  |  |
|  |  |  | B1(4g) | 0.41109 |  | 0.91109 |  | 0.00000 |  |  |
| YB | Cmcm (63) | a = 3.550, b = 12.962, c = 3.192 | Y1(4c) | 0.00000 |  | 0.37554 |  | 0.25000 |  |  |
|  |  |  | B1(4c) | 0.00000 |  | 0.02315 |  | 0.25000 |  |  |
| Y3B4 | Immm (71) | a = 3.784, b = 17.308, c = 3.261 | Y1(2c) | 0.50000 |  | 0.50000 |  | 0.00000 |  |  |
|  |  |  | Y2(4g) | 0.00000 |  | 0.16862 |  | 0.00000 |  |  |
|  |  |  | B1(4g) | 0.00000 |  | 0.39619 |  | 0.00000 |  |  |
|  |  |  | B2(4h) | 0.00000 |  | 0.44347 |  | 0.50000 |  |  |
| Y2B3 | P63/mmc (194) | a = 3.293, b = 3.293, c = 16.476 | Y1(4f) | 0.33333 |  | 0.66667 |  | 0.13898 |  |  |
|  |  |  | B1(4f) | 0.33333 |  | 0.66667 |  | 0.51116 |  |  |
|  |  |  | B2(2d) | 0.33333 |  | 0.66667 |  | 0.75000 |  |  |
| YB2 | P6/mmm (194) | a = 3.296, b = 3.296, c = 3.858 | Y1(1a) | 0.00000 |  | 0.00000 |  | 0.00000 |  |  |
|  |  |  | B1(2d) | 0.33333 |  | 0.66667 |  | 0.50000 |  |  |
| Y2B5 | P121/c1 (14) | a = 7.136, b=7.159, c = 7.183 | Y1(4e) | 0.23226 |  | 0.19256 |  | 0.62620 |  |  |
|  |  |  | Y2(4e) | 0.24228 |  | 0.81458 |  | 1.25293 |  |  |
|  |  |  | B1(4e) | 0.50341 |  | 0.67373 |  | 0.53959 |  |  |
|  |  |  | B2(4e) | 0.50109 |  | 0.08926 |  | 1.41081 |  |  |
|  |  |  | B3(4e) | 0.50347 |  | 0.03824 |  | 1.17433 |  |  |
|  |  |  | B4(4e) | 0.07411 |  | 0.99012 |  | 0.92498 |  |  |
|  |  |  | B5(4e) | 0.68603 |  | 0.00197 |  | 1.04120 |  |  |
| YB3 | R-3m (166) | a = 5.404, b = 5.404, c = 11.886 | Y1(6c) | 0.00000 |  | 0.00000 |  | 0.16558 |  |  |
|  |  |  | B1(2e) | 0.32933 |  | 0.00402 |  | 0.33333 |  |  |
| YB4 | P4/mbm (127) | a = 7.104, b = 7.104, c = 4.022 | Y1(4g) | 0.31772 |  | 0.81772 |  | 0.00000 |  |  |
|  |  |  | B1(4e) | 0.00000 |  | 0.00000 |  | 0.20297 |  |  |
|  |  |  | B2(4h) | 0.91312 |  | 0.41312 |  | 0.50000 |  |  |
|  |  |  | B3(8j) | 0.17611 |  | 0.03843 |  | 0.50000 |  |  |
| YB6 | Pm-3m (221) | a = 4.098, b = 4.098, c = 4.098 | Y1(1a) | 0.00000 |  | 0.00000 |  | 0.00000 |  |  |
|  |  |  | B1(6f) | 0.50000 |  | 0.50000 |  | 0.19895 |  |  |
| YB12 | Fm-3m (225) | a =7.495, b = 7.495, c = 7.495 | Y1(4a) | 0.00000 |  | 0.00000 |  | 0.00000 |  |  |
|  |  |  | B1(48i) |  | 0.50000 |  | 0.16879 |  | 0.16879 |

Table S2 Calculated lattice parameters, a, b and c Åcell volume per formula unit V(Å3), total enthalpies per formula unit H eV and formation enthalpies per atom ∆H (eV) for the lowest formation enthalpy of each compositions of the Y−B binary system, compared with previous results.

|  | Space group | a (Å) | b (Å) | c (Å) | V (Å3) | H (eV) | ∆H (eV) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Y2B | Pnma | 6.358 | 3.697 | 11.424 | 67.13 | 19.62 | 0.01 |
| Y3B2 | P4/mbm | 6.778 | 6.778 | 4.191 | 96.28 | 33.40 | 0.14 |
| YB | Cmcm | 3.550 | 12.962 | 3.192 | 146.87 | 27.95 | 0.41 |
| Y3B4 | Immm | 3.784 | 17.308 | 3.261 | 106.78 | 49.19 | 0.43 |
| Y2B3 | P63/mmc | 3.294 | 3.294 | 16.476 | 77.41 | 31.20 | 0.36 |
| YB2 | P6/mmm | 3.296 | 3.296 | 3.858 | 36.29 | 21.58 | 0.58 |
|  |  | 3.298a | 3.298a | 3.843a |  |  |  |
|  |  | 3.288b | 3.288b | 3.836b |  |  |  |
| Y2B5 | P121/c1 | 7.093 | 7.103 | 7.125 | 87.35 |  | 0.61 |
| YB3 | R-3m | 5.404 | 5.404 | 11.886 | 150.28 | 27.11 | 0.14 |
| YB4 | P4/mbm | 7.104 | 7.104 | 4.022 | 50.74 | 36.26 | 0.60 |
|  |  | 7.111a | 7.111a | 4.017a |  |  |  |
|  |  | 7.106b | 7.106b | 4.020b |  |  |  |
|  |  | 7.107c | 7.107c | 4.018c |  |  |  |
| YB6 | Pm-3m | 4.098 | 4.098 | 4.098 | 68.82 | 49.50 | 0.41 |
|  |  | 4.113a | 4.113a | 4.113a |  |  |  |
|  |  | 4.102b | 4.102b | 4.102b |  |  |  |
|  |  | 4.110d | 4.110d | 4.110d |  |  |  |
| YB12 | Fm-3m | 7.495 | 7.495 | 7.495 | 105.25 | 90.16 | 0.25 |
|  |  | 7.501a | 7.501a | 7.501a |  |  |  |
|  |  | 7.501b | 7.501b | 7.501b |  |  |  |
| aReference 1. bReference 2. cReference 3. dReference 4. |  |  |  |  |  |  |  |

References

1. P.K. Liao, K.E. Spear, The B−Y(boron−yttrium) system, J. Phase Equilib. 16 (6) (1995) 521−524.

2. C. Colinet, J.C. Tedenac, Enthalpies of formation of rare-earth borides from first principles. Comparison with experimental values, Calphad 62 (2018) 4960.

3. J.A. Zaykoski, M.M. Opeka, L.H. Smith, I.G. Talmy, Synthesis and characterization of YB4 ceramics, J. Am. Ceram. Soc. 94 (11) (2011) 4059–4065.

4. M. Romero, A. Benitez-Rico, E.P. Arévalo-López, R.W. Gómez, M.L. Marquina, J.L. Rosas, R. Escamilla, First-principles calculations of the structural, elastic, vibrational and electronic properties of YB6 compound under pressure, Eur. Phys. J. B 92 (2019) 159.