Supplementary material

Efficient reduction of NOx emissions from waste double-base propellant in

co-pyrolysis with pine sawdust

Guorui Jin a, b, Moru Wang a, b, Jianwei Zhang a, b, Ling Chen a, b, Xin Liao a, b, Weidong He a, b, *

a School of Chemistry and Chemical Engineering, Nanjing University of Science and Technology, Nanjing, 210094, China

b Key Laboratory of Special Energy Materials, Ministry of Education, Nanjing, 210094, China

* Corresponding authors at: School of Chemistry and Chemical Engineering, Nanjing University of Science and Technology, Nanjing, 210094, China

E-mail address: hewedong@njust.edu.cn (W.D. He).

Table S1

MGA6 Technical specifications.

| Measuring gas | Measuring method | measuring range | resolution ratio | accuracy |
| --- | --- | --- | --- | --- |
| O2 | Electrochemistry | 0~25Vol% | 0.01 Vol% | 0.2% |
| NO | NDIR | 0~1000/4000 ppm | 0.1 ppm | 2%FS |
| NO2 | NDIR | 0~500/1000 ppm | 0.1 ppm | 2%FS |
| SO2 | NDIR | 0~500/1000 ppm | 0.1 ppm | 2%FS |
| CO2 | NDIR | 0~40 Vol% | 0.01 Vol% | 2%FS |
| CO | NDIR | 0~1000/10000 ppm | 0.1 ppm | 2%FS |
| CH4 | NDIR | 0~3000/10000 ppm | 0.1 ppm | 2%FS |

Fig. S1. SEM images of the raw material and the residue after pyrolysis at 900 ℃.

(a) DP raw material, (b) PS raw material, (c) DP pyrolysis residue, (d) PS pyrolysis residue, (e) D2P8 pyrolysis residue, (f) D4P6 pyrolysis residue, (g) D6P4 pyrolysis residue, (h) D8P2 pyrolysis residue, (i) D9P1 pyrolysis residue.

Fig. S2. EDS results of the raw material and the residue after pyrolysis at 900 ℃.

(a) DP raw material, (b) PS raw material, (c) DP pyrolysis residue, (d) PS pyrolysis residue, (e) D2P8 pyrolysis residue, (f) D4P6 pyrolysis residue, (g) D6P4 pyrolysis residue, (h) D8P2 pyrolysis residue, (i) D9P1 pyrolysis residue.