Supporting Information

Dual Functions of Nitrogen and Phosphorus Co-doped Carbon Dots for Drug-targeted Delivery and Two-photon Cell Imaging

Yanxu Liu a#, Kaiyue Sun a#, Nana Shi a#, Ronghui Li a, Jianjun Zhang b, Juan Zhao c, Lina Geng a*, Yuhua Lei c*

- College of Chemistry and Material Science, Hebei Key Laboratory of Organic Functional Molecules, Hebei Normal University, Shijiazhuang 050024, China.

- Testing and Analysis Center, Hebei Normal University, Shijiazhuang 050024, China

- College of Basic Medicine, Hebei Medical University, Shijiazhuang 050017, R. P. China.

# These authors contributed equally to this study.

* Corresponding author. E-mail addresses: lyh5615@163.com; genglina0102@126.com

Figure S1 fluorescence stability of N, P-CDs at different pH (A) and NaCl (B) solutions

Table S1:The comparison of drug loading efficiency between this work and the reported literature.

| Drug Loading System | Drug Loading Efficiency | Ref. |
| --- | --- | --- |
| FA-CDs-DOX | 31.43% |  |
| CDs-Hep/DOX | 32.2% |  |
| G-CDs/DOX | 28% |  |
| CDs-DOX | 1.87% |  |
| DOX-CDs | 6.82% |  |
| N,P-CDs-DOX | 39.11% | This Work |

Table S2 Fitting results of N, P-CDs-DOX release at different pH

| pH | Models | Equations | R2 |
| --- | --- | --- | --- |
| 5.0 | Zero Order | F% = 20.4 + 0.838*t | 0.798 |
|  | First order | F% = 55.9*(1 - exp(-0.0980*t)) | 0.984 |
|  | Weibull | F% = 58.8*(1 - exp( -(0.0903*(t-0.5284))^0.801)) | 0.986 |
|  | Higuchi | F% =7.911*(t^0.5)+5.45 | 0.920 |
|  | Ritger-Peppas | F% = 12.6*(t^0.399) | 0.938 |
| 6.5 | Zero Order | F% = 17.0 + 0.553*t | 0.836 |
|  | First order | F% = 40.2*(1 - exp(-0.1081*t)) | 0.964 |
|  | Weibull | F% = 42.17*( 1 - exp( -(0.073*(t+2.36))^0.976) ) | 0.996 |
|  | Higuchi | F% = 5.17*(t^0.5)+7.27 | 0.946 |
|  | Ritger-Peppas | F% = 10.85*(t^0.352) | 0.967 |
| 7.4 | Zero Order | F% = 8.7 + 0.409*t | 0.852 |
|  | First order | F% = 26.87*(1 - exp(-0.0809*t)) | 0.986 |
|  | Weibull | F% = 27.77*( 1 - exp( -(0.0667*(t+1.122))^0.98) ) | 0.992 |
|  | Higuchi | F% =3.81*(t^0.5)+1.61 | 0.953 |
|  | Ritger-peppas | F% =5.21*(t^0.4308) | 0.961 |

Fig. S2 in vitro release models of N, P-CDs-DOX and free DOX at pH=5.0: Zero-order kinetics (A), First-order kinetics, (B) Weibull equation (C), Ritger-Peppas equation (D), Higuchi equation (E)

Table S3 Fitting results of N, P-CDs-DOX and free DOX release at pH=5.0

| Samples | Models | Equations | R2 |  |
| --- | --- | --- | --- | --- |
| Free-DOX | Zero Order | F% = 80.51872+ 1.01046*t |  | 0.73843 |
|  | First order | F% = 94.07092(1 - exp(-1.2026t)) |  | 0.38393 |
|  | Weibull | F% = 103.68512(1- exp(- (0.23931(t +4.51992))0.77006)) |  | 0.95995 |
|  | Higuchi | F% = 6.95497*t^0.5 + 70.71141 |  | 0.88125 |
|  | Ritger-Peppas | F% = 73.9211(t^0.10603) |  | 0.9488 |
| N,P-CDs-DOX | Zero Order | F% = 18.90357 + 0.86885*t |  | 0.80959 |
|  | First order | F% = 56.22266(1 - exp(-0.09382t)) |  | 0.98462 |
|  | Weibull | F% =59.88391(1- exp(- (0.08292(t-0.50357))0.78057)) |  | 0.98725 |
|  | Higuchi | F% = 8.09547*t^0.5 + 3.94474 |  | 0.93081 |
|  | Ritger-Peppas | F% = 11.94393 (t^0.41317) |  | 0.94511 |

Table S4 Release mechanism

Samples Release models n Release mechanism

Free-DOX Weibull 0.10603 Fick

N,P-CDs-DOX Weibull 0.41317 Fick

Reference

Wang, S. C., L. Chen, J. L. Wang, et al., 2020. Enhanced-fluorescent imaging and targeted therapy of liver cancer using highly luminescent carbon dots-conjugated foliate. Materials Science & Engineering C-Materials for Biological Applications. 116,  https://doi.org/10.1016/j.msec.2020.111233

Zhang, M., P. Yuan, N. L. Zhou, et al., 2017. pH-Sensitive N-doped carbon dots-heparin and doxorubicin drug delivery system: preparation and anticancer research. Rsc Advances. 7, 9347-9356. https://doi.org/10.1039/c6ra28345d

Cailotto, S., E. Amadio, M. Facchin, et al., 2018. Carbon Dots from Sugars and Ascorbic Acid: Role of the Precursors on Morphology, Properties, Toxicity, and Drug Uptake. ACS medicinal chemistry letters. 9, 832-837. https://doi.org/10.1021/acsmedchemlett.8b00240

Xue, X., T. Fang, L. Y. Yin, et al., 2018. Multistage delivery of CDs-DOX/ICG-loaded liposome for highly penetration and effective chemo-photothermal combination therapy. Drug delivery. 25, 1826-1839. https://doi.org/10.1080/10717544.2018.1482975

Sun, Y. Q., S. H. Zheng, L. Liu, et al., 2020. The Cost-Effective Preparation of Green Fluorescent Carbon Dots for Bioimaging and Enhanced Intracellular Drug Delivery. Nanoscale Research Letters. 15, https://doi.org/10.1186/s11671-020-3288-0