Supporting Information

Phytogenic fabrication of iron oxide nanoparticles and evaluation of their in vitro antibacterial and cytotoxic activity

Sheik Aliyaa, Muruganantham Rethinasabapathya, Jingon Yooa, Eunsu Kima, Joo-Yoon Chungb, Jong-Ho Chab,c*, Yun Suk Huha*

a NanoBio High-Tech Materials Research Center, Department of Biological Sciences and Bioengineering, Inha University, Incheon, Republic of Korea

b Department of Biomedical Sciences, College of Medicine, Inha University, Incheon, Korea

c Department of Biomedical Science and Engineering, Graduate School, Inha University, Incheon, Korea

*Corresponding author.

E-mail addresses: yunsuk.huh@inha.ac.kr (Y. S. Huh).

: chajongho@inha.ac.kr (J. H. Cha).

Figure S1. Light-brown colored FeCl3 into dark colored Fe3O4 after the addition of N. sativa extract in the presence citric acid stabilizer.

Figure S2. Zeta potential study of IONPs

Figure S2a. Zeta potential study of NS-IONPs synthesized using Nigella sativa.

Figure S3. SEM and EDX analysis of NS-IONPs.

Figure S4. TEM and EDS analysis of NS-IONPs.

Figure S5. Bacterial inhibition assay.

Figure S6. Scanning electron microscopic images of S.typhimurium -  Control and treated with NS-IONPs.

Figure S7. Effect of NS-IONPs on the HCT116 and A549 cancer cell lines. The yellow arrows show cells undergone cell lysis.

Figure S8. Effect of NS-IONPs on the A549 cancer cell line. (a) The yellow arrow shows the accumulation of NS-IONPs in the cytoplasm at 24 h. (b) The red arrow shows cell lysis at 48 h.

Figure S9. EDX analysis of (a) control cells and (b) treated cells.

Figure S10. EDX analysis of E. coli treated with NS-IONPs.

Figure S11. Effect of NS-IONPs in colony formation in HCT116 and A549 cell lines.

Figure S12. Cell cycle effects of NS-IONPs in lung cancer cell lines (A549). a. control without propidium iodide; b and c. effect of 50 µg/mL and 100 µg/mL increase in concentration of the NS-IONPs respectively.

Table S1. Gene specific primers for qRT-PCR analysis.

| ` | Name (Gene Accession #) | ` |
| --- | --- | --- |
| 1 | β-Actin | F: 5'-CCG AGG ACT TTG ATT GCA CAT TG-3' R: 5'-TGG GGT GGC TTT TAG GAT GG-3' |
| 2 | TP53 | F: 5'-GGC CCA CTT CAC CGT ACT AA-3' R: 5'-TGA GGT AGG TGC AAA TGC CA-3' |
| 3 | BCl2 | F: 5'-ATC GCC CTG TGG ATG ACT GA-3' R: 5'-GGG CCG TAC AGT TCC ACA A-3' |
| 4 | BAX | F: 5'-AGC GAC TGA TGT CCC TGT CT-3' R: 5'-CTC CCG CCA CAA AGA TGG TC-3' |