Supplementary Material

The selective and enhanced adsorptive behaviors of supramolecular recrystallized 1,3,5-benzenetricarboxylic acid assembled nano-bacterial cellulose

Zengbei Lia, Xin Huanga, b, c*, Haijuan Dua, b,*, Xinjie Denga, Chaoyang Denga, Shaobo Wanga, b,*, Xianyang Yuea, b, and Xiaozhou Sua, b

a Department of Light Chemical Engineering, College of Textiles, Zhongyuan University of Technology, No. 41 Zhongyuan Road (M), Zhengzhou, Henan Province 450007, China

b Collaborative Innovation Centre of Advanced Textile Equipment and Technology Co-constructed by Ministry of Education and Henan provincial Government, Zhengzhou, Henan Province 451191, China

c Zhengzhou Key Laboratory of Green Dyeing and Finishing Technology, Zhengzhou, Henan Province 451191, China

Correspondence information:

*Xin Huang, Haijuan Du and Shaobo Wang, Department of Light Chemical Engineering, College of Textiles, Zhongyuan University of Technology, No. 41 Zhongyuan Road (M), Zhengzhou, Henan Province 450007, China.

- mail: xinhuang@zut.edu.cn (X. Huang), duhaijuan2009@126.com (H. Du), and shaobowang@zut.edu.cn (S. Wang).

- Tel.: +86-(0)371-6997-5723.

SM-1. Crystal data

Table S1 Crystal data and structure refinement details for RCTMA.

| Item | RCTMA |
| --- | --- |
| formula | C9H6O6 |
| formula weight | 210.14 |
| crystal system space group | Monoclinic C2/c |
| a/Å | 26.5231(3) |
| b/Å | 16.42797(19) |
| c/Å | 26.5471(3) |
| α/deg | 90 |
| /deg | 91.5695(10) |
| γ/deg | 90 |
| vol/Å3 | 11562.8(2) |
| Z | 48 |
| Dc/g·cm-3 | 1.449 |
| µ/mm-1 | 1.095 |
| F(000) | 5184.0 |
| rflns collected | 46211 |
| unique rflns | 11031 |
| GOF | 1.043 |
| R1a (I > 2ó(I)) | 0.0463 |
| wR2a (all data) | 0.1420 |
| Δρmax/Δρmin (e·Å-3) | 0.34/-0.45 |

aR1 = ||Fo| - |Fc||/ |Fo|; wR2 = [ w(Fo2 - Fc2)2/ w(Fo2)2]1/2.

SM-2. Photographs of RCTMA@NBC.

Fig. S1. Photographs of RCTMA@NBC (a) before and (b) after the adsorption of MB dyes.

SM-3. Adsorption thermodynamics analysis of MB.

Fig. S2. (a) Effect of temperature on adsorption amount of MB using RCTMA@NBC and (b) linear relation diagram of lnKC vs. 1/temperature.

Table S2 Thermodynamic parameters of adsorption of MB using RCTMA@NBC.

| ΔH （kJ/mol） | ΔS（kJ/mol/K） | R2 | ΔG （kJ/mol） |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | 298 K | 313 K | 333 K |
| -68.4895 | -0.2055 | 0.9085 | -7.2505 | -4.1680 | -0.0580 |

SM-4. Adsorption isotherms analysis of MB.

Fig. S3. (a) Langmuir, (b) Freundlich, (c) Dubnin-Radushkevich (D-R) and (d) Temkin models of MB dyes adsorption using RCTMA@NBC.

SM-5. Adsorption kinetics analysis.

The adsorption kinetics was analyzed by the pseudo-first-order (Equation S1), pseudo-second-order (Equation S2), and intraparticle diffusion models (Equation S3).

（S1）

（S2）

（S3）

Where qt (mg/g) is the adsorption ability at various time while qe (mg/g) is the equilibrium adsorption capacity. k1 (min-1), k2 (g/mg·min), and ki (mg/g/min1/2)  stand for the first order rate constant, the second order rate constant, and a rate constant of the intraparticle diffusion, respectively. C (mg/g) is a constant. The fitting result was shown in the Fig. S4.

Fig. S4. Langmuir, Freundlich, Dubnin-Radushkevich (D-R) and Temkin models of (a-c) cationic golden XGL and (d-f) brilliant crocein dyes’ adsorption using RCTMA@NBC.