- COx -free H2 Production via Catalytic Decomposition of CH4 over Fe Supported on Tungsten oxide-activated Carbon Catalyst: Effect of Tungsten Loading

Hossein Bayahia1, Anis H. Fakeeha2,3, Salma A. Al-Zahrani4, Salwa B. Alreshaidan5, Abdulrhman S. Al-Awadi2,3, Mohammed F. Alotibi6, Rawesh Kumar7*, Ahmed S. Al-Fatesh2*

1 Chemistry Department, Faculty of Science, Albaha University, Albaha, Saudi Arabia.

2Chemical Engineering Department, College of Engineering, King Saud University, P.O. Box 800, Riyadh 11421, Saudi Arabia.

3King Abdullah City for Atomic & Renewable Energy, Energy Research & Innovation Center (ERIC) in Riyadh, Riyadh 11451, Saudi Arabia.

4Department of Chemistry, College of Sciences, University of Hail, Hail, 2440, Saudi Arabia.

5Department of Chemistry, Faculty of Science, King Saud University, P.O. Box 800, Riyadh 11451, Saudi Arabia.

6Institute of Refining and Petrochemicals Technologies, King Abdulaziz City for Science and Technology (KACST), P.O. Box 6086, Riyadh 11442, Kingdom of Saudi Arabia

7Department of Chemistry, Indus University, Ahmedabad, Gujarat-382115 India.

*Correspondence: aalfatesh@ksu.edu.sa  (A.S.A.-F.), kr.rawesh@gmail.com (R.K); mfalotaibi@ksacst.edu.sa

Table S1. A comparative table of literature report over supported catalyst system towards CH4 decomposition reaction.

| Catalysts | Method | Activity |  |  | Temp (oC) | TOS (minute) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | % |  |  |  |  |
| Ni/Activated carbon | Activated carbon is obtained from coconut shell and then Ni is impregnated over it. | - | 75 | - | 850 | 4h | Sarada Prasad et al., 2011 |
| Ni/Activated carbon | Activated carbon is obtained from coal liquefaction residue then Ni is impregnated over it | - | 60 | - | 850 | 9h | hang et al., 2013 |
| 10Ni/SiO2 | Impregnation | 10 | - | - | 500-800 | 300 | Dong et al., 2015 |
|  | Impregnation | 35 | - | - | 650 | 60 |  |
| 30Ni/SiO2 | Impregnation | 10 | - | - | 600 | 500 | Venugopal et al., 2007 |
| Ni/SiO2 | Impregnation | 30 |  |  | 548 | 130 | Bonura et al., 2006 |
| Ni/MgO | Impregnation | 30 |  |  | 548 | 210 | Bonura et al., 2006 |
| Ni/ZSM-5 Si/Al = 300 | Nano nickel is prepared by sol-gel and then it is impregnated over ZSM-5 | 45 | - | - | 700 | 14 | Michalkiewicz and Majewska, 2014 |
| Ni/LiAlO2 | Impregnation | 27 | - | - | 548 | 60 | Bonura et al., 2006 |
| Ni-MgO solid solution | Hydrothermal | - | - | 45% |  | 3h |  |
| Ni/SiO2.MgO | Co-precipitation | >50 | - | - | 575 | 600 min | Karimi et al., 2021 |
| Ni/Hydrotalcite Ni:Al:La: 2:0.7:0.3 | Co-precipitation | 30 | - | - | 550 | 24h | Anjaneyulu et al., 2015 |
| 65Ni-10Fe-25SiO2 | Heterophase sol-gel method | 20 | - | - | 550 | 440 | Wang et al., 2012 |
| Co-Al | Co-precipitation | 75 |  |  | 750 | - | Zardin and Perez-Lopez, 2017 |
| Co/Al2O3 coated silica | Silica fabric is wash-coated with dispersed alumina and then Co is impregnated over it. | 90 | - | - | 700 | 11.6 h | Italiano et al., 2010 |
| 70Ni-10Cu-10Fe/Al2O3 | Mechanochemical activation of metal oxide mixture |  | 77 hydrogens |  | 700 | 14 | Chesnokov and Chichkan, 2009 |
| 60Fe/Al2O3 | Co-precipitation |  |  | 77 | 700 | 4h | Ibrahim et al., 2015 |
| Fe-Al/Activated carbon Fe/Al = 24/16 | Impregnation | 35 | - | - | 850 | 100h | Jin et al., 2013 |

= Conversion of CH4,   = Mol % of CH4,  = Yield of H2, TOS = Time on Stream, Temp.= Temperature, Ref. = Reference

Fig. S2. N2-adsorption isotherm and porosity distribution profile of (A) 30Fe5W95Ac catalyst (B) 30Fe95W5Ac catalyst

Fig. S3. H2-TPR profile of Fe2O3, 30Fe100Ac, 30Fe5W95Ac, 30Fe10W90Ac and 30Fe25W75Ac

Table S4. H2-consumption per gram catalyst form H2-TPR profile

| Catalyst | Total H2- consumption (cm3/g) |
| --- | --- |
| Fe2O3 | 417.24 |
| 30Fe100Ac | 240 |
| 30Fe5W95Ac | 169.24 |
| 30Fe10W90Ac | 137.44 |
| 30Fe25W75Ac | 183 |
| 30Fe50W50Ac | 174.2 |
| 30Fe90W10Ac | 72.28 |
| 30Fe95W5Ac | 68.24 |
| 30Fe100W | 46.32 |

Table S5. Carbon yield (%) of 30FexW100-xAc  (x = 5, 25, 50, 90, 95) catalyst

| Catalyst | Wp (g) | Wcat (g) | *Carbon yield (%) |
| --- | --- | --- | --- |
| 30Fe5W95Ac | 0.17 | 0.15 | 13.3 |
| 30Fe25W75Ac | 0.36 | 0.15 | 140 |
| 30Fe50W50Ac | 0.31 | 0.15 | 107 |
| 30Fe75W25Ac | 0.16 | 0.15 | 6.7 |
| 30Fe90W10Ac | 0.25 | 0.15 | 66.6 |
| 30Fe95W5Ac | 0.29 | 0.15 | 93.3 |

*Carbon yield (%)= 𝑊𝑝 is the weight of the product after reaction and 𝑊𝑐𝑎𝑡 is the weight of the fresh catalyst.

Fig S6. SEM image of (A) Fresh 30Fe10W90Ac (B) Fresh 30Fe90W10Ac  (C) Spent 30Fe10W90Ac (D) Spent 30Fe90W10Ac