**Self-exothermic reaction assisted green synthesis of carbon dots for the detection of para-nitrophenol and β-glucosidase activity**

Bocong Li, Guoqiang Xiang\*, Gao Huang, Xiuming Jiang, Lijun He

School of Chemistry and Chemical Engineering, Henan University of Technology, Zhengzhou, 450001, P.R. China

\* E-mail: xianggq@haut.edu.cn

1. **Stability of G-CDs**

****

**Fig. S1** Study on the stability of G-CDs. Effect of NaCl concentration on the fluorescence intensity of G-CDs (A), Effect of storage time on the fluorescence intensity of G-CDs (B), Effect of irradiation time on the fluorescence intensity of G-CDs (C).

1. **Comparison of analytical performance**

**Table S1** Analytical performance of fluorescence assays for β-Glu activity based on CDs.

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Carbon source | Methods | Conditions | Linear range(U·L-1) | Detection limit(U·L-1) | Ref |
| 1,2-diaminobenzene, EDA | Solvothermal method | 180 °C, 12 h | 0-250 | 12.3 | (Kong et al., 2020) |
| 1,2-diaminobenzene, EDA | Hydrothermal method | 180 °C, 12 h | 1-60 | 0.3 | (Lu et al., 2016) |
| Hydroquinone,EDA | Hydrothermal method | 180 °C, 12 h | 1-15 | 0.3 | (Gong et al., 2019) |
| Cysteine,CuCl2 | Hydrothermal method | 150 °C, 21 h | 0.5-700 | 0.2 | (Liu et al., 2019) |
| Ganpu tea | Self-exothermic reaction | Room temperature, 5 min | 0.1-20 | 0.074 | This work |

References：

Gong, P., Sun, L., Wang, F., Liu, X., Yan, Z., Wang, M., Zhang, L., Tian, Z., Liu, Z., You, J., 2019. Highly fluorescent N-doped carbon dots with two-photon emission for ultrasensitive detection of tumor marker and visual monitor anticancer drug loading and delivery. Chem Eng J 356, 994–1002. https://doi.org/10.1016/j.cej.2018.09.100

Kong, B., Yang, T., Hou, P., Li, C.H., Zou, H.Y., Huang, C.Z., 2020. Enzyme‐triggered fluorescence turn‐off/turn‐on of carbon dots for monitoring β‐glucosidase and its inhibitor in living cells. Luminescence 35, 222–230. https://doi.org/10.1002/bio.3717

Liu, Z., Tian, Y., Han, Y., Bai, E., Li, Y., Xu, Z., Liu, S., 2019. A “turn off-on” fluorescent nanoprobe consisting of CuInS2 quantum dots for determination of the activity of β-glucosidase and for inhibitor screening. Microchim Acta 186, 806. https://doi.org/10.1007/s00604-019-3918-3

Lu, S., Li, G., Lv, Z., Qiu, N., Kong, W., Gong, P., Chen, G., Xia, L., Guo, X., You, J., Wu, Y., 2016. Facile and ultrasensitive fluorescence sensor platform for tumor invasive biomaker β-glucuronidase detection and inhibitor evaluation with carbon quantum dots based on inner-filter effect. Biosens Bioelectron 85, 358–362. https://doi.org/10.1016/j.bios.2016.05.021