Supplementary Information

Acid assisted-hydrothermal carbonization of solid waste from essential oils industry: optimization using I-optimal experimental design and removal dye application

Faiçal El Ouadrhiri1*, Ebraheem Abdu Musad Saleh2, Kakul Husain2, Abderrazzak Adachi1, Anouar Hmamou1, Ismail Hassan2, Marwa Mostafa Moharam2,3, Amal Lahkimi1

1 Laboratory of Engineering, Molecular Organometallic Materials and Environment, Faculty of Sciences Dhar El Mehraz, Sidi Mohamed Ben Abdellah University, Fez, Morocco.

2 Chemistry Department, College of Arts & Science, Prince Sattam Bin Abdulaziz University, Wadi Al-Dawaser, Alkharj, Saudi Arabia.

3 Chemical and Electrochemical Processing Department, Central Metallurgical Research and Development Institute (CMRDI), P.O. Box 87, Helwan 11421, Egypt.    *Corresponding author Email: Faical.elouadrhiri@usmba.ac.ma

MATERIAL AND METHOD:

Optimal design of experimental

Tableau S1 : Facteur de severite en fonction de la temperature et le temps

| Niveau | 1 | 2 | 3 | 4 | 5 | 6 |
| --- | --- | --- | --- | --- | --- | --- |
| HTCT (°C) | 180 | 195 | 210 | 210 | 210 | 210 |
| HTCt (min) | 180 | 180 | 180 | 60 | 120 | 240 |
| SF | 4.61 | 5.05 | 5.49 | 5.02 | 5.32 | 5.62 |

Adsorption study

Table S2:isotherm and kinetic equations used in the adsorption of HCop and AHCop

| Utility | Equation | reference |
| --- | --- | --- |
| Pseudo-First Order | ln⁡(Qe-Qt) = ln (Qe) - K1.t | [1] |
| Pseudo-Second Order | t.Qt = tQe+1K2.Qe2 | [2] |
| Modele de Langmuir | 1Qe=1KLQmax.Ce+1Qmax | [3] |
| Modele de Freundlich | ln (Qe)= 1nFln(Ce)+ln(KF) | [4] |
| Arrhenius équation | Ln(K)=Ln(A) - EaRT | [5] |

C0 (mg.L-1) and Ce,t (mg.L-1) are the initial and equilibrium concentrations respectively. m (g) is the mass of carbocatalyst V (L) is the volume of Dye. Qe is the equilibrium quantity. KL (L.mg-1) is a direct measure of the adsorption intensity.Qmax is the maximum adsorption capacity. KF ((mg.g-1)(L.mg-1)1/n) is the adsorption capacity. (1/nF): is the intensity of adsorption for 1/nF=0 irreversible, 1/nF>1 unfavorable and for 0<1/nF<1 the adsorption is favorable.

RESULT AND DISCUSSION:

Numerical Optimization of MY and CRR model

Table S3 : Optimization constraints for factors and responses

| Name | Goal | Importance | Graph |
| --- | --- | --- | --- |
| X1 : HTCcat | minimize | 3 |  |
| X2 : SF | minimize | 1 |  |
| MY (%) | None | 1 |  |
| CRR (%) | maximize | 3 |  |

Figure S1 : (a) bar histogram (b) graphical representation of the desirability function for the optimal solution (D=0,739).

Figure S2 : N2 Adsorption-desorption and PSD profil of HCop

Table S4:  Maximum adsorption capacity of MB dye by various low-cost adsorbents.

| Adsorbent | SBET (m2.g-1) | Qm (mg.g-1) | reference |
| --- | --- | --- | --- |
| Activated-hydrochar from surgane bagasse | 15.34 | 357.14 | [6] |
| Treated sugarcane bagasse | 1.018 | 58.9 | [7] |
| Activated hydrochar from loblolly pine | 1703 | 719.4 | [8] |
| Hydrochar from orange peel | 46.16 | 66.23 | [9] |
| Hydrochar from orange peel | 34.08 | 36.63 |  |
| Activated-hydrochar from solid waste (essential oil industry) | 989.81 | 588.24 | This study |

REFERENCE

[1]	Y. S. Ho and G. McKay, “Pseudo-second order model for sorption processes,” Process Biochem., vol. 34, no. 5, pp. 451–465, Jul. 1999, doi: 10.1016/S0032-9592(98)00112-5.

[2]	J. P. Simonin, “On the comparison of pseudo-first order and pseudo-second order rate laws in the modeling of adsorption kinetics,” Chem. Eng. J., vol. 300, pp. 254–263, 2016, doi: 10.1016/j.cej.2016.04.079.

[3]	I. Langmuir, “The constitution and fundamental properties of solids and liquids. Part I. Solids,” J. Am. Chem. Soc., vol. 38, no. 11, pp. 2221–2295, Nov. 1916, doi: 10.1021/ja02268a002.

[4]	L. Liu, X. B. Luo, L. Ding, and S. L. Luo, “Application of Nanotechnology in the Removal of Heavy Metal From Water,” Nanomater. Remov. Pollut. Resour. Reutil., pp. 83–147, Jan. 2019, doi: 10.1016/B978-0-12-814837-2.00004-4.

[5]	R. Tomer and P. Biswas, “Dehydration of glucose/fructose to 5-hydroxymethylfurfural (5-HMF) over an easily recyclable sulfated titania (SO42-/TiO2) catalyst,” New J. Chem., vol. 44, no. 47, pp. 20734–20750, Dec. 2020, doi: 10.1039/d0nj04151c.

[6]	F. Zhou et al., “Efficient removal of methylene blue by activated hydrochar prepared by hydrothermal carbonization and NaOH activation of sugarcane bagasse and phosphoric acid,” RSC Adv., vol. 12, no. 3, pp. 1885–1896, Jan. 2022, doi: 10.1039/d1ra08325b.

[7]	A. salah omer et al., “Adsorption of crystal violet and methylene blue dyes using a cellulose-based adsorbent from sugercane bagasse: characterization, kinetic and isotherm studies,” J. Mater. Res. Technol., vol. 19, pp. 3241–3254, Jul. 2022, doi: 10.1016/j.jmrt.2022.06.045.

[8]	A. I. Sultana, C. Chambers, M. M. N. Ahmed, P. Pathirathna, and T. Reza, “Multifunctional Loblolly Pine-Derived Superactivated Hydrochar: Effect of Hydrothermal Carbonization on Hydrogen and Electron Storage with Carbon Dioxide and Dye Removal,” Nanomaterials, vol. 12, no. 20, p. 3575, Oct. 2022, doi: 10.3390/nano12203575.

[9]	N. Saha, M. Volpe, L. Fiori, R. Volpe, A. Messineo, and M. T. Reza, “Cationic Dye Adsorption on Hydrochars of Winery and Citrus Juice Industries Residues: Performance, Mechanism, and Thermodynamics,” Energies, vol. 13, no. 18, p. 4686, 2020, doi: 10.3390/en13184686.