Influence of pore structural properties in Metal-Organic Frameworks on the Host-Guest Interaction in drug Delivery

Xiao-Wei Yan a†, Somayeh Tarasi b†, Su-Juan Wang a†, Kobra Rostamizadeh d, Mao-Lin Hu*c, Ali Morsali*b, Ali Ramazani*e ,f, Roghayeh Tarasi g, Yavar Ahmadih

a Guangxi Key Laboratory of Health Care Food Science and Technology, College of Food and Bioengineering, Hezhou University, No. 18 West Ring Road, Hezhou, Guangxi 542899, P.R. China

b Department of Chemistry, Faculty of Sciences, Tarbiat Modares University, P.O. Box: 14115-175, Tehran, Iran. E-mail:     Morsali_a@modares.ac.ir

c College of Chemistry and Materials Engineering, Wenzhou University, Wenzhou 325035, China. E-mail: 00111024@wzu.edu.cn

d  Zanjan Pharmaceutical Nanotechnology Research Center, Zanjan University of Medical Sciences, Zanjan, Iran.

e Department of Chemistry, Faculty of Science, University of Zanjan, Zanjan 45371-38791, Iran.

f Department of Biotechnology, Research Institute of Modern Biological Techniques (RIMBT), University of Zanjan, Zanjan 45371-38791, Iran. E-mail: aliramazani@gmail.com; aliramazani@znu.ac.ir

g Department of Pharmacology, School of Medicine, Shahid Beheshti University of Medical Sciences, Tehran, Iran.                         h Department of Basic Sciences, Farhangian University, Tehran 1939614464, Iran.

Methods

In vitro cytotoxicity assay. To evaluate the in vitro cytotoxicity of the synthesized MOFs on the growth of cancer cells, MTT [3-(4, 5-dimethylthiazol-2-yl)-2, 5-diphenyl tetrazolium bromide] assay against the HT-29 cell line was used. The cells were grown into 24-well plates (5 × 104 cells/well) containing RPMI (Roswell Park Memorial Institute, 1000 µL) culture medium and incubated in a humidified atmosphere of  CO2 (5%) for 24h at 37 °C. Then, the cells were exposed to different concentrations of MOFs@Curcumin (100, 200 and 500 µg/µL) and curcumin (250, and 500 µg / µL in 0.1% DMSO) for 24h at 37 °C under 5% CO2. At this concentration, DMSO showed no significant cytotoxic effect on HT-29. The medium without any MOFs@Curcumin and curcumin was used as the control group. Then, 20 µL MTT labeling reagent (5 mg/mL PBS) was added to each well. After further incubation for 4h at 37 °C, the cell culture medium was removed and DMSO (1 mL) was added to each well and the plates were agitated for 1 min to solubilize the formazan crystals, formed during the MTT test. The optical density (OD) of each well was measured by a plate reader. The survival rate was determined according to the following equation:

Viable rate %=( OD (treated))/ (OD (control)) ×100

Where OD (treated) and OD (control) are absorbance of the cells in the treated group with MOFs and absorbance of the cells in the absence of MOFs, respectively.

Activation Method. For the purpose of activation and to removing DMF molecules, synthesized crystals were then soaked in 5 mL of CH3CN solvent for 5 days, with fresh CH3CN added every 24 h. After 5 days, the CH3CN solution was decanted, and crystals were dried at 120 °C under vacuum for at least 24 h and crystals activated were obtained.

Figure S1. Solid state

Figure S1. UV-vis spectroscopy of (a) TMU-6(RL1), (b) TMU-6(RL1) and (c) TMU-59

Figure S2. Thermogravimetric analysis of TMU-6(RL1) and TMU-21(RL2)

Figure S3. Thermogravimetric analysis of TMU-59

Figure S4. FE-SEM images of TMU-59 (a,b), TMU-6(RL1) (c,d) and TMU-21(RL2) (e,f) as-synthesized particles (a) Adsorption (b)

Figure S5.Fluorescence emission spectra and Stern -Volmer (SV) plots of TMU-21(RL2) dispersed in water solution at different concentrations of Curcumin.

Figure S6.Fluorescence emission spectra and Stern -Volmer (SV) plots of TMU-6(RL1) dispersed in water solution at different concentrations of Curcumin.

Figure S7.Fluorescence emission spectra and Stern -Volmer (SV) plots of TMU-59 dispersed in water solution at different concentrations of Curcumin.

| Table S1. Comparison of Contact angle, DLE, DLC, KSV and Detection Limit MOFs for C curcumin |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Contact angle of MOFs | Contact angl (MOFs@Curcumin) | Drug loading encapsulation efficiency (DLE) | Drug loading capability (DLC) | KSV (M-1) | Detection Limit |
| TMU-6(RL1) | 590 | 1080 | 18% | 78% | 42958 | 38nM |
| TMU-21(RL2) | 710 | 1060 | 20% | 70% | 1×106 | 3.6nM |
| TMU-59 | 890 | 990 | 3.6% | 13.6% | 8740 | 375nM |
| Curcumin | 1260 | - | - | - | - | - |

a

b

a

c

Figure S8. UV-vis spectra of Curcumin in the presence of (a) TMU-6(RL1), (b) TMU-21(RL2) and (c) TMU-59

c

b

a

e

d

Figure S9. (a) XPS survey spectrum and high resolution XPS spectra of (b) Zn 2p (c) C 1s, (d) O 1S, and (e) N 1S of TMU-6(RL1), respectively.

c

b

a

e

d

Figure S10. (a) XPS survey spectrum and high resolution XPS spectra of (b) Zn 2p (c) C 1s, (d) O 1S, and (e) N 1S of TMU-59, respectively.

TMU-59@Curcumin

TMU-21(RL2)@Curcumin

TMU-6(RL1)@Curcumin

3

2

1

Curcumin

Figure S11. Contact angles of TMU-6(RL1)@Curcumin, TMU-21(RL2)@Curcumin, TMU-59@Curcumin and Curcumin