Supplementary Material

Study of the activity and stability of sulfonated carbon catalyst from agroindustrial waste in biodiesel production: Influence of pyrolysis temperature on functionalization

Ana Paula da Luz Corrêaa, Paula Maria Melo da Silvaa, Matheus Arrais Gonçalvesa, Rafael Roberto Cardoso Bastosa, Geraldo Narciso da Rocha Filhoa, Leyvison Rafael Vieira da Conceiçãoa*.

a Federal University of Pará, Institute of Exact and Natural Sciences, Graduate in Chemistry Program, Laboratory of Catalysis and Oleochemical, 66075–110, Belém, Pará, Brazil.

*Corresponding author. Tel.: +55 91 98102 1185.

E-mail address: rafaelvieira@ufpa.br (Leyvison Rafael Vieira da Conceição).

Table S1 ― Raman analysis for biochars and catalysts: intensity of D and G bands.

| Sample | ID (u. a.) | IG (u. a.) | ID/IG |
| --- | --- | --- | --- |
| BC450 | 260.04 | 491.67 | 0.53 |
| BC600 | 167.62 | 291.41 | 0.57 |
| BC750 | 50.69 | 69.87 | 0.73 |
| BC450-S | 127.16 | 207.97 | 0.61 |
| BC600-S | 9.39 | 15.62 | 0.60 |
| BC750-S | 39.44 | 51.17 | 0.77 |

Figure S1 ― TG/DTG plots for the catalysts after reuse: (a) BC450-S, (b) BC600-S and (c) BC750-S.

Figure S2 ― Graphical analysis of the effects of temperature and time variables in the first reaction cycle of the catalysts: Percentage of effects in (a), (c) and (e), and Probability graph in (b), (d) and (f).

Figure S3 ― Graphical analysis of the effects of the temperature and time variables in the second reaction cycle of the catalysts: Percentage of effects in (a), (c) and (e) and Probability graph in (b), (d) and (f).