Supporting material

Corrosion inhibition properties of spinach extract on carbon steel in a hydrochloric acid medium

Fig.S1 Plots of ( a) Arrhenius plots and (b) transition-state plots for Q235 steel dissolution reaction in a 0.5M of hydrochloric acid with and without AESPE

Fig. S2 Langmuir isotherm for AESPE adsorption of Q235 steel in a 0.5M of hydrochloric acid

Fig.S3 Plot of lnKads versus T-1 for adsorption of AESPE of Q235 Steel in a 0.5M of hydrochloric acid

Fig. S4 Temkin isotherm for AESPE adsorption of Q235 steel in a 0.5M of hydrochloric acid

Figure S5 Equivalent circuit

(a)

(c)

(b)

Figure S6 contact angle on the Q235 steel surface

（a）The newly uncorroded sample (102°)，（b）The sample in the 0.5M of hydrochloric acid (65°)，（c）The sample in the 0.5M of hydrochloric acid with AESPE (94°)

HOMO

LUMO

Fig. S7 HOMO and LUMO orbitals of chlorophyll