Fabrication of BN/CuO@MWCNTs composites for enhancing heat transfer and photothermal conversion of phase change materials

Weifang Han a,, Deyi Liu a, Guoliang Wang a, Suliang Li b, En You b, Zhengfeng Jia a, Yuchao Li a

a School of Materials Science and Engineering, Liaocheng University, Liaocheng, 252059, China

b Zhejiang Construction Engineering Co., Ltd. of China Construction Eighth Engineering Division, Zhejiang, 311215, China

E-mail: hanweifang@lcu.edu.cn (W. Han); liyuchao@lcu.edu.cn (Y. Li)

Table S1. The amount of raw material used for the preparation of BN@CuO hybrids.

| Material Type | Boric acid (H3BO3) | Melamine (C3N6H6) | CuSO4 | aRB/Cu |
| --- | --- | --- | --- | --- |
| BN/CuO | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.010 mol (1.60g) | 10.0 |
|  | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.015 mol (2.40 g) | 6.7 |
|  | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.020 mol (3.20 g) | 5.0 |
|  | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.025mol (4.00 g) | 4.0 |
|  | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.030 mol (4.80g) | 3.3 |

aRB/Cu: Molar ratio of H3BO3 to CuSO4.

Table S2. The amount of raw material used for the preparation of BN/CuO@MWCNTs composite.

| Material Type | Boric acid (H3BO3) | Melamine (C3N6H6) | CuSO4 | MWCNTs | PVP |  |
| --- | --- | --- | --- | --- | --- | --- |
| BN/CuO@MWCNTs | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.005 mol (0.80g) | 0.01mol (0.12 g) | 1 g |  |
|  | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.01 mol (1.60 g) | 0.05 mol (0.6 g) | 1 g |  |
|  | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.02 mol (3.20 g) | 0.1 mol (1.2 g) | 1 g |  |
|  | 0.1 mol (6.1830 g) | 0.05 mol (6.3060 g) | 0.03 mol (4.79 g) | 0.15 mol (1.8 g) | 1 g |  |

Fig. S1. SEM images of the BN/CuO hybrids prepared at different RB/Cu: (a) 10.0, (b) 6.7, (c) 4.0, (d) 3.3.

Fig. S2. Elemental mapping images of BN/CuO hybrid: (b) B, (c) N, (d) C, (e) Cu and (f) O elements.

Fig. S3. XPS analysis of hybrid. (a) Survey spectrum, (B) high-resolution spectrum of (b) B 1s, (c) Cu 2p and (d) C 1s (e) N 1s (f) O 1s.

Fig. S4. XRD pattern of CuO

Fig. S4. SEM images of the BN/CuO/MWCNTs composites prepared at RB/Cu=3.6 and different amount of MWCNTs: (a) 0.01mol, (b) 0.50 mol and (c) 0.15 mol.

Fig. S5. XRD pattern of CuO

Fig. S6. Devices for testing the heat transfer performance

Fig. S7. Nitrogen adsorption/desorption isotherms of BN, BN/CuO hybrid and BN/CuO@MWCNTs composite

Fig. S8. UV–vis–NIR spectra absorption spectra

Table S3. Thermophysical properties of PEG and PEG-based composite PCMs.

| Sample | ΔΗm (J/g) | Tm (°C) | ΔΗc (J/g) | Tc (°C) |
| --- | --- | --- | --- | --- |
| PEG | 172.3 | 58.6 | 169.4 | 38.4 |
| PEG/BN | 153.1 | 58.1 | 151.8 | 40.0 |
| PEG/BN/CuO | 153.4 | 57.5 | 152.3 | 41.7 |
| PEG/BN/CuO@MWCNTs | 154.5 | 56.4 | 153.2 | 43.8 |

Table S4. Solar-thermal conversion efficiencies data of the PEG/BN/CuO and PEG/BN/CuO@MWCNTs composites.

|  | PEG/BN/CuO | PEG/BN/CuO@MWCNTs |
| --- | --- | --- |
| m (g) | 0.10 | 0.10 |
| P (mW/cm2) | 100 | 100 |
| s (cm2) | 1.16 | 1.16 |
| Δt (s) | 174.54 | 144.40 |
| Input energy a (J) | 20.25 | 16.75 |
| Thermal energy storage b (J) | 15.34 | 15.45 |
| η (%) | 75.8 | 92.2 |

a Input energy= P×s×Δt

b Thermal energy storage = m×ΔHm

Table S5. The comparison of heat transfer and photothermal conversion between this work and some previously reported PEG-based PCMs.

| Composite PCMs | Filler | TC (W/m·K) | η (%) | Ref. |
| --- | --- | --- | --- | --- |
| PEG/GNPs | 4 | 3.11 | 86 | 2018[1] |
| PEG/Ti3C2Tx | 20 w% | 0.293 | 94.5% | 2019[2] |
| RHTC/PEG | 7 | 0.51 | 90.1 | 2021[3] |
| Ti3C2Tx@PVA/PEG | 7.68 | 0.428 | 96.5 | 2021[4] |
| B-GAPCM | --- | 1.07 | 89.3 | 2021[5] |
| CF/(HO-BNNS@CuO)/PEG | 10 wt% | 1.12 | 91.8 | 2022[6] |
| PAAAM/RHTC/PEG |  | 0.76 | 93.3 | 2022[7] |
| PI/PR Aerogel/PEG | 16 | 0.3469 | 82.5 | 2022[8] |
| FCPCMs | 40 | 1.733 | 95 | 2022[9] |
| PU/GO/PEG | 11 | 0.972 | 95.3 | 2022[10] |
| MXene@PVP/PEG | 10 | 0.533 | 96.2 | 2023[11] |
| PVDF/RB/PEG | 9.1 | 1.01 | 92.1 | 2024[12] |
| PEG@PFCC | --- | 1.61 | 91.5 | 2024[13] |
| BCNSs/PEG | 14.3 | 0.635 | 80.2 | 2024[14] |
| PEG/CPAC | 3.9 | 0.61 | 94.6 | 2024[15] |
| CuO@PEG | 20 | 0.52 | 91.6 | 2024[16] |
| MPC@PEG |  | 0.96 | 90.8 | 2024[17] |
| PEG/BN/CuO@MWCNTs | 10 | 2.35 | 92.2 | This work |

Reference

[1] T. Qian, S. Zhu, H. Wang, A. Li, B. Fan, Comparative study of single-walled carbon nanotubes and graphene nanoplatelets for improving the thermal conductivity and solar-to-light conversion of PEG-infiltrated phase-change material composites, ACS Sustainable Chem. Eng., 7 (2019) 2446-2458.

[2] X. Fan, L. Liu, X. Jin, W. Wang, S. Zhang, B. Tang, MXene Ti3C2Tx for phase change composite with superior photothermal storage capability, J. Mater. Chem. A, 7 (2019) 14319-14327.

[3] H. Yang, Y. Bai, C. Ge, S. Li, X. Zhang, High Thermal Conductivity of Carboxyl-rich Carbon/Polyethylene Glycol Composites for Enhanced Photothermal Conversion and Latent Heat Storage, Chin. J. Chem., 39 (2021) 3245-3254.

[4] Z. Mo, P. Mo, M. Yi, Z. Hu, G. Tan, M.S. Selim, Y. Chen, X. Chen, Z. Hao, X. Wei, Ti3C2Tx@Polyvinyl alcohol foam-Supported Phase Change Materials with Simultaneous Enhanced Thermal Conductivity and Solar-Thermal Conversion Performance, Sol. Energy Mater. Sol. Cells, 219 (2021) 110813.

[5] Z. Bao, N. Bing, H. Yao, Y. Zhang, H. Xie, W. Yu, Three-dimensional interpenetrating network phase-change composites with high photothermal conversion and rapid heat storage and release, ACS Appl. Energy Mater., 4 (2021) 7710-7720.

[6] H. Yang, L. He, R. Liu, C. Ge, C. Ma, X. Zhang, Ultralight and flexible carbon-based phase change composites with high porosity for enhanced shape memory and photothermal conversion performance, Sol. Energy Mater. Sol. Cells, 244 (2022) 111816.

[7] H. Yang, Y. Bai, C. Ge, L. He, W. Liang, X. Zhang, Polyethylene glycol-based phase change materials with high photothermal conversion efficiency and shape stability in an aqueous environment for solar water heater, Compos. Part A, 154 (2022) 106778.

[8] Z. Zheng, T. Shi, H. Liu, D. Wu, X. Wang, Polyimide/phosphorene hybrid aerogel-based composite phase change materials for high-efficient solar energy capture and photothermal conversion, Appl. Therm. Eng., 207 (2022) 118173.

[9] J. Chen, Z. Mo, Y. Chen, P. Mo, Z. Hu, X. Chen, J. Yu, Z. Hao, X. Zeng, R. Sun, J. Xu, Highly Stable MXene-Based Phase Change Composites with Enhanced Thermal Conductivity and Photothermal Storage Capability, ACS Appl. Energy Mater., 5 (2022) 11669-11683.

[10] J. Wang, Z. Wu, H. Xie, T. Wang, Y. Wang, Y. Huang, L. Dong, Graphene oxide/polyurethane-based composite solid–solid phase change materials with enhanced energy storage capacity and photothermal performance, Int. J. Energy Res., 46 (2022) 22744-22756.

[11] Y. Chen, J. Chen, Z. Hao, M.S. Selim, J. Yu, X. Chen, Polyvinylpyrrolidone-bridged MXene skeleton constructed by photothermal assisted sacrificial template method for phase change materials with form stability and photothermal conversion, Chem. Eng. J., 463 (2023) 142375.

[12] H. Yang, M. Si, Y. guo, C. Ge, L. He, X. Zhang, RHTC/HO-BNNS structure collaboratively improves thermal conductivity and photothermal conversion properties of phase change materials, Sol. Energy Mater. Sol. Cells, 268 (2024) 112746.

[13] L. Wang, M. Zhou, H. Fu, An in-situ growth Fe3O4 and polyaniline on carbon cloth encapsulated composite phase change materials with high thermal conductivity and photothermal energy conversion and storage, J. Energy Storage, 78 (2024) 110090.

[14] J. Zhang, Z. Zheng, L. Xu, H. Xie, Z. Fei, P.J. Dyson, N. Yan, Light- and electro-driven phase change materials derived from activated porous biochar nanosheets and encapsulated polyethylene glycol, Colloids Surf., A, 690 (2024) 133783.

[15] Y. Liu, Y. Liu, W. Chen, X. Hu, Y. He, Y. Ma, Y. Xie, W. Luo, L. Luo, L. Jiang, X. Jiang, Q. Li, Polyethylene glycol/melamine foam composite phase change materials modified by CdS/Ag exhibits high photothermal conversion performance, Desalination, 585 (2024) 117783.

[16] H. Pang, G. Li, L. Cheng, C. He, X. Wang, X. Zhang, 3D flower-like CuO@PEG composite phase change materials with photo response for applications in energy conversion and storage, J. Energy Storage, 82 (2024) 110537.

[17] S. Wang, Q. Huang, Z. Sun, Y. Wang, T. Liang, B. Wang, C. Fan, C. Liu, Porous carbon network-based composite phase change materials with heat storage capacity and thermal management functions, Carbon, 226 (2024) 119174.