Bimetallic FeCo metal-organic framework based cascade reaction system: Enhanced peroxidase activity for antibacterial performance

Siyuan Zhanga,#, Wenbo Wua,#, Ya Lia, Dongxin Wanga,b, Xiangjun Lic, Jisheng Nie*,a,b, Hong Cui*,a,b

a School of Public Health, Shanxi Medical University, 56 Xinjian South Road, Taiyuan, 030001, China

b MOE Key Laboratory of Coal Environmental Pathogenicity and Prevention, Shanxi Medical University, 56 Xinjian South Road, Taiyuan, 030001, China

c School of Chemical Sciences, University of Chinese Academy of Sciences, 19A Yuquan Road, Beijing, 100049, China

Fig. S1 XPS spectrum of Fe4CoMOF and Fe4CoMOF + H2O2.

Table S1 The kinetic constants of different MOF-based nanozymes using H2O2 as substrate.

| Catalyst | Km [mM] | Vmax [10-7 M·s−1] | Ref. |
| --- | --- | --- | --- |
| MOF (Co/2Fe) | 4.22 | 0.491 | Yang et al., 2017 |
| MOF-919 (Fe-Cu) | 1.36 | 1.462 | Kulandaivel et al., 2022 |
| FeMOF | 1.3 | 0.25 | Xu et al., 2019 |
| 2D Co-MOF | 0.24 | 5.01 | Wan et al., 2021 |
| Fe3NiMOF | 0.1128 | 1.4986 | Mu et al., 2022 |
| MIL-88B-Fe/Zn | 4.7 | 0.92 | Shi et al., 2023 |
| Fe4CoMOF | 1.78 | 1.01 | This work |

Fig. S2 SEM images of (a) Fe4CoMOF; (b) Fe4CoMOF + H2O2. (c) XRD patterns of Fe4CoMOF, Fe4CoMOF + H2O2. (d) FTIR spectra of Fe4CoMOF, Fe4CoMOF and H2O2.

Fig. S3 Stability of Fe4CoMOF for catalytic H2O2.

Fig. S4 Detection of GSH depletion by Fe4CoMOF represented by the absorbance of TNB-.

Fig. S5 (a) Zeta potential of Fe4CoMOF and GOx with different mass ratios. (b) XRD patterns of Fe4CoMOF and GOx with different mass ratios.

Fig. S6 Effect of different mass ratios of Fe4CoMOF and GOx on the catalytic performance of Fe4CoMOF/GOx in the presence of Glu.

Fig. S7 Stability of Fe4CoMOF/GOx for catalytic Glu.

Fig. S8 Solid agar plate photographs (a) and photographs (b) of Fe4CoMOF/GOx + Glu system after different incubation time in the presence of methyl red: (1) Control; (2) 1 h; (3) 2 h; (4) 3 h; (5) 4 h; (6) 5 h. (c) The survival rate of E. coli treated with control group and Fe4CoMOF/GOx + Glu system after different incubation time.

Fig. S9 Cell viability of L929 cells treated with different concentrations of Fe4CoMOF.

Fig. S10 Quantitative analysis of the expression levels of IL-6 and TNF-α.

References

- Kulandaivel, S., Lin, C.H., Yeh, Y.C., 2022. The bi-metallic MOF-919 (Fe-Cu) nanozyme capable of bifunctional enzyme-mimicking catalytic activity. Chem. Commun. 58, 569-572. https://doi.org/10.1039/D1CC05908D.

- Mu, Z., Wu, S., Guo, J.J., et al., 2022. Dual mechanism enhanced peroxidase-like activity of Iron-nickel bimetal-organic framework nanozyme and its application for biosensing. ACS Sustainable Chem. Eng. 10, 2984-2993. https://doi.org/10.1021/acssuschemeng.1c07975.

- Shi, Q.Y., Zhao,Y., Liu, M.H., et al., 2023. Engineering platelet membrane-coated bimetallic MOFs as biodegradable nanozymes for efficient antibacterial therapy. Small, 2309366.  https://doi.org/10.1002/smll.202309366.

- Wan, H.M., Wang, Y.F., Chen, J., et al., 2021. 2D CoMOF nanosheet-based nanozyme with ultrahigh peroxidase catalytic activity for detection of biomolecules in human serum samples. Microchim. Acta. 188, 130. https://doi.org/10.1007/s00604-021-04785-2.

- Xu, W.Q., Jiao, L., Yan, H.Y., et al., 2019. Glucose oxidase-integrated metal-organic framework hybrids as biomimetic cascade nanozymes for ultrasensitive glucose biosensing. ACS Appl. Mater. Inter. 11, 22096-22101. https://doi.org/10.1021/acsami.9b03004.

- Yang, H.G, Yang, R.T., Zhang, P., et al., 2017. A bimetallic (Co/2Fe) metalorganic framework with oxidase and peroxidase mimicking activity for colorimetric detection of hydrogen peroxide. Microchim. Acta. 184,4629-4635. https://doi.org/10.1007/s00604-017-2509-4.

* Corresponding authors. E-mail addresses: niejisheng@sxmu.edu.cn (J.S.N.), cuihong19872007@126.com (H.C.).

# co-first authors