Development in Gelatin-matrix Composite Films: The Incorporation of Vitamin C Adducts Enhances the Optical Behaviors of Gelatin Films.

Azhin Ayad Shamsallaha, Srood Omer Rashida*

a Department of Chemistry, College of Science, University of Sulaimani, Sulaimani, Kurdistan Regional Government, Iraq

* Corresponding author: Department of Chemistry, College of Science, University of Sulaimani, Sulaimani, Kurdistan Region, Iraq.             E-mail address: srood.rashid@univsul.edu.iq (S. Omer Rashid).

Figure S1 Photos of the pure gelatins utilized in this study. These gelatins were sourced from Mr. P Ingredients.

| Table S1 | Composite film thickness, appearance, and optical properties |  |  |  |
| --- | --- | --- | --- | --- |
| Films | Film thickness | appearance | Refractive index (n) | Optical band gaps (Eg) |
| CG | 0.135 |  | 1.16 | 4.9 |
| PG | 0.065 |  | 1.15 | 4.9 |
| BG | 0.045 |  | 1.16 | 4.8 |
| FG | 0.090 |  | 1.16 | 4.9 |

| Table S2 | Composite film thickness, appearance, and optical properties |  |  |  |
| --- | --- | --- | --- | --- |
| Films | Film thickness | Appearance | Refractive index (n) | Optical band gaps (Eg) |
| VC-3a@CG | 0.058 |  | 1.18 | 3.6 |
| VC-3a@PG | 0.063 |  | 1.17 | 3.7 |
| VC-3a@BG | 0.050 |  | 1.17 | 3.6 |
| VC-3a@FG | 0.070 |  | 1.17 | 3.6 |
| VC-3b@CG | 0.068 |  | 1.3 | 3.4 |
| VC-3b@PG | 0.063 |  | 1.28 | 3.5 |
| VC-3b@BG | 0.067 |  | 1.32 | 3.7 |
| VC-3b@FG | 0.099 |  | 1.28 | 3.7 |

Figure S1 1H NMR and 13C NMR spectra of 3a.

Figure S2 1H NMR and 13C NMR spectra of 3b.

Figure S3 FTIR spectra of a dopant vitamin C adducts 3a and 3b.

Figure S4 FTIR spectrum of CG and their composite polymers (VC-3a@CG & VC-3b@CG).

Figure S5 FTIR spectrum of PG and their composite polymers (VC-3a@PG & VC-3b@PG).

Figure S6 FTIR spectrum of BG and their composite polymers (VC-3a@BG & VC-3b@BG).

Figure S7 FTIR spectrum of FG and their composite polymers (VC-3a@FG & VC-3b@FG).

Figure S8 XRD pattern of pure chicken gelatin and doped polymers (VC-3a@CG and VC-3b@CG).

Figure S9 XRD pattern of pure porcine gelatin and doped polymers (VC-3a@PG and VC-3b@PG).

Figure S10 XRD pattern of pure bovine gelatin and doped polymers (VC-3a@BG and VC-3b@BG).

Figure S11 XRD pattern of pure fish gelatin and doped polymers (VC-3a@FG and VC-3b@FG).

Figure S12 Absorption spectra of pure chicken gelatin and composite films (VC-3a@CG and VC-3b@CG).

Figure S13 Absorption spectra of pure porcine gelatin and composite films (VC-3a@PG and VC-3b@PG).

Figure S14 Absorption spectra of pure bovine gelatin and composite films (VC-3a@BG and VC-3b@BG).

Figure S15 Absorption spectra of pure fish gelatin and composite films (VC-3a@FG and VC-3b@FG).

Figure S16 Refractive index (n) of pure chicken gelatin and composite films (VC-3a@CG and VC-3b@CG).

Figure S17 Refractive index (n) of pure porcine gelatin and composite films (VC-3a@PG and VC-3b@PG)

Figure S18 Refractive index (n) of pure bovine gelatin and composite films (VC-3a@BG and VC-3b@BG).

Figure S19 Refractive index (n) of pure fish gelatin and composite films (VC-3a@FG and VC-3b@FG).

Figure S20 Plot of (h) 1/n versus h for the neat chicken gelatin and its composites. Where n= 1/2, 2, 2/3, and 3.

Figure S21 Plot of (h) 1/n versus h for the neat pork gelatin and its composites. Where n = 1/2, 2, 2/3, and 3.

Figure S22 Plot of (h) 1/n versus h for the neat bovine gelatin and its composites. Where n= 1/2, 2, 2/3, and 3.

Figure S23 Plot of (h) 1/n versus h for the neat fish gelatin and its composites. Where n= 1/2, 2, 2/3, and 3.

Figure S24 Plot of (h) 1/n versus h for the neat gelatins and polymer composites. Where n= 1/2, 2, 2/3, and 3.