### A Comprehensive study of facemask pyrolysis using Py-GC/MS, kinetic analysis

### and ANN modeling

### Imad A. Idrisa, Jurarat Nisamaneenatea, Duangduen Atongb, Viboon Sricharoenchaikula,c*

a Department of Environment Engineering, Faculty of Engineering, Chulalongkorn University, Bangkok 10330, Thailand

b National Metal and Materials Technology Center (MTEC), National Science and Technology Development Agency (NSTDA), Thailand Science Park, Pathum Thani 12120, Thailand

c Energy Research Institute, Chulalongkorn University, Bangkok 10330, Thailand

* Corresponding author. Tel.: +662 218 6689; Fax: +662 218 6666; E-mail: viboon.sr@chula.ac.th

| * Corresponding author: Dr. Viboon Sricharoenchaikul | E-Mail: viboon.sr@chula.ac.th |  |
| --- | --- | --- |
| Tel.: +662 218 6689; Fax: +662 218 6666 |  |  |

Supplementary Data

Fig S1. Milled facemask filters layers

Fig S2. a) FT-IR results of surgical facemask filter layers and b) ear loop

Fig S3. Change of dα/dT and Tα with conversion (α)

Py- GC/MS results of gaseous products

| Table S1. Mean peak areas % of different compound families obtained in facemask pyrolysis at 550°C. |  |
| --- | --- |
| Compound | Area % |
| Alcohol |  |
| (2,4,6-Trimethylcyclohexyl) methanol | 1.82 |
| 11-Methyldodecanol | 1.20 |
| 1-Heptanol, 2,4-diethyl- | 1.01 |
| 11-Methyldodecanol | 0.71 |
| (2,4,6-Trimethylcyclohexyl) methanol | 0.57 |
| 1-Heptanol, 2,4-diethyl- | 0.35 |
| 10-Dodecen-1-ol, 7,11-dimethyl- | 1.04 |
| Aliphatic hydrocarbons |  |
| Lineal |  |
| Propene | 8.44 |
| Pentane, 2-methyl- | 5.54 |
| 1-Pentene, 2-methyl- | 4.74 |
| 1-Pentene, 2,4-dimethyl- | 3.88 |
| 1,3-Pentadiene, 2,3-dimethyl- | 2.92 |
| 1-Hexene, 3,3-dimethyl- | 2.57 |
| Heptane, 4-methyl- | 2.33 |
| 1,5-Hexadiene, 2,5-dimethyl- | 2.27 |
| 1-Hexene, 3,3,5-trimethyl- | 2.26 |
| 2,4-Heptadiene, 2,6-dimethyl- | 3.72 |
| 2,4-Dimethyl-1-heptene | 1.89 |
| 1-Octene, 2-methyl- | 1.85 |
| Octane, 2,3,7-trimethyl- | 1.35 |
| Heptane, 3-ethyl-5-methyl- | 1.28 |
| Nonane, 2,6-dimethyl- | 2.46 |
| 1-Decene, 2,4-dimethyl- | 1.91 |
| 1-Undecene, 7-methyl- | 1.87 |
| Dodecane, 4,6-dimethyl- | 1.55 |
| Hexane, 1-(hexyloxy)-5-methyl- | 1.07 |
| Cyclic |  |
| Cyclohexane, 1,2,3,5-tetraisopropyl- | 4.24 |
| Cyclohexane, 1,3,5-trimethyl- | 3.94 |
| Cyclohexane, 2,4-diethyl-1-methyl- | 1.66 |
| Cyclooctane, 1-methyl-3-propyl- | 1.40 |
| Cyclopropane, 1-methyl-2-(1-methylpentyl)- | 1.59 |
| 1,1'-Bicyclohexyl | 1.68 |
| Cyclohexane, 1,2-diethyl-3-methyl- | 0.77 |
| Ketones |  |
| 2-Pentanone, 3-[(acetyloxy)methyl]-3,4-dimethyl- | 3.61 |
| Bicyclo[3.1.1]heptan-3-one, 6,6-dimethyl-2-(2-methylpropyl)- | 1.32 |
| Ethers |  |
| Dodecyl nonyl ether | 0.55 |
| Eicosyl octyl ether | 0.24 |
| Hexacosyl nonyl ether | 0.13 |
| Esters |  |
| Citronellyl butyrate | 1.00 |
| 6-Octenoic acid, 3,7-dimethyl-, 3,7-dimethyl-6-octenyl ester | 0.87 |
| 11,13-Dimethyl-12-tetradecen-1-ol acetate | 0.13 |

Kinetic analysis

Fig S4. Linear plots for calculation of Ea during the pyrolysis of facemask filters and ear loop blend using a) FR method, b) KAS method and c) FWO method

Criado method

The results obtained by the Criado method, also known as the master plots method, are demonstrated in Figs. S5 – S8.

Fig S5. Master plots of experimental (TG) curves at different heating rates

Fig S6. Master plots comparison of experimental and model predictions at a heating rate of 5°C/min

Fig S7. Master plots comparison of experimental and model predictions at a heating rate of 20°C/min

Fig S8. Master plots comparison of experimental and model predictions at a heating rate of 30°C/min

- ANN modeling

Table S2. hyperparameters used to tune the ANN topology

| Number of hidden layers | Number of Neurons impeded in a layer | MSE | R2 |
| --- | --- | --- | --- |
| 1 | 10 | 92 | 0.95 |
| 2 | 8 | 6.08 | 0.966 |
| 2 | 10 | 0.8834 | 0.9995 |

Fig S9. Error distribution vs conversion

Fig S10. Experimental vs predicted α in the active zone (300 – 550 °C)

Fig S11. Error distribution between the experimental and predicted weight loss data in the active zone (300 – 550 °C)