Appendix A

Supporting information

# Na-CDs as an eco-friendly and efficient corrosion inhibitor for Q235 in 1 M HCl

Liming Donga, Jingbao Wangb, Yuyue Mab, Yilei Ruana, Zhiyong Hua, Xuemei Maa

a: School of chemistry and Chemical Engineering, North University of China, Taiyuan 030051, China

b: School of Materials Science and Engineering, Beijing University of Chemical Technology, Beijing 100029, China

Table S1. Data from three weight loss measurements.

|  | Content (mg/L) | Long (mm) | Wide (mm) | High (mm) | Φ (mm) | A (cm2) | W0(g) | W(g) | Corrosion rate (g∙cm–2∙h–1) | η (%) | ΔW(g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0 | 35.2000 | 27.7333 | 2.0000 | 4.0333 | 21.7882 | 15.7494 | 14.9014 | 0.1622 | 0.0000 | 0.8480 |
|  | 50 | 35.2333 | 27.9000 | 2.0333 | 4.0333 | 21.9700 | 15.7411 | 15.6619 | 0.0150 | 0.9074 | 0.0792 |
|  | 100 | 35.3667 | 27.7333 | 2.1000 | 4.1333 | 21.9942 | 15.8540 | 15.7935 | 0.0115 | 0.9293 | 0.0605 |
|  | 150 | 35.2333 | 27.8333 | 2.1000 | 4.0667 | 21.9937 | 15.8191 | 15.7841 | 0.0066 | 0.9591 | 0.0350 |
|  | 200 | 35.2333 | 27.8333 | 2.0000 | 4.0333 | 21.8825 | 15.5173 | 15.4402 | 0.0147 | 0.9095 | 0.0771 |
| 2 | 0 | 35.3667 | 27.7333 | 2.0333 | 4.0333 | 21.9251 | 15.6959 | 14.8413 | 0.1624 | 0.0000 | 0.8546 |
|  | 50 | 35.2000 | 27.7333 | 2.0333 | 4.1333 | 21.8195 | 15.7011 | 15.6148 | 0.0165 | 0.8985 | 0.0863 |
|  | 100 | 35.3667 | 27.7333 | 2.1000 | 4.0667 | 21.9986 | 15.8212 | 15.7490 | 0.0137 | 0.9158 | 0.0722 |
|  | 150 | 35.2333 | 27.9000 | 2.0333 | 4.0333 | 21.9700 | 15.7986 | 15.7521 | 0.0088 | 0.9457 | 0.0465 |
|  | 200 | 35.2000 | 27.8333 | 2.0000 | 4.0333 | 21.8626 | 15.4800 | 15.3947 | 0.0163 | 0.8999 | 0.0853 |
| 3 | 0 | 35.3667 | 27.7333 | 2.0333 | 4.1333 | 21.9187 | 15.7011 | 14.8413 | 0.1635 | 0.0000 | 0.8598 |
|  | 50 | 35.2333 | 27.9000 | 2.0333 | 4.0667 | 21.9678 | 15.7411 | 15.6680 | 0.0139 | 0.9153 | 0.0730 |
|  | 100 | 35.2000 | 27.7333 | 2.1000 | 4.0667 | 21.8992 | 15.7251 | 15.6692 | 0.0106 | 0.9349 | 0.0559 |
|  | 150 | 35.3667 | 27.8333 | 2.0000 | 4.0333 | 21.9620 | 15.8139 | 15.7800 | 0.0064 | 0.9607 | 0.0338 |
|  | 200 | 35.2000 | 27.8333 | 2.0000 | 4.0667 | 21.8605 | 15.7199 | 15.6377 | 0.0157 | 0.9041 | 0.0822 |

Fig S1. Freundlich isotherm equation.

Table S2. In the original state, EDS data were obtained by soaking 1M HCl for 24h and soaking 1M HCl containing 150mg/L Na-CDs for 24h.

| condition | element | wt% | Wt % Sigma | At% |
| --- | --- | --- | --- | --- |
| Original | C | 3.44 | 0.2 | 14.12 |
|  | O | 0.32 | 0.07 | 0.99 |
|  | Fe | 96.24 | 0.21 | 84.89 |
| 1 M HCl | C | 3.69 | 0.28 | 11.12 |
|  | O | 15.34 | 0.14 | 34.71 |
|  | Cl | 4.54 | 0.06 | 4.63 |
|  | Fe | 76.43 | 0.27 | 49.54 |
| 150mg/L Na-CDs | C | 5.72 | 0.26 | 20.68 |
|  | O | 2.84 | 0.08 | 7.69 |
|  | Na | 0 | 0.07 | 0 |
|  | Cl | 1.34 | 0.04 | 1.65 |
|  | Fe | 90.1 | 0.26 | 69.99 |

Fig S2. (a) In its original state, (b)1M HCl soaked for 24h, (c) Soak in 1M HCl containing 150mg/L Na-CDs for 24h.

Fig S3. Morphology of Q235 carbon steel soaked in 1 M HCl solution containing other concentrations of Na-CDs for 24h ：(a) and (a1) 200 mg/L, (b) and (b1) 100 mg/L, (c) and (c1) 50 mg/L.

Fig S4. Morphology of Q235 carbon steel soaked in 1 M HCl solution with 150mg/L concentration of Na-CDs for 24h without rinsing (a) (a1) and slowly rinsed with deionized water (b) (b1), as well as EDS data, (a2) without rinsing, (b2) slowly rinsed with deionized water.

Corresponding author.

E-mail: maxuemei@nuc.edu.cn