Supporting Information

Photothermal-triggered release of alkyl radicals hydrogel via versatile carbon dots chelating Ag+ and its synergistic anti-bacterial and biofilm activities

Wen Liua,b,d*, Baizhi Sub, Hua Songb, Xueyun Zhangb, Guodong Renb, Xuewei Wangb, Lili Yanb,d, Sufang Mab, Lihong Lib,d, Lixia Guoc, Shuming Xue, Boye Zhangb, Haipeng Diaob,d*, Zhifang Wua, Sijin Lia, Chengwu Zhangb

a The First Hospital of Shanxi Medical University, The First Clinical Medical School of Shanxi

Medical University, Taiyuan 030001, P.R. China

b School of Basic Medical Sciences, Shanxi Medical University, Taiyuan 030001, P.R. China

c college of pharmacy, Shanxi Medical University, Taiyuan 030001, P.R. China

d Key Laboratory of Cellular Physiology at Shanxi Medical University, Ministry of Education,

Taiyuan 030001, P. R. China

e Women health center of Shanxi, Taiyuan 030013, P.R. China

* Corresponding authors.

E-mail addresses: liuwen@sxmu.edu.cn (W. Liu), diaohp@sxmu.edu.cn (H. Diao)

Fig.S1-Fig.S10

Fig. S1. Fluorescence intensity of PTCDs under different synthesis conditions. (A) different reaction temperatures; (B) different reaction times; (C) the molar ratio of different reactants.

Fig. S2. The high resolution C1S XPS spectrum (A), N1S XPS spectrum (B) and O1S XPS spectrum (C).

Fig. S3. (A) Fluorescence emission spectra of PTCDs at different excitation wavelengths; (B) Effect of ionic strength (NaCl) on fluorescence intensity of PTCDs; (C) Effect of different pH on fluorescence intensity of PTCDs; (D) The time-dependence of fluorescent intensity of PTCDs at the various time.

.

Fig. S4. The absorption spectra of PTCDs incubated with different concentrations of Ag+.

Fig. S5. Alkyl radicals produced by AIPH (A) at different concentrations in a water bath for 55 ℃ and (B) at different times in a water bath for 55 ℃ and (C) at different temperatures and (D) at different pH in a water bath for 55 ℃. The insets: the color change of the solution before and after ABTS interacted with the alkyl radical produced by AIPH.

Fig. S6. (A) Photographs of hydrogels in the gel and sol states, (B, C) High-resolution SEM of Hydrogel and composite hydrogel (PTCDs@Ag-AIPH Hydrogel), (D) Swelling rates of Hydrogel and PTCDs@Ag-AIPH Hydrogel, (E, F) Rheological properties of PTCDs@Ag-AIPH Hydrogel: strain scan (E), frequency scan (F).

Fig. S7. Cytotoxicity tests of PTCDs at different concentrations and Hydrogels.

Fig. S8. (A) The plate photos of S. aureus cocultured with PBS, AIPH and Hydrogel@AIPH under 660 nm laser irradiation or not ([AIPH]=0.80 mg/mL). The final bacteria suspension concentrations were adjusted to 106 CFU·mL−1. (B) The viability rate of the different treatments against S. aureus.

Fig. S9. The difference of white blood cell value in mice before and after cyclophosphamide induction (**p<0.01).

Fig. S10. H&E staining analyses of major organs and infected wound tissues in mice with various treatments. Scale bar = 200 μm.