Supporting Information

Insights on Z-scheme interfacial charge transfer of TiO2-NRAs/BiOI-NFs/Au-NPs nanoheterostructures and unveiling enhanced photoelectrochemical performances

Zhufeng Shao†,*, Yonglong Zhang†,, Xiujuan Yang†, Guoyang Yu, Yunfei Song, Min Zhong, Xiaoming Xiu†,*

†College of physical science and technology, Bohai University, Jinzhou, Liaoning, 121000, China

College of chemistry and materials engineering, Bohai University, Jinzhou, Liaoning, 121000, China

National key laboratory of shock wave and detonation physics, Institute of fluid physics, China academy of engineering physics, Mianyang, China

*Corresponding authors Email: jinhaiyuan@126.com, xiuxiaomingdl@126.com

Figure S1. The X-ray photoelectron spectroscopy (XPS) survey spectra of pristine TiO2-NRAs and TiO2-NRAs/BiOI-NFs/Au-NPs nanocomplex (a), and the high-resolution XPS spectra of (b) Ti 2p, (c) Bi 4f, (d) I 3d, (e) Au 4f, respectively.

Figure S2. Time-resolved PL (TRPL) spectra of the pristine TiO2-NRAs, pure BiOI-NFs, BiOI-NFs/Au-NPs, TiO2-NRAs/BiOI-NFs, and TiO2-NRAs/BiOI-NFs/Au-NPs nanoheterojunctions, respectively.

Figure S3. N2 adsorption-desorption isotherms of pristine TiO2-NRAs, pure BiOI-NFs, BiOI-NFs/Au-NPs, TiO2-NRAs/BiOI-NFs, and TiO2-NRAs/BiOI-NFs/Au-NPs composites.

Figure S4. (a)-(e) Cyclic voltammograms at different scan rates increasing from 20 mV/s to 100 mV/s, and (f) current density differences of pristine TiO2-NRAs, pure BiOI-NFs, BiOI-NFs/Au-NPs, TiO2-NRAs/BiOI-NFs, and TiO2-NRAs/BiOI-NFs/Au-NPs plotted against scan rates.

Figure S5. Transient photocurrent response (a), and electrochemical impedance spectra (b) of pristine TiO2-NRAs, pure BiOI-NFs, BiOI-NFs/Au-NPs, TiO2-NRAs/BiOI-NFs, and TiO2-NRAs/BiOI-NFs/Au-NPs, respectively.

Figure S6. DMPO spin-trapping ESR spectra of O2- and OH under simulated solar light irradiation illustrated in (a) and (c), and in dark conditions of (b) and (d) for as-obtained pristine TiO2-NRAs, pure BiOI-NFs, BiOI-NFs/Au-NPs, TiO2-NRAs/BiOI-NFs, and TiO2-NRAs/BiOI-NFs/Au-NPs, respectively.

Table S1. Surface atomic ratios Ti3+/Ti4+ of Ti 2p XPS spectra for spin-orbit splitting doublets Ti 2p1/2 and Ti 2p3/2 towards to the specimens of pure TiO2-NRAs, binary TiO2-NRAs/BiOI-NFs, and ternary TiO2-NRAs/BiOI-NFs/Au-NPs, respectively.

| as-prepared samples | assignment | binding energy (eV) | surface atomic ratio Ti3+/Ti4+ |
| --- | --- | --- | --- |
| TiO2-NRAs | Ti 2p3/2 | 459.0 | 0.906 |
|  | Ti3+ 2p3/2 | 458.7 |  |
|  | Ti4+ 2p3/2 | 459.1 |  |
|  | Ti 2p1/2 | 464.7 |  |
|  | Ti3+ 2p1/2 | 464.2 |  |
|  | Ti4+ 2p1/2 | 465.0 |  |
| TiO2-NRAs/BiOI-NFs | Ti 2p3/2 | 458.4 | 1.04 |
|  | Ti3+ 2p3/2 | 458.4 |  |
|  | Ti4+ 2p3/2 | 458.8 |  |
|  | Ti 2p1/2 | 464.2 |  |
|  | Ti3+ 2p1/2 | 463.9 |  |
|  | Ti4+ 2p1/2 | 464.5 |  |
| TiO2-NRAs/BiOI-NFs/Au-NPs | Ti 2p3/2 | 458.7 | 1.19 |
|  | Ti3+ 2p3/2 | 458.3 |  |
|  | Ti4+ 2p3/2 | 458.9 |  |
|  | Ti 2p1/2 | 464.4 |  |
|  | Ti3+ 2p1/2 | 463.5 |  |
|  | Ti4+ 2p1/2 | 464.4 |  |

Table S2. Surface Vo/(Lo + Ao) molar ratios of O 1s XPS spectra for the specimens of pristine TiO2-NRAs, pure BiOI-NFs, BiOI-NFs/Au-NPs, TiO2-NRAs/BiOI-NFs, and TiO2-NRAs/BiOI-NFs/Au-NPs, respectively.

| As-obtained specimens | Assignment | Binding energy (eV) | Vo/(Lo + Ao) |
| --- | --- | --- | --- |
| pristine TiO2-NRAs | Lo | 529.7 | 0.109 |
|  | Vo | 531.2 |  |
|  | Ao | 532.2 |  |
| pure BiOI-NFs | Lo | 529.9 | 0.087 |
|  | Vo | 530.9 |  |
|  | Ao | 532.1 |  |
| BiOI-NFs/Au-NPs | Lo | 530.0 | 0.186 |
|  | Vo | 531.2 |  |
|  | Ao | 532.1 |  |
| TiO2-NRAs/BiOI-NFs | Lo | 530.1 | 0.313 |
|  | Vo | 531.1 |  |
|  | Ao | 532.4 |  |
| TiO2-NRAs/BiOI-NFs/Au-NPs | Lo | 530.3 | 0.367 |
|  | Vo | 531.6 |  |
|  | Ao | 532.4 |  |

Table S3 Fast and slow decay times along with their amplitudes and average PL lifetime (avg) for as-obtained specimens, respectively.

| Sample code | ex (nm) | em (nm) | 1 (ns) | A1/(A1+A2) (%) | 2 (ns) | A2/(A1+A2) (%) | avg (ns) | (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| pristine TiO2-NRAs | 375 | 396 | 4.26 | 25.7 | 0.56 | 74.3 | 3.25 | 4.3 |
| pure BiOI-NFs | 375 | 425 | 4.35 | 26.5 | 0.63 | 73.5 | 3.27 | 4.9 |
| BiOI-NFs/Au-NPs | 375 | 608 | 4.42 | 28.6 | 0.68 | 71.4 | 3.32 | 5.8 |
| TiO2-NRAs/BiOI-NFs | 375 | 639 | 4.63 | 38.3 | 0.73 | 61.7 | 3.65 | 8.9 |
| TiO2-NRAs/BiOI-NFs/Au-NPs | 375 | 659 | 4.88 | 41.5 | 0.76 | 58.5 | 4.16 | 9.9 |

Table S4 BET surface area (SBET), pore volumes (Vp), and the electrochemical double-layer capacity (Cdl) of pristine TiO2-NRAs, pure BiOI-NFs, BiOI-NFs/Au-NPs, TiO2-NRAs/BiOI-NFs, and TiO2-NRAs/BiOI-NFs/Au-NPs, respectively.

| Specimens | SBET (m2﹒g-1) | Vp (cm3﹒g-1) | Cdl (μF﹒cm-2) |
| --- | --- | --- | --- |
| pristine TiO2-NRAs | 22.8 | 0.06 | 10.27 |
| pure BiOI-NFs | 9.8 | 0.02 | 43.31 |
| BiOI-NFs/Au-NPs | 15.5 | 0.03 | 71.19 |
| TiO2-NRAs/BiOI-NFs | 28.7 | 0.13 | 87.92 |
| TiO2-NRAs/BiOI-NFs/Au-NPs | 37.9 | 0.18 | 96.36 |